Supplementary

Preparation of carboxymethyl cellulose (CMC) derived from palm fiber waste: Effect of ozone pretreatment on CMC properties

Agustu Sholeh Pujokaroni1,2, Hideaki Ichiura3,*

1 The United Graduate School of Agricultural Sciences, Ehime University, 3-5-7 Tarumi, Matsuyama, Ehime 790-8566, Japan

2 Faculty of Agriculture, Mulawarman University, Jl. Kuaro, Gn. Kelua, Kec. Samarinda Ulu, Kota Samarinda, Kalimantan Timur 75119, Indonesia

3 Faculty of Agriculture and Marine Science, Kochi University, 200 Monobe-Otsu, Nankoku, Kochi 783-8502, Japan

Table S1 DP and carboxylate content of cellulose extracted from palm fiber treated with ozone

| Ozone treatment time for extracted cellulose (h) | DP | Carboxylate contents (mmol/g) |
| --- | --- | --- |
| 0 | 1012 | 0.45 |
| 1 | 294 | 1.38 |
| 3 | 207 | 1.82 |
| 5 | 185 | 2.05 |

(c)

(d)

(g)

(h)

(a)

(b)

Figure S1 Images and SEM Images of palm fiber [(a) and (b)], extracted cellulose [(c) and (d), oxidized cellulose [(e) and (f)] and CMC-10-(3) [(g) and (h)].

(f)

(e)

Figure S2 XRD of (a) extracted cellulose, (b) oxidized cellulose and (c) CMC-10-(3).

(a)

(b)

(c)