Supplementary Information

Boosting ionic conductivity of antiperovskite solid electrolyte by potassium ions substitution for cation clusters

Lei Gao, Hao Zhang, Songbai Han, Jinlong Zhu, Liping Wang, Shuai Li, Ruo Zhao, Song Gao, Yonggang Wang, Ruqiang Zou, Yusheng Zhao

Fig. 1 DSC curve of (Li2OH)0.95K0.05Cl in the range between RT and 350 C.

Fig. 2 DSC curve of (Li2OH)0.9K0.1Cl in the range between RT and 350 C.

Table 1. Crystallographic information for Li2OHCl from Rietveld refinement of PXRD.

| Total refinement results: Rwp:4.06; Rp:2.18; GOF:4.78 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Li2OHCl, orthorhombic, PmC21, a = 3.8739 Å, b = 3.8251 Å, c = 7.9997 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 2b | 0.5 | 0.49778 | 0.25 | 0.813 | 0.023 |
| O | 2a | 0 | -0.01706 | 0 | 1.0 | 0.029 |
| Li1 | 2a | 0 | 0.05229 | 0.25 | 0.911 | 0.060 |
| Li2 | 2b | 0.5 | 0.06188 | 0 | 0.911 | 0.138 |

Table 2. Crystallographic information for (Li2OH)0.99K0.01Cl from Rietveld refinement of PXRD.

| Total refinement results: Rwp:3.98; Rp:2.49; GOF:4.15 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| (Li2OH)0.99K0.01Cl, cubic, Pm-3m, a = 3.9072 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 1b | 0.5 | 0.5 | 0.5 | 1 | 0.015 |
| O | 1a | 0 | 0 | 0 | 0.99[a] | 0.031 |
| Li | 3d | 0.5 | 0 | 0 | 0.659 | 0.078 |
| K | 1a | 0 | 0 | 0 | 0.01[a] | 0.010 |

Table 3. Crystallographic information for (Li2OH)0.95K0.05Cl from Rietveld refinement of PXRD.

| Total refinement results: Rwp:3.7; Rp:2.24; GOF:3.84 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| (Li2OH)0.95K0.05Cl, cubic, Pm-3m, a = 3.9036 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 1b | 0.5 | 0.5 | 0.5 | 1 | 0.031 |
| O | 1a | 0 | 0 | 0 | 0.9339 | 0.045 |
| Li | 3d | 0.5 | 0 | 0 | 0.622 | 0.059 |
| K | 1a | 0 | 0 | 0 | 0.0661 | 0.036 |

Table 4. Crystallographic information for (Li2OH)0.9K0.1Cl from Rietveld refinement of PXRD.

| Total refinement results: Rwp:3.69; Rp:2.25; GOF:2.73 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| (Li2OH)0.9K0.1Cl, cubic, Pm-3m, a = 3.8994 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 1b | 0.5 | 0.5 | 0.5 | 1 | 0.035 |
| O | 1a | 0 | 0 | 0 | 0.87 | 0.061 |
| Li | 3d | 0.5 | 0 | 0 | 0.579 | 0.062 |
| K | 1a | 0 | 0 | 0 | 0.129 | 0.013 |

[a]: For (Li2OH)0.99K0.01Cl, because the amount of doped K is low, the occupancy of O and K is set fixed during refinements.

Table 5. Crystallographic information for Li2OHCl from small-box least square refinement of PDF.

| Total refinement results: Rw:14.5 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Li2OHCl, orthorhombic, PmC21, a = 3.8960 Å, b = 3.8266 Å, c = 8.0334 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 2b | 0.5 | 0.5 | 0.25 | 0.951 | 0.017 |
| O | 2a | 0 | 0 | 0 | 1 | 0.033 |
| Li1 | 2a | 0 | 0 | 0.25 | 1 | 0.038 |
| Li2 | 2b | 0.5 | 0 | 0 | 0.960 | 0.119 |

Table 6. Crystallographic information for (Li2OH)0.99K0.01Cl from small-box least square refinement of PDF.

| Total refinement results: Rw:16.0% |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| (Li2OH)0.99K0.01Cl, cubic, Pm-3m, a = 3.9161 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 1b | 0.5 | 0.5 | 0.5 | 1 | 0.021 |
| O | 1a | 0 | 0 | 0 | 0.99[b] | 0.034 |
| Li | 3d | 0.5 | 0 | 0 | 0.615 | 0.075 |
| K | 1a | 0 | 0 | 0 | 0.01[b] | 0.010 |

Table 7. Crystallographic information for (Li2OH)0.95K0.05Cl from small-box least square refinement of PDF.

| Total refinement results: Rw:15.7% |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| (Li2OH)0.95K0.05Cl, cubic, Pm-3m, a = 3.9133 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 1b | 0.5 | 0.5 | 0.5 | 1 | 0.022 |
| O | 1a | 0 | 0 | 0 | 0.942 | 0.028 |
| Li | 3d | 0.5 | 0 | 0 | 0.573 | 0.067 |
| K | 1a | 0 | 0 | 0 | 0.058 | 0.104 |

Table 8. Crystallographic information for (Li2OH)0.9K0.1Cl from small-box least square refinement of PDF.

| Total refinement results: Rw:15.2% |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| (Li2OH)0.9K0.1Cl, cubic, Pm-3m, a = 3.9088 Å |  |  |  |  |  |  |
| Atoms | Wyckoff | x | y | z | Occupancy | Uiso |
| Cl | 1b | 0.5 | 0.5 | 0.5 | 1 | 0.023 |
| O | 1a | 0 | 0 | 0 | 0.892 | 0.025 |
| Li | 3d | 0.5 | 0 | 0 | 0.498 | 0.066 |
| K | 1a | 0 | 0 | 0 | 0.121 | 0.092 |

[b]: For (Li2OH)0.99K0.01Cl, because the amount of doped K is low, the occupancy of O and K is set fixed during PDF refinements.

Fig. 3 a-d Nyquist plots of Li2OHCl and (Li2OH)1-xKxCl SSEs measured in the temperature range from 25 to 120 C.

Fig. 4 a Differential capacity curves of the LiFePO4 | Li ASSLB based on (Li2OH)0.99K0.01Cl at 18, 36, 54, and 72 mA g-1 current rates. b Differential cacpacity curves of the LiFePO4 | Li ASSLB based on (Li2OH)0.99K0.01Cl at different cycles.

Fig. 5 XPS of (Li2OH)1-xKxCl, the peaks intensity of potassium (K) 2p increases with the increase of K-doping.

Fig. 6 The lattice parameters of (Li2OH)1-xKxCl at RT decrease with the increase of K-doping according to the PDF refinement.

Fig. 7 The O(K)-Cl interatomic distances of (Li2OH)1-xKxCl at RT decrease with the increase of K-doping according to the PDF refinement.

Fig. 8 The O(K)-O(K) interatomic distances of (Li2OH)1-xKxCl at RT decrease with the increase of K-doping according to the PDF refinement.