Preparation of low-cost functionalized diatomite and its effective removal of ammonia nitrogen from wastewater

Shuju Fang1†, Gufeng Li1†; Hongyu Shi1; Junxiu Ye1; Hongbin Wang1; Xuemei Ding1; Lijun Luo1; Guizhen Li1; Min Yang1*

(1 Key Laboratory of Resource Clean Conversion in Ethnic Regions, Education Department of Yunnan, School of Chemistry and Environment, Yunnan Minzu University, Kunming 650500, P. R. China)

Email:

Gufeng Li1† - 1250191263@qq.com

Min Yang1* - 826677468@qq.com

† These authors contributed equally to this work

* Corresponding author

.

Captions of Supporting Figures

Fig. S1. N2 adsorption/desorption isotherms of the DTR (a), DTA (b), DTA-Na (c) and DTCA-Na (d).

Fig. S2. Effect of concentration of the NaCl reagent on the desorption rate and removal efficiency.

Fig. S3. (a) Effect of contact time at different temperatures on the adsorption capacity of the DTCA-Na, (b) The pseudo-first-order kinetics model fitting, (c) The pseudo-second-order kinetics model fitting, (d) The intraparticle diffusion model fitting.

Fig. S4. (a) The adsorption isotherms of NH+ 4-N on the DTCA-Na at 25 ℃, (b) Non-linear fitting curve of Freundlich model, (c) Non-linear fitting curve of Langmuir model, (d) Non-linear fitting curve of Temkin model.

Captions of Supporting Tables

Table S1 Removal efficiency of NH+ 4-N by different diatomite.

Table S2 Effect of different modifiers on NH+ 4-N removal efficiency.

Table S3 Effect of different desorption reagents on the desorption rate and removal efficiency.

Supporting Figures

Fig. S1. N2 adsorption/desorption isotherms of the DTR (a), DTA (b), DTA-Na (c) and DTCA-Na (d).

Fig. S2. Effect of concentration of the NaCl reagent on the desorption rate and removal efficiency.

Fig. S3. (a) Effect of contact time at different temperatures on the adsorption capacity of the DTCA-Na, (b) The pseudo-first-order kinetics model fitting, (c) The pseudo-second-order kinetics model fitting, (d)The intraparticle diffusion model fitting.

Fig. S4. (a) The adsorption isotherms of NH+ 4-N on the DTCA-Na at 25 ℃, (b) Non-linear fitting curve of Freundlich model, (c) Non-linear fitting curve of Langmuir model, (d) Non-linear fitting curve of Temkin model.

Supporting Tables

Table S1

Removal efficiency of NH+ 4-N by different diatomite

| Adsorbent | Dosage of adsorbent (g) | The removal efficiency (%) |
| --- | --- | --- |
| DTR DTW DTA | 0.80 0.80 0.80 | 0.74 1.72 43.51 |

Table S2

Effect of different modifiers on NH+ 4-N removal efficiency

| Modifier | Dosage of adsorbent (g) | The mass fraction of the modifier (%) | The removal efficiency (%) |
| --- | --- | --- | --- |
| La2O3 NaCl LaCl3 | 0.80 0.80 0.80 | 5.00 5.00 5.00 | 69.76 73.64 2.69 |

Table S3

Effect of different desorption reagents on the desorption rate and removal efficiency

| Regenerant | The desorption rate (%) | The removal efficiency (%) |
| --- | --- | --- |
| NaCl | 96.19 | 81.42 |
| Na2CO3 | 87.04 | 70.73 |
| NaOH | 80.18 | 57.12 |
| HCl | 77.89 | 27.96 |
| Distilled water | 11.57 | 4.63 |

The mass fraction of all regenerants were 5.00%.