Supporting information

Two Cu(I\II) coordination polymers for photocatalytic degradation of organic dyes and efficient detection of Fe3+ ions

Chenyan Xu1#, Wenqian Chen1#, Jiajun Wang1*, Qiuyu Wu1, Pengyan Wu2*, Liang Tang1*

- Key Laboratory of Organic Compound Pollution Control Engineering, Ministry of Education, School of Environmental and Chemical Engineering, Shanghai University, Shanghai 200444, PR China

- School of Chemistry and Materials Science, Jiangsu Normal University, 221116, PR China

# Equal contribution

* Corresponding author. E-mail addresses: Jiajun Wang (email: wangjiajun123@shu.edu.cn) Pengyan Wu (email: wpyan@jsnu.edu.cn) Liang Tang (email: tang1liang@shu.edu.cn)

Figure S1. H-bonded network of Cu-dpe(I) (O-H…O in the orthophosphate). Hydrogen bonds are highlighted with a red dotted line. Cu, P, N, O, C and H atoms are shown in purple, green, light blue, red, gray and light pink, respectively. The unit of the H-bond distance is Å.

Figure S2. TGA of Cu-dpe(I) (red) and Cu-dpe(II) (blue).

Figure S3. (a) Infra-red (IR) spectroscopy of ligand dpe (black), Cu-dpe(I) (red) and Cu-dpe(II) (blue). (b) Raman of ligand dpe (black), Cu-dpe(I) (red) and Cu-dpe(II) (blue).

Figure S4. (a) UV-vis absorption spectra of ligand dpe (black), Cu-dpe(I) (red) and Cu-dpe(II) (blue). (b) The Tauc plot (αhv)1/2 vs (hv) of Cu-dpe(I) (red) and Cu-dpe(II) (blue), where α is absorbance.

Figure S5. Solid-state fluorescence intensity of ligand dpe (black), Cu-dpe(I) (red) and Cu-dpe(II) at a room temperature.

Figure S6. A control experiment: fluorescence intensities of Cu-dpe(I) in aqueous solution (black), addition of 200 L M(NO3)n solutions (1 × 10−3 mol L−1; red), and with Fe3+ ions (1 × 10−3 mol L−1; blue) under an excitation of 381 nm.

Figure S7. PXRD patterns of Cu-dpe(I) (black) and Cu-dpe(I) after dispersed in Fe3+ solution (10−3 M) for 24 hours (red).

Table S1. Crystallographic data for Cu-dpe(I) and Cu-dpe(II).

| Compound | Cu-dpe(I) | Cu-dpe(II) |
| --- | --- | --- |
| Empirical Formula | C66H65Cu5N11O27P5 | C12H22CuN2O10P |
| Formula weight (g mol−1) | 1916.84 | 448.82 |
| Crystal system | Monoclinic | Monoclinic |
| Space group | C2/c | C2 |
| a (Å) | 34.041 (7) | 8.2343(19) |
| b (Å) | 17.776 (4) | 26.830(6) |
| c (Å) | 26.056 (5) | 9.490(2) |
| α (°) | 90 | 90.00 |
| β (°) | 93.06 (3) | 115.245(2) |
| γ (°) | 90.00 | 90.00 |
| Volume (Å3) | 15744(5) | 1896.4(8) |
| Z | 8 | 4 |
| ρ (g cm−3) | 1.617 | 1.572 |
| (mm−1) | 1.516 | 1.288 |
| F (000) | 7792.0 | 928.0 |
| GOF | 1.127 | 1.032 |
| R1 | 0.1019 | 0.0346 |
| wR2 | 0.3270 | 0.0932 |

Selected bond length (Å) and bond angle (º) for Cu-dpe(I).

| Cu(1) - N(1) | 1.919 (5) | N(1) - Cu(1) - O(1) | 103.689 (18) |
| --- | --- | --- | --- |
| Cu(1) - O(1) | 2.238 (4) | N(1) - Cu(1) - N(2) | 153.2 (2) |
| Cu(1) - N(2) | 1.917 (5) | O(1) - Cu(1) - N(2) | 103.03 (18) |
| Cu(2) - N(3) | 1.907 (5) | N(3) - Cu(2) - O(2) | 105.13 (18) |
| Cu(2) - O(2) Cu(2) - N(4) Cu(3) - N(6) Cu(3) - O(3) Cu(3) - N(5) Cu(4) - N(8) Cu(4) - O(4) Cu(4) - N(7) Cu(5) - O(5) Cu(5) - N(9) Cu(5) - N(10) | 2.222 (4) 1.922 (5) 1.915 (5) 2.250 (4) 1.924 (4) 1.922 (5) 2.334 (5) 1.921 (5) 2.238 (4) 1.914 (5) 1.917 (5) | N(3) - Cu(2) - N(4) N(4) - Cu(2) - O(2) N(6) - Cu(3) - N(5) N(6) - Cu(3) - O(3) N(5) - Cu(3) - O(3) N(8) - Cu(4) - O(4) N(7) - Cu(4) - N(8) N(7) - Cu(4) - O(4) N(9) - Cu(5) - O(5) N(9) - Cu(5) - N(10) N(10) - Cu(5) - O(5) | 152.8 (2) 102.01 (18) 153.8 (2) 105.07 (18) 101.06 (17) 104.08 (19) 152.9 (2) 102.04 (19) 105.78 (19) 153.0 (2) 101.07 (18) |

Selected bond length (Å) and bond angle (º) for Cu-dpe(II).

| Cu(1) - O(51) | 1.948 (2) | O(51) - Cu(1) - N(1) | 89.3 (4) |
| --- | --- | --- | --- |
| Cu(1) - N(1) | 2.026 (11) | O(51) - Cu(1) - N(9) | 89.6 (4) |
| Cu(1) - N(9) | 2.076 (14) | O(51) - Cu(1) - O(7w) | 112.38 (10) |
| Cu(1) - O(1) | 1.938 (2) | N(1) - Cu(1) - N(9) | 175.75 (12) |
| Cu(1) - O(7w) | 2.307 (3) | N(1) - Cu(1) - O(7w) | 88.1 (4) |
|  |  | N(9) - Cu(1) - O(7w) | 88.5 (4) |
|  |  | O(1) - Cu(1) - O(51) O(1) - Cu(1) - N(1) O(1) - Cu(1) - N(9) O(1) - Cu(1) - O(7w) | 154.94 (11) 92.4 (4) 90.4 (4) 92.67 (10) |

| Compounds | Removal efficiencies & Time | Reference |
| --- | --- | --- |
| [Cu(tptc)0.5(bpy)(H2O)]n | 90.07%, 120 min，Xe lamp (250 W) | Inorg. Chem. Commun, 2020, 119, 108121 |
| ### [Zn2(bbmb)2(tdc)2]·2H2O | 87.00%, 120 min,Hg lamp (500 W) | Inorg.Chem. Commun, 2019, 106, 81-85 |
| [Ni(4-pmp)(H2O)3] | 93.93%, 100 min,Xe lamp (300 W) | Inorg.Chem. Commun, 2020, 119, 108123 |
| {[Zn3(mtrb)3(btc)2]·3H2O}n | 64.30%, 180 min, Xe lamp | Dalton Transactions, 2018, 47, 6189-6198 |
| [1-D [Cu(tba)2(H2O)]⋅2H2O | 84.90%, 90 min,Hg lamp (300 W) | Colloids Surf A Physicochem Eng Asp, 2020, 603, 125147 |
| Cu-dpe(I) | 88.10%, 120 min,LED | This work |
| Cu-dpe(II) | 97.20%, 120 min,LED | This work |

Table S2. Degradation rate of the reported CPs for methylene blue.

| Compounds | Quenching Constant (Ksv / M−1) | Reference |
| --- | --- | --- |
| [Zn5(hfipbb)4(trz)2(H2O)2] | 4.09 104 | Inorg. Chem., 2016, 5, 10580-10586 |
| ### Eu–HODA | 2.09 104 | Inorg. Chem., 2016, 55, 12660–12668 |
| [Zn2(L)2(bpe)2(H2O)2] | 2.395 103 | Dalton Trans., 2015, 44, 18795–18803 |
| {[Cd(L)(BPDC)]·2H2O}n | 6.4 103 | Cryst. Growth Des., 2016, 17, 67-72 |
| {[Cd(L)(SDBA)(H2O)]·0.5H2O}n | 4.97 103 | Cryst. Growth Des., 2016, 17, 67-72 |
| H3O[In3(dcpy)4(OH)2]·3DMF·4H2O | 4.3 103 | Inorg. Chem., 2018, 57, 15262-15269 |
| {[Cd(1,4-ndc)(3-abit)].H2O}n | 9.54 103 | New. J. Chem., 2017, 41, 8107-8117 |
| {[Zn2(1,4-ndc)2(3-abpt)]·2DMF}n | 2.38 104 | New. J. Chem., 2017, 41, 8107-8117 |
| Cu-dpe(I) | 1.25 104 | This work |

Table S3. Quenching constants of the reported LCPs for Fe3+ in aqueous solution.