Supplementary Materials for

A mesoscale self-assembly into bulk bassanite via delicate control of water activity to mimic biomineralization

Chunli Wang1, 2, Xuelu Ma3, Zhihao Zhang1, Hai Xiao4, Xianlai Zeng5, Jing Zhang1, 2, *, Zhang Lin1, 2, *

* Corresponding authors: jingzhang@rcees.ac.cn (J. Z.); zhang_lin@csu.edu.cn (Z. L.)

The PDF file includes:

Supplementary methods and thermodynamic model

Tables S1 to S2

Figs. S1 to S14

Supplementary methods

Distribution of initial nanoparticles

The diameter and concentration of nanoparticles in suspension were determined using Nano Sight NTA technology (NS500, Bruker, Germany).1

Precipitation of CaSO4 particles in n-propanol (NPA) solution

Bassanite precursors were synthesized by reacting 5 ml n-propanol (NPA) solutions of CaCl2 (0.1M) and 26 μl H2SO4 (2 vol% H2O) at 22 oC. Then, different amounts of ultrapure water, final water weight fractions are ranging from 0 to 19.3 wt%, were added into the above suspension. All the operations were done at room temperature. All the reagents used in this study were purchased from Sino Pharm Chemical Reagent Co., Ltd., China.

Surface structure screening

All the candidate slab structures were generated from the conventional cell using the pymatgen package 2. The Wulff construction indicates that the distance of a facet from the crystal center is proportional to the surface energy of that facet, and the inner convex hull of all facets forms the Wulff shape3. Here, we use the methodology developed by Miracle-Soleto to construct the Wulff shape4. The Wulff shape provides the area fraction fhklA of each symmetrically distinct facet under equilibrium conditions. The weighted surface energy γ can be defined by using the fraction, as given by the following equation:

γ=hklγhklAhklΣAhkl=hklγhklfhklA#(1-1)

where γ is used as a basis for comparison with experimentally determined surface energies. γhkl is the surface energy of a unique facet existing in the Wulff shape, Ahkl is the total area of all facets in the {hkl} family in the Wulff shape, and fhklA is the area fraction of the {hkl} family in the Wulff shape5,6. The excess energy of surface atoms is important in understanding the crystal’s equilibrium shape and a variety of factors, such as the broken bonds yielding undercoordinated atoms, can significantly affect the surface energy. Therefore, we considered all the possible bond-breaking modes on these selected surfaces, where the reconstruction of the surface atom was performed based on DFT. These calculated surface energies are arranged and combined to fit the morphology of the experiment by plotting the Wulff shape. The finally selected surfaces are shown in Supplementary Fig. 7 and 8.

XRD refinement

Structural refinements of X-ray diffraction were made using the Fullprof suite7. We first prepared a batch of samples by mixing bassanite and gypsum with a different percentage. These samples were used to perform the structural refinement to get a series of phase contents, which were then used to fit the real phase and calculate the weight percentage of different phases (Supplementary Fig. 12). Using this coefficient, the simulation of experimental XRD date was performed to quantify the phase content of bassanite and gypsum.

Thermodynamic model

The total Gibbs free energies (ΔG) of the water-driven aggregation and coalescence of bassanite nanoparticles (BPs) either to directly form bulk bassanite or to phase transform into gypsum by adding a different amount of water are discussed below.

Based on the experimental results, we consider the formation of bulk bassanite and gypsum via nucleation, aggregation and further phase transformation of BPs. As schemed in Supplementary Fig. 9, the total Gibbs energy variation ΔG will consequently have three components associated with (1) formation of BPs (ΔGbp), (2) aggregation of the BPs into primary nanorods (PNs) (ΔGass-1), and (3) either further aggregation of x nanorods into secondary rod-shaped bassanite mesocrystal (ΔGass-2) when adding aa small amount of water (e.g. < 3.85 wt%), or conversion of the assembly into the final gypsum phase (ΔGgyp) at the higher water ratios.

The formation of BPs can be modeled in terms of classical nucleation theory, where the Gibbs energy variation (ΔGbp) is a function described by the radius of bassanite particle (Rbp), Gibbs energy gain per unit volume of the formed phase (gbp), and the interfacial tension between the primary particle and the solvent (γbp).

∆Gbp=43πRbp3gbp+4πRbp2γbp#2-1

The aggregation of the BPs into PNs is assumed to not involve a change in both the bulk energy and the interfacial tension, but simply a decrease of the interfacial energy due to a decrease in the interfacial area. Assuming the PN to be a cylinder with a cross-section radius Rpn and a height Hpn, composing of n=πRpn2Hpn43πRbp3 BPs with radius Rbp. The Gibbs energy variation on the aggregation (ΔGass-1) can be expressed as:

∆Gass-1=γbp2πRpn2+2πRpnHpn-4πnRbp2#2-2

Where 2πRpn2+2πRpnHpn-4πnRbp2 is the difference of surface area from single PN to n BPs, simplifying to:

Δass-1=πRpn28Rpngbp+18γbp#2-3

When a certain amount of water (e.g. < 3.85 wt%) is added into the PNs colloid, it will initiate the secondary aggregation of the nanorods into the rod-shaped mesocrystal with cross-section radius Rmeso, accompanying with Gibbs energy variation (ΔGass-2) but no the bulk energy change. The introduction of water molecules could change the interfacial tension of PNs8, so we define the new interfacial tension γmeso = γbp + wδmeso to describe the surface energy of secondary rod-shaped mesocrystal, where δmeso represents the surface Gibbs energy variation into mesocrystal bassanite in the unit surface area after the addition of one percent water (wt%) and w is the percentage of water added (wt%). The Gibbs energy variation from x NPs into the mesocrystal (ΔGass-2) can be expressed as:

∆Gass-2=2πγmesoRmeso2+RmesoHmeso-2xπγbpRpn2+RpnHpn#2-4

Where 2πRmeso2+RmesoHmeso and 2xπRpn2+RpnHpn represent the surface area of single mesocrystal bassanite and the sum of surface areas of x PNs, respectively. Eq. (2-4) can be simplified to:

ΔGass-2=18Rmeso2π-Rmesoγbp+Rpnwδmeso+γbpRpn#2-5

Notably, we introduce a potential approximation that the aspect ratio of the cylinder will remain unchanged from PNs to secondary rod-shaped mesocrystal. Accordingly, the aspect ratio of PNs and secondary rod-shaped mesocrystal in our experiment both are measured as about 4, namely the Hpn (Hmeso) is equal to 8Rpn (8Rmeso). The secondary rod-shaped mesocrystal comprise x (x=πRmeso2HmesoπRpn2Hpn) PNs. The hierarchical assembly (ΔGagg), that is the BPs aggregate to mesocrystal, can be consequently summarized as:

∆Gagg=nxΔGbp+x∆Gass-1+∆Gass-2#2-6

which can be simplified to:

ΔGagg=2πRmeso24Rmesogbp+9wδmeso+9γbp#2-7

When more water is added into the PNs colloid, bassanite nanorods will transform into gypsum during the water-driven aggregation process. The conversion of the bassanite to gypsum involves a variation in the bulk energy density, Δgconv = ggyp – gbp, and a change of interfacial energy, Δγ = γgyp – γbp, where ggyp and γgyp represent bulk energy density and surface tension of gypsum phase, respectively. Similarly, we define the interfacial energy of gypsum as γgyp = γgn + wδgyp, where δgyp, which is analogue to δmeso, represents the surface energy variation changed into gypsum by adding one percent of water (wt%).

The Gibbs free energy conversion of the PNs into the rod-like mesocrystal gypsum phase, ΔGgyp, can be expressed as:

∆Ggyp=πRgyp2Hgypggyp-xπRpn2Hpngbp+2πγgypRgyp2+RgypHgyp-2xπγbpRpn2+RpnHpn#2-8

Where the πRgyp2Hgypggyp-xπRpn2Hpngbp is the difference of bulk energy from x PNs to a single mesocrystal gypsum and the 2πγgypRgyp2+RgypHgyp-2xπγbpRpn2+RpnHpn represents the corresponding difference of surface energy. The aspect ratio of gypsum is also estimated as 4 (Hgyp = 8Rgyp). Consequently, the ΔGgyp can be simplified as:

ΔGgyp=2π-9Rmeso3γbp+Rpn4Rgyp3ggyp+9Rgyp2wδgyp+γgn-4Rmeso3gbpRpn#2-9

This Gibbs free energy variation (ΔGtgyp) from bassanite to gypsum can be accordingly summarized as:

∆Gtgyp=nxΔGbp+x∆Gass-1+∆Ggyp#2-10

Taking ΔGbp (eq. 2-1), ΔGass-1 (eq. 2-1), and ΔGgyp (eq. 2-9), into the formula (2-10), we then obtain:

ΔGtgyp=2πRgyp24Rgypggyp+9wδgyp+9γgn#2-11

During the phase transformation, the energy difference (ΔGdif) between ΔGtgyp and ΔGagg determines the prior pathway for formation of bassanite aggregation (ΔGdif > 0) or conversion (ΔGdif < 0) thermodynamically. As the first two steps for formation of bassanite nanoparticles and nanorods are in the same conditions before adding extra water, ΔGdif is thus obtained as:

ΔGdif=ΔGtgyp-ΔGagg#2-12

Knowing Eqs. (2-7) and (2-11), ΔGdif can now be calculated as:

ΔGdif=2πRmeso24RmesoΔgconv+9wΔδconv+9Δγconv#2-13

where we define Δgconv=ggyp – gbp, Δδconv = δgyp – δmeso, and Δγconv = γgn – γbp, and Rmeso represents the mesocrystal with cross-section radius of bassanite or gypsum.

Therefore, at the phase boundary for mesocrystal bassanite and gypsum, we have ΔGdif = 0. Then, we replace Δγconv and Δgconv with the referred constants of 2.5 J∙m−2 (1 J∙m−2 for ligands free) and −0.1 × 106 kJ∙m−3 .9 With too many variables, the exact values are difficult to calculate, so here we estimate the Δgconv from the standard formation enthalpies of bassanite and Δγconv from calculated surface energy with density functional theory, respectively9. Actually, the variation law of free energy is independent of these specific values, but only depends on their relative values (see Supplementary Fig. 10). As a result, we can obtain the effect of water-dependent Δδconv on the phase conversion boundary in terms of the critical size (Rconv), which is Rmeso at ΔGdif = 0:

Rconv=22.5wΔδconv+56.25#2-14

In our systems, we have Δδconv < 0, where adding more water will result in earlier transformation of bassanite into gypsum at a smaller critical size, Rconv, which is in coincident with our experimental observation.

Supplementary results

Supplementary Table 1 Results of Rietveld refinement of hierarchically structured mesoscale bassanite with conventional cell

| Sample | Cell parameters (Å) |  |  |  | Rp |  | Rwp |  | Rexp |  | χ2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | a | b | c |  |  |  |  |  |  |  |  |
| Refinement | 17.68 | 7.02 | 12.16 | 5.78 |  | 7.46 |  | 4.60 |  | 2.63 |  |
| Bassanite | 17.58 | 7.04 | 12.20 | 0 |  | 0 |  | 0 |  | 0 |  |

Supplementary Table 2 Results of Rietveld refinement of gypsum

| Sample | Cell parameters (Å) |  |  |  | Rp |  | Rwp |  | Rexp |  | χ2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | a | b | c |  |  |  |  |  |  |  |  |  |
| Refinement | 8.18 | 8.19 | 5.75 | 8.91 |  | 13.1 |  | 4.76 |  | 7.82 |  |
| Gypsum | 8.19 | 8.19 | 5.76 | 0 |  | 0 |  | 0 |  | 0 |  |

Supplementary Fig. 1. Protocol for the synthesis of bulk bassanite and gypsum in solution at room temperature. (A) CaCl2 (0.1 M) is dissolved in the NPA solution with PVP (200 g/L). (B) The suspension of bassanite nanorods is obtained by adding equimolar H2SO4 into the solution A. (C, D) Bulk bassanite is formed after less than 3.85 wt% of water is added to the mixture B, while gypsum is obtained with the addition of the above 19.35 wt% of water. The insert picture shows the suspension in B after standing for more than 24 h.

Supplementary Fig. 2. (a) XRD patterns of dry PVP powder and monodispersed nano bassanite synthesized in n-propanol with polyvinyl pyrrolidone (NPA-PVP). The XRD pattern of the initial precipitates exhibits a poorly ordered structure, with one broad hump at approximately 22°, which might come from the combined scattering of the amorphous precipitates and the PVP macromolecules, but different from the characteristics of PVP. (b) Determination of the particle size/concentration using Nano Sight NTA technology. The inset shows 3D graph of diameter, intensity, and concentration.

Supplementary Fig. 3. FTIR spectra of phase-pure bassanite (top: 3.85 wt% of water) and gypsum (bottom: 19.35 wt% of water) for the vibrations of SO42- (a) and H2O (b).

Supplementary Fig. 4. (a) XRD pattern of bulk bassanite after 24 hours of aging. (b) A batch of XRD patterns of the samples obtained by varying water amount in presence of PVP at 30 min.

Supplementary Fig. 5. (a) XRD patterns of nano-bassanite and bulk gypsum coexistence synthesized by respectively adding 3 wt% and 1 wt% water to n-propanol solution without PVP. (b) SEM image of the samples collected at 30 min with 1 wt% water content.

Supplementary Fig. 6. The simulated Wulff shape of bassanite based on the calculation of surface energies.

Supplementary Fig. 7. Calculated surface energy of the candidate slab of bassanite with different planes.

Supplementary Fig. 8. Selected crystal planes and energies for Wulff construction. The annotation of letters is used to index the structures.

Supplementary Fig. 9. Schematic of the formation process of mesocrystal bassanite and gypsum.

Supplementary Fig. 10. (a) Critical size (Rconv) for transformation of bassanite into gypsum as a function of Δδconv at different water addition (w = 0, 3.85 and 7.7 wt%). In our systems, we have Δδconv < 0, where adding more water will result in earlier transformation of bassanite into gypsum at a smaller critical size, Rconv. (b) ΔGdif as a function of Rmeso at the specific Δδconv = -0.2 J∙m-2, -0.1 J∙m-2, and 0 J∙m-2, to show the critical transformation size for gypsum (Rconv at ΔGdif = 0 marked in the figure). It reveals that Δδconv only affects the absolute value of the critical size, rather than the thermodynamic trend in the phase transformation from bassanite into gypsum.

Supplementary Fig. 11. Comparison between the ΔGdif curves as a function of Rmeso for mesostructural bassanite and gypsum at w = 0, 3.85, 7.7 wt%, respectively. The vertical line indicates the critical size for bassanite conversion into gypsum, Rconv. The horizontal dotted line represents ΔGdif = 0.

Supplementary Fig. 12. Comparisons of bassanite content from XRD refinement and the reference of the actual content of two-phase mixture.

Supplementary Fig. 13. Energy (a) and temperature (b) evolution during the MD process.

Supplementary Fig. 14. Schematic drawing to show that part of the added water can combine with PVP ligands and move away together, while the others adsorb on the bassanite surface, where both of these processes facilitate the assembly of bassanite nanorods into mesostructure via particle attachment.

References

1.	Wang. L, Miao. X, Ali. J, Lyu. T, Pan. G, Quantification of Oxygen Nanobubbles in Particulate Matters and Potential Applications in Remediation of Anaerobic Environment. ACS Omega  3, 10624-10630 (2018).

2.	Ong. S. P., et al., Python Materials Genomics (pymatgen): A robust, open-source python library for materials analysis. Comput. Mater. Sci. 68, 314-319 (2013).

3.	Carter. W. C., Balluffi, R. W., Allen. S, Kinetics of Materials. In John Wiley & Sons: 2005.

4.	Miracle-Sole, Facet shapes in a Wulff crystal. 2012.

5.	Tran. R, Xu Z., Radhakrishnan B., Winston D., Sun W., Persson K. A., Ong S. P., Surface energies of elemental crystals. Sci Data 3, 160080-160080 (2016).

6.	Ong S. P., Richards W. D., Jain A., Hautier G., Kocher M., Cholia S., Gunter D., Chevrier, V. L., Persson K. A., Ceder G., Python Materials Genomics (pymatgen): A robust, open-source python library for materials analysis. Comput. Mater. Sci. 68, 314-319 (2013).

7.	Rodríguez-Carvajal J., Recent advances in magnetic structure determination by neutron powder diffraction. Physica B Condens. Matter 192, 55-69 (1993).

8.	H. Z. Zhang, B. Gilbert, F. Huang, J. F. Banfield, Water-driven structure transformation in nanoparticles at room temperature. Nature 424, 1025-1029 (2003).

9.	P. Atkins, T. Overton, Shriver and Atkins' inorganic chemistry, Oxford University Press, USA, 2010.