Supplementary Information

Theoretical study of metal-free catalytic for catalyzing CO-oxidation with a synergistic effect on P and N co-doped graphene

Sarinya Hadsadee 1, Siriporn Jungsuttiwong 2*, Rui-Qin Zhang 3, Thanyada Rungrotmongkol 1,4*

1Center of Excellence in Biocatalyst and Sustainable Biotechnology, Department of Biochemistry, Faculty of Science, Chulalongkorn University, Bangkok 10330, Thailand.

2Department of Chemistry and Center of Excellence for Innovation in Chemistry, Ubon Ratchathani University, Ubon Ratchathani 34190, Thailand E-mail: siriporn.j@ubu.ac.th

3Department of Physics and Materials science and Centre for Functional Photonics (CFP), City University of Hong Kong, Hong Kong, China.

4Program in Bioinformatics and Computational Biology, Graduate School, Chulalongkorn University, Bangkok 10330, Thailand. E-mail: thanyada.r@chula.ac.th

Figure 1. PDOS plots for (a) single vacancy P-embedded graphene, (b) N-doped single vacancy P-embedded graphene, (c) two N-doped single vacancy P-embedded graphene, (d) three N-doped single vacancy P-embedded graphene. The Fermi level is set to zero.

Figure 2. The band structures of (a) PC3-G, (b) PN1C2-G, (c) PN2C1-G, and (d) PN3-G monolayers, which show unpaired spins.

Figure 3. The potential energy as a function of time, obtained from molecular dynamics simulations (MD).

Figure 4. The temperature as the function of time obtained from molecular dynamic simulations (MD).

Figure 5. Electron density difference maps of O2 adsorption on (a) PN1C2-G-(End-on), (b) PN1C2-G-(Side-on), (c) PN2C1-G, and (d) PN3-G. (the isovalue is ±0.02)

Figure 6. Optimized geometries CO molecule on PNC-G surfaces.

Figure 7. Optimized initial structure of O2 and CO molecules for end-on configuration of O2 on PN1C2-G

Figure 8. Optimized geometries O2 molecule on PC3-G.

Figure 9. The co-adsorption of O2 and CO molecules on PN2C1-G.

Figure 10. Optimized geometries for the adsorption of O on PN1C2-G and PN2C1-G

Figure 11 The potential energy surface diagram of CO oxidation shows the LH mechanism for PN1C2-G. All bond distances are in Å.

Figure 12. The potential energy surface diagram of CO oxidation via the second step in pathway A. (a) PN1C2-G and (b) PN2C1-G. All bond distances are in Å.

Figure 13. The corresponding PDOS plots for the intermediate (IM-B) of OCO on (a) PN1C2-G and (b) PN2C1-G in pathway B.

Figure 14. The potential energy surface diagram for CO oxidation via a NER mechanism (a) PN1C2-G and (b) PN2C1-G. All bond distances are in Å.

Figure 15. Gibbs free energy dependent on the temperature obtained from DFT calculations.

Fig. S16. The potential energy surface diagram of CO oxidation via an ER mechanism the first step of PN1C2-G for end-on configuration of O2. All bond distances are in Å.

Table 1 Calculated atomic charges on the P atom (qP, |e|) and formation energies (Eform, eV) of PNxCy-G graphitic monolayers.

| Surface | qP | Eform |
| --- | --- | --- |
| PC3-G | 0.638 | -1.76 |
| PN1C2-G | 0.692 | -1.90 |
| PN2C1-G | 0.810 | -1.06 |
| PN3-G | 0.903 | -0.74 |

Table 2 The O2 and CO adsorption energies (Eads, eV) on P-NxCy-G, their corresponding Mulliken charge (q, |e|) of O2/CO.

| Surfaces | Adsorbate | Eads | q(P) | q(N) | q(C) | q(gas) |
| --- | --- | --- | --- | --- | --- | --- |
| PC3-G | Bare | - | 0.638 | - | -0.334 | - |
|  | O2 (End-on) | -1.50 | 1.103 | - | -0.365 | -0.565 |
| PN1C2-G | Bare | - | 0.692 | -0.595 | -0.349 | - |
|  | O2 (End-on) | -0.54 | 1.382 | -0.642 | -0.406 | -0.614 |
|  | O2 (Side-on) | -1.76 | 1.401 | -0.652 | -0.388 | -0.685 |
|  | CO | 0.48 | 0.716 | -0.573 | -0.339 | 0.001 |
|  | O* | -4.83 | 1.196 | -0.722 | -0.362 | -0.541 |
| PN2C1-G | Bare | - | 0.810 | -0.601 | -0.371 | - |
|  | O2 (Side-on) | -2.83 | 1.532 | -0.653 | -0.403 | -0.674 |
|  | CO | -0.20 | 0.817 | -0.605 | -0.351 | 0.007 |
|  | O* | -4.53 | 1.332 | -0.737 | -0.376 | -0.522 |
| PN3-G | Bare | - | 0.903 | -0.612 | - | - |
|  | O2 (Side-on) | -4.58 | 1.348 | -0.645 | - | -0.592/-0.582 |
|  | CO | -0.23 | 0.909 | -0.617 | - | 0.008 |

Table 3. Activation energies of the rate-determining step for CO oxidation on some metal-free catalysts.

| Catalyst | Rate determining step (eV) |
| --- | --- |
| Si-C3N nanosheet [1] | 0.38 (LH) |
| B-N3 graphene [2] | 0.39 (ER) |
| N-doped / P-doped graphene [3] | 0.67 (LH)/ 0.54 (LH) |
| B-doped/B-N doped penta-graphene [4] | 0.34 (ER)/ 0.39 (ER) |
| P/FeP4/ CoP4/ NP4- doped graphene[5] | 1.19/0.87/0.81/0.79 (LH) |
| PN1C2-G /PN2C1-G | 0.60/0.26 (ER) (the present study) |
| PN1C2-G | 0.86 (LH) (the present study) |
| PN1C2-G /PN2C1-G | 1.46 /1.19 (NER) (the present study) |

References

1	Esrafili, M. D. & Heydari, S. An effective approach for tuning catalytic activity of C3N nanosheets: Chemical-doping with the Si atom. Journal of Molecular Graphics and Modelling 92, 320-328, doi:https://doi.org/10.1016/j.jmgm.2019.08.011 (2019).

2	Esrafili, M. D. & Mousavian, P. Boosting graphene reactivity with co-doping of boron and nitrogen atoms: CO oxidation by O2 molecule. Applied Surface Science 455, 808-814, doi:https://doi.org/10.1016/j.apsusc.2018.06.053 (2018).

3	Esrafili, M. D., Mohammad-Valipour, R., Mousavi-Khoshdel, S. M. & Nematollahi, P. A Comparative Study of CO Oxidation on Nitrogen- and Phosphorus-Doped Graphene.  16, 3719-3727, doi:https://doi.org/10.1002/cphc.201500488 (2015).

4	Krishnan, R., Wu, S.-Y. & Chen, H.-T. Catalytic CO oxidation on B-doped and BN co-doped penta-graphene: a computational study. Physical Chemistry Chemical Physics 20, 26414-26421, doi:10.1039/C8CP04745F (2018).

5	Xu, X.-Y., Lin, S., Xu, H., Guo, H. & Zhao, C. Mechanistic insights into the CO oxidation reaction catalyzed by P-coordinated metal-doped graphene: The roles of phosphorus and metal atom. Applied Surface Science 556, 149776, doi:https://doi.org/10.1016/j.apsusc.2021.149776 (2021).