Comparison of experimental and quantum chemical studies of the effect of different functionalities of graphene oxide/polymer composites onto selective CO2 capture

Branislav Stankovica,b, Iranzu Barbarina, Oihane Sanz,a Radmila Tomovskaa,c,* and Fernando Ruipérezd,*

aPOLYMAT and Departamento de Química Aplicada, Facultad de Ciencias Químicas, University of the Basque Country UPV/EHU, Joxe Mari Korta Zentroa, Tolosa Hiribidea, 72, 20018 Donostia-San Sebastián, Spain;

bFaculty of Physical Chemistry, University of Belgrade, Studentski Trg 12-16, Belgrade, 11050 Republic of Serbia

cIKERBASQUE, Basque Foundation for Science, María Díaz de Haro 3, 48013 Bilbao, Spain

dPOLYMAT and Physical Chemistry Department, Faculty of Pharmacy, University of the Basque Country, 01006 Vitoria-Gasteiz, Spain

Content:

- Figure S1. Optimized geometry of the GO

- Figure S2. Optimized geometry of the MMA/BA/Am + CO2 complex

- Figure S3. Optimized geometry of the MMA/BA/AEMH + CO2 complex

- Figure S4. Optimized geometry of the MMA/BA/BS + CO2 complex

- Figure S5. Optimized geometry of the MMA/BA/MClA + CO2 complex

- Figure S6. Optimized geometry of the MMA/BA/GMA + CO2 complex

- Figure S7. (a) Optimized geometry of the MMA/BA/HEMA + CO2 complex. (b) Geometry of the copolymer without CO2

- Figure S8. Optimized geometry of the MMA/BA/NaSS + CO2 complex

- Figure S9. Optimized geometry of the GO/MMA/BA/GMA + CO2 complex

- Figure S10. Optimized geometry of the GO/MMA/BA/AEMH + CO2 complex

- Figure S11. Optimized geometry of the GO/MMA/BA/NaSS + CO2 complex

- Figure S12. Optimized geometry of the GO/MMA/BA/HEMA + CO2 complex

- Figure S13. Optimized geometry of the GO/MMA/BA/AEMH + N2 complex

- Figure S14. Optimized geometry of the GO/MMA/BA/NaSS + N2 complex

- Figure S15. Optimized geometry of the GO/MMA/BA/HEMA + N2 complex

- Figure S16. Optimized geometry of the GO/MMA/BA/GMA + N2 complex

- Figure S17. TGA curves of the functionalized GO-polymer composites

- Table S1. CO2 and N2 adsorption by the neat functionalized polymers and functionalized GO-polymer composites obtained at T = 25 oC and P = 1 atm

1. Figures:

Figure S1. Optimized geometry of the GO

Figure S2. Optimized geometry of the MMA/BA/Am + CO2 complex

Figure S3. Optimized geometry of the MMA/BA/AEMH + CO2 complex

Figure S4. Optimized geometry of the MMA/BA/BS + CO2 complex

Figure S5. Optimized geometry of the MMA/BA/MClA + CO2 complex

Figure S6. Optimized geometry of the MMA/BA/GMA + CO2 complex

Figure S7. (a) Optimized geometry of the MMA/BA/HEMA + CO2 complex. (b) Geometry of the copolymer without CO2

Figure S8. Optimized geometry of the MMA/BA/NaSS + CO2 complex

Figure S9. Optimized geometry of the GO/ MMA/BA/GMA + CO2 complex

Figure S10. Optimized geometry of the GO/ MMA/BA/AEMH + CO2 complex

Figure S11. Optimized geometry of the GO/ MMA/BA/NaSS + CO2 complex

Figure S12. Optimized geometry of the GO/MMA/BA/HEMA + CO2 complex

Figure S13. Optimized geometry of the GO/MMA/BA/AEMH + N2 complex

Figure S14. Optimized geometry of the GO/MMA/BA/NaSS + N2 complex

Figure S15. Optimized geometry of the GO/MMA/BA/HEMA + N2 complex

Figure S16. Optimized geometry of the GO/MMA/BA/GMA + N2 complex

Figure S17. TGA curves of the functionalized GO-polymer composites

2. Tables:

Table S1. CO2 and N2 adsorption by the neat functionalized polymers and functionalized GO-polymer composites obtained at T=25oC and P=1 atm

| Composite | CO2 adsorption (mmol/g) |  | N2 adsorption (mmol/g) |
| --- | --- | --- | --- |
|  | Neat polymer | GO/polymer | GO/polymer |
| GO/pol-NaSS | 0.067 | 0.67 | 0.60 |
| GO/pol-GMA | 0.057 | 0.61 | 0.61 |
| GO/pol-AEMH | 0.062 | 0.40 | 0.34 |
| GO/pol-HEMA | 0.076 | 1.11 | 0.74 |