Supplemental figures

Supplemental Figure 1

Fig S1. Fluorescence labeling of HAp crystals. HAp was labeled via fluorexon to explore cellular uptake. Briefly, 100mg HAp and 10 mL fluorexon solution (10 mg/ml) were mixed and stirred for 30min at room temperature. Then the HAP crzystals were then collected through centrifugation, washed several times with anhydrous ethanol and distilled water to ensure that no free fluorexon remained, and dried. The fluorexon-labeled HAp was observed under fluorescence and bright field microscope (magnification, ×200). Scale bar: 100 m. Abbreviations: S-HAp, synthetic HAp; H-HAp, human-derived HAp.

Supplemental Figure 2

Fig S2. Human-derived HAp induced osteogenic transdifferentiation of VSMCs and extracellular calcification. (A) Effect of hHAp on the protein expression of ALP, RUNX2 and OPN after culturing VSMCs with hHAp for 5 days. They were all increased after hHAp treatment. (B) Measurement of ALP activities in VSMCs after culturing with hHAp or nHAp for 7 days. Either hHAp or nHAp increased ALP activity as compared with the control. (C) Calcific nodules were visualized by Alizarin Red staining after VSMCs were treated as indicated with hHAp for 1 day, and washed to remove hHAp and cultured for 14 days. The calcified nodules increased significantly on day 14 compared with day 1, and osteogenic medium (OM) enhanced calcification induced by H-HAp. (D) Quantification of Alizarin Red extracted from the cells to represent the amount of calcium. (E) Total calcium on the dishes was quantified. Data are expressed as the mean ± SD. (*p < 0.05).

Supplemental Figure 3

Fig S3. Histology of implanted Matrigels. Hematoxylin and eosin (H&E) staining of the subcutaneous implanted tissues recovered from dorsal subcutaneous pocket in mice after 1 month of implantation. Red arrows indicate calcium deposits.

Supplemental Figure 4

Fig S4. H-HAp promoted accumulation of autophagosomes in VSMCs.

A) TEM images show that the autophagosomes accumulated in VSMCs treated with 100 μg/ml hHAp crystals. Black arrows point at double-membrane autophagosome. Scale bar, 1μm. Autophagic vacuoles were quantified in the bar graph. B) Western Blot analysis of LC3-II and p62 in VSMCs after they were treated with hHAp (100 μg/ml) for 24h. The bar graphs show the quantification of the relative LC3-II and p62 protein level.

Supplemental Figure 5

Fig S5. Nano-induced formation of autophagosomes is independent of mTOR inhibition.  A) Western blot analysis of phosphorylation of mTOR and AMPK in VSMCs that were treated with 100 μg/ml for specified time. No significant difference in phosphorylated mTOR and AMPK was observed between treated and untreated cells. B）Western blot analysis of LC3 in VSMCs that were treated with rapamycin or/and nano-HAp for 24 h. The relative LC3-II protein level was quantified by comparing with LC3-II in control (no HAp nor RAPA).

Supplemental Figure 6

Fig S6. Nano-HAp had no effect on mRNA level of LC3 and p62. VSMCs were treated with 100 μg/ml nano-HAp for 24 h, and mRNAs of LC3 and p62 were analyzed by RT-PCR.

Supplemental Figure 7

Fig S7. Effects of nHAp on p62 in VSMCs. Representative immunoﬂuorescence images show p62 (red) in VSMCs after treated with or without nHAp (100 μg/mL) for 24h. Scale bar: 50 m. The relative ﬂuorescence intensity of p62 was quantiﬁed.

Supplemental Figure 8

Fig S8. Nano-HAp did not affect the fusion of autophagosome with lysosome. Immunofluorescent staining of VSMCs with antibodies against LAMP1 (red) and LC3B (green). Cells were treated with or without nHAp for 24 h. Scale bar: 50 m. The bar graph shows statistical analysis of the colocalization coefficient of LC3 and LAMP1. The colocalization coefficient was represented as percentage of punctate signals of LC3 that were positive for LAMP1.

Supplemental Fig 9

Fig S9. Schematic diagram of autophagosome and autolysosome formation and action sites of rapamycin (RAPA) and Chloroquine (CQ).

Supplemental Fig 10

Fig S10. Effects of nHAp on the expression of EEA1 and LAMP1. VSMCs were treated with or without 100 μg/ml sHAp for 24 h and processed as follows. A) Western blot analysis of EEA1 and LAMP1 expression. The expression of EEA1 and LAMP1 was quantified in the bar graph. N=3, * p< 0.05. B) Fluorescent immunostaining of EEA1 in VSMCs. EEA1 fluorescence intensity was quantified in the bar graph. Scale bar: 25 m C) Fluorescent immunostaining of LAMP1. LAMP1 fluorescence intensity was quantified in the bar graph. Scale bar: 50 m. Data are expressed as mean ± SD. (* p < 0.05).

Supplemental Figure S11

Fig S11. Characterization of exosomes purified from conditioned medium of VSMCs. A) Representative TEM images of exosomes derived from VSMCs. Scale bar, 200 nm. The bar graph shows the statistical number of Exos extracted from VSMCs treated with/without S-HAp per TEM view. B) Size distribution of exosomes analyzed by granularmetric analysis. The graph shows concentration of Exos extracted from VSMCs treated with/without S-HAp. C) Western blots analysis for Alix, TSG101, CD9 and GAPDH in the whole cell lysate (W), purified exosomes (E) from the conditioned medium of VSMCs, and supernatants after ultracentrifugation (S).

Supplemental materials and methods

Ethics statement

All animal experiments were performed with approval of the Animal Use and Care Committee of Zhejiang University, which complies with the Guide for the Care and Use of Laboratory Animals, 8th edition published by the USA National Institutes of Health. Human carotid atherosclerotic plaque samples were obtained from patients underwent carotid endarterectomy after informed consent. Human aorta sample was obtained from one patient underwent the ascending aorta replacement surgery after informed consent. The approval for the study was granted by the Ethics Review Committee from the Second Affiliated Hospital of Zhejiang University.

Cellular Uptake of HAP

Transmission electron microscope (TEM) and confocal laser scanning microscope (CLSM) were used to visualize cellular uptake of HAp. Briefly, VSMCs were cultured with 100 μg/mL HAp for 24h. After incubation, SMCs were collected and fixed with 2.5% glutaraldehyde at 4°C overnight, Then, the cells were postfixed in 0.1M cacodylate buffer containing 1% osmium tetroxide for 1 h at 4°C, dehydrated stepwise in ethanol, and embedded in epoxy resin. Ultrathin sections (70 nm) were cut using an ultramicrotome, collected on copper grids, and observed by TEM (T10, FEI, USA). For CLSM imaging, after exposure of SMCs to 100μg/mL fluorexon-HAPs for 24 h, the cells were fixed with 4% paraformaldehyde and stained with rhodamine–phalloidin and 4′,6-diamidino-2-phenylindole (DAPI). Images were taken with a CLSM (LSM710; Carl Zeiss Meditec AG, Jena, Germany).

Transmission electron microscopy (TEM)

TEM was used to detect cellular internalization of HAp and observe the ultrastructures of the autophagosomes and lysosomes. The human aorta tissue or VSMCs were fixed with 2.5% glutaraldehyde overnight. After washing three times with PBS, the specimens were post-fixed with 1% OsO4 for 1–2 h. Next, the specimens were dehydrated by an ethanol gradient, followed by acetone for overnight infiltration. After the specimens were embedded in Spurr resin and sectioned in an ultramicrotome (Ultracut UCT, Leica, Germany), the sections were stained with uranyl acetate and alkaline lead citrate, and the image procured by TEM (T10, FEI, USA).

Cell transduction.

Lentiviral vector expressing mouse GFP was provided by Vigene Bioscience Co., Ltd. (Jinan, China). VSMCs were cultured on a 6-well plate with an initial 5×104 cells per well in 2 ml DMEM medium with 10% FBS. After 24 h culture, medium was replaced with fresh DMEM with 10% FBS, and 20 μl viral vector was added along with polybrene (final concentration of 8 μg/ml, Sigma) to each multiplicities of infection (MOI) of 50. After 8 h incubation, the supernatant was replaced with fresh DMEM medium with 10% FBS. Cells were cultured for another 48 h.

Western Blot

Cell lysate was prepared using RIPA lysis buffer (Beyotime, China). The samples were separated by SDS-polyacrylamide gel ( SDS-PAGE ), transferred to a polyvinylidene fluoride membrane, and immunoblotted with the following antibodies: anti-Runx2 ( 1:1000 ) (ET1612-47, HUABIO, China), anti-osteopontin (0806-6, HUABIO, China), anti-ALP (AF2910,RD systems, USA ), anti-LC3 ( ab51520,abcam,UK ), anti-p62 (EM0704, HUABIO, China),

anti-LAMP1 (sc-19992, Santa Cruz Biotechnology, USA), anti-EEA1 (M1503-1,HUABIO, China), anti-CTSD (ET1608-49, HUABIO, China), anti-p-mTOR (5536,Cell Signaling Technology), anti-mTOR (2983, Cell Signaling Technology), anti-p-AMPK (50081, Cell Signaling Technology, USA) , anti-AMPK (5832, Cell Signaling Technology, USA), anti-EGFR (ET1604-44, HUABIO, China), anti-Alix (2171, Cell Signaling Technology, USA), anti-TSG101, anti-CD9 (ET1601-9, HUABIO, China), anti-Actin (ET1701-80, HUABIO, China), anti-GAPDH (ET1702-66, HUABIO, China) at 4°C overnight, then incubated with secondary goat-antirabbit or goat-anti-mouse or goat-anti-rat IgG conjugated with horse radish peroxidase (HRP) (HUABIO, China) at room temperature for 1 hour. After being washed three times with PBS-T, the membranes were infiltrated with ECL (Bio-Rad, USA) and visualized by ChemiDoc™MP Imaging System (Bio-Rad, USA).

Real Time RT-PCR. Total RNA was extracted using TRIzol (TaKaRa, Dalian, China) according to the manufacturer’s protocol. DNase-I treated RNA (1000 ng) was reversed to cDNA using the PrimeScript™ 1st Strand cDNA Synthesis Kit (TaKaRa), and SYBR® Premix Ex TaqTM II (Tli RNaseH Plus) (TaKaRa) was applied for the quantitative real-time RT-PCR process on the ABI PRISM 7500 fast Detection System (Applied Biosystems, Carlsbad, USA). The sequences of PCR primers are listed as follows: β-actin: F-5’-GCCTTCCTTCTTGGGTATGG-3’, R-5’-GCACTGTGTTGGCATAGAGG-3’, LC3: F-5’-GCTGTAAGGAGGTGCAGCAG-3’,R-5’-TGGTCTTATCCAGGACAGGCA-3’, p62: F-5’- TGATCCCCGGCTGATTGAGT-3’, R-5’- TCTGTAGGAGCCTGGTGAGC -3’. All re-actions were done in triplicate and target genes were normalized to β-actin for quantification. PCR data were calculated by the comparative ΔΔct.

Immunofluorescence staining. Cells were grown directly on 14-mm coverslips, then washed three times with PBS, fixed with 4% paraformaldehyde for 30 min at room temperature, then washed with PBS three times and incubated with 0.25% Triton for 10 min. As for tissue sections, the tissue was excised and fixed in 10% formalin for 24 h, then dehydrated, embedded in paraffin, and cut into 5-µm -thick sections. The slides were deparaffinized, dehydrated and washed in PBS. After blocking with 3% BSA in PBS for 20 min, cells or tissue slides were reacted with primary antibodies for LC3, p62, LAMP1, EEA1, Rab7 (sc-376362,Santa Cruz Biotechnology, USA), V-ATPase (abs132663,Absin, China), EGFR or Runx2 (1:200 dilution in 3% BSA) at 4°C overnight. Then, the cells or tissue slides were incubated with secondary Alexa Fluor 488 anti-rabbit antibody, Alexa Fluor 555 anti-mouse antibody or Alexa Fluor 555 anti-rat antibody (1:200 dilution in 3%BSA) at room temperature for 1 h followed by incubation with DAPI (VECTASHIELD, USA) for nuclear staining. Images were generated with a fluorescence microscope (Leica, Germany).