Supplementary Information

Figure S1. Calcium aluminosilicate glass density around the focal diameter of simulated laser pulse at the peak intensity (left), Temperature profile of the pulse (PE = 100 eV) (red) and the focal volume (black)(right).

Figure S2. Five-coordinated Al for all simulated CAS systems as a function of silica concentration and pulse energy.

Figure S3. Distribution of CAS15.70 AlOx units (at x = 3, 4, 5 and 6) as a function of shell number. Shell zero represents the combine statistics within the focal volume (shells one through five).

Table S1. Distribution statistics for Al-O, Al-Al and Al-O-Si bonding under ambient and laser modified conditions in CAS15.70

| Parameter |  |  | Ambient | 10 eV | 15 eV | 25 eV | 50 eV | 100 eV |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al-O-Al | Mean Median Std. dev. |  | 117.9 ± 0.16 | 117.4 ± 0.16 | 116.9 ± 0.16 | 116.6 ± 0.16 | 116.5 ± 0.17 | 116.3 ± 0.16 |
|  |  |  | 116.6 | 115.8 | 115.1 | 114.8 | 114.7 | 114.6 |
|  |  |  | 20.1 | 20.3 | 20.3 | 20.2 | 20.3 | 20.3 |
| Al-O-Si | Mean Median Std. dev. |  | 136.6 ± 0.08 | 135.4 ± 0.08 | 134.9 ± 0.08 | 134.5 ± 0.08 | 134.2 ± 0.08 | 133.9 ± 0.08 |
|  |  |  | 135.3 | 134.2 | 133.7 | 133.3 | 133.0 | 132.9 |
|  |  |  | 17.6 | 18.3 | 18.4 | 18.6 | 18.5 | 18.6 |
| O-Al-O |  | Mean | 108.7 ± 0.04 | 108.4 ± 0.05 | 108.3 ± 0.05 | 108.2 ± 0.06 | 108.2 ± 0.06 | 108.1 ± 0.06 |
|  |  | Median | 107.2 | 106.2 | 105.8 | 105.5 | 105.3 | 105.2 |
|  |  | Std. dev. | 14.3 | 16.6 | 17.4 | 17.9 | 18.1 | 18.4 |
| d(Al-O) |  | Mean | 1.769 ± 0.000 | 1.790 ± 0.000 | 1.794 ± 0.000 | 1.796 ± 0.000 | 1.797 ± 0.001 | 1.798 ± 0.001 |
|  |  | Median | 1.750 | 1.768 | 1.771 | 1.772 | 1.773 | 1.774 |
|  |  | Std. dev. | 0.099 | 0.121 | 0.123 | 0.124 | 0.124 | 0.125 |
| d(Al-Al) |  | Mean | 3.105 ± 0.002 | 3.132 ± 0.002 | 3.133 ± 0.002 | 3.133 ± 0.002 | 3.137 ± 0.002 | 3.134 ± 0.002 |
|  |  | Median | 3.098 | 3.128 | 3.128 | 3.129 | 3.132 | 3.135 |
|  |  | Std dev. | 0.263 | 0.270 | 0.275 | 0.275 | 0.279 | 0.278 |

Table S2. Distribution statistics for Si-O, Si-Si and -O-Si bonding under ambient and laser modified conditions in CAS15.70

| Parameter |  | Ambient | 10 eV | 15 eV | 25 eV | 50 eV | 100 eV |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Si-O-Si | Mean | 148.0 ± 0.06 | 146.8 ± 0.07 | 146.3 ± 0.07 | 146.0 ± 0.07 | 146.0 ± 0.07 | 145.9 ± 0.07 |
|  | Median | 147.8 | 146.8 | 146.2 | 145.8 | 145.8 | 145.6 |
|  | Std. dev. | 14.1 | 14.7 | 14.9 | 15.0 | 15.1 | 15.1 |
| O-Si-O | Mean | 109.3 ± .01 | 109.2 ± .02 | 109.2 ± .02 | 109.2 ± .02 | 109.2 ± .02 | 109.2 ± .02 |
|  | Median | 108.8 | 108.6 | 108.5 | 108.5 | 108.5 | 108.4 |
|  | Std. dev. | 6.68 | 8.38 | 8.68 | 8.84 | 8.92 | 9.02 |
| d(Si-O) | Mean | 1.611 ± 0.000 | 1.621 ± 0.000 | 1.621 ± 0.000 | 1.621 ± 0.000 | 1.622 ± 0.000 | 1.622 ± 0.00 |
|  | Median | 1.607 | 1.614 | 1.614 | 1.614 | 1.614 | 1.614 |
|  | Std. dev. | 0.054 | 0.074 | 0.074 | 0.074 | 0.074 | 0.074 |
| d(Si-Si) | Mean | 3.096 ± 0.000 | 3.111 ± 0.001 | 3.109 ± 0.001 | 3.108 ± 0.001 | 3.110 ± 0.000 | 3.109 ± 0.001 |
|  | Median | 3.102 | 3.111 | 3.111 | 3.109 | 3.110 | 3.109 |
|  | Std dev. | 0.111 | 0.133 | 0.135 | 0.137 | 0.138 | 0.139 |

Figure S4. Running coordination for Al-Al, Si-Si and Al-Si (CAS15.70) after exposure to various pulse energies

Figure S5. Distribution of CAS20.60 AlOx units (at x = 3, 4, 5 and 6) as a function of shell number. Shell zero represents the combine statistics within the focal volume (shells one through five).

Table S3. Distribution statistics for Al-O, Al-Al and Al-O-Si bonding under ambient and laser modified conditions in CAS20.60

| Parameter |  | Ambient | 10 eV | 15 eV | 25 eV | 50 eV | 100 eV |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al-O-Al | Mean | 119.3 ± 0.12 | 118.1 ± 0.12 | 117.5 ± 0.12 | 117.2 ± 0.12 | 117.2 ± 0.12 | 117.2 ± 0.12 |
|  | Median | 118.1 | 116.9 | 116.3 | 115.9 | 115.8 | 115.9 |
|  | Std. dev. | 19.2 | 19.8 | 20.0 | 19.9 | 20.13 | 20.0 |
| Al-O-Si | Mean | 136.5 ± 0.07 | 135.1 ± 0.07 | 134.4 ± 0.07 | 134.1 ± 0.07 | 133.7 ± 0.07 | 133.7 ± 0.08 |
|  | Median | 135.2 | 134.0 | 133.2 | 132.9 | 132.4 | 132.4 |
|  | Std. dev. | 17.1 | 17.9 | 18.0 | 18.1 | 18.2 | 18.2 |
| O-Al-O | Mean | 108.6 ± 0.04 | 108.3 ± 0.05 | 108.1 ± 0.05 | 108.1 ± 0.05 | 108.0 ± 0.05 | 108.0 ± 0.05 |
|  | Median | 107.1 | 105.8 | 105.4 | 105.1 | 104.9 | 104.8 |
|  | Std. dev. | 14.7 | 17.5 | 18.3 | 18.6 | 18.9 | 19.1 |
| d(Al-O) | Mean | 1.769 ± 0.00 | 1.795 ± 0.000 | 1.798 ± 0.000 | 1.799 ± 0.000 | 1.801 ± 0.000 | 1.801 ± 0.000 |
|  | Median | 1.750 | 1.772 | 1.775 | 1.776 | 1.777 | 1.777 |
|  | Std. dev. | 0.098 | 0.123 | 0.125 | 0.125 | 0.126 | 0.126 |
| d(Al-Al) | Mean | 3.110 ± 0.002 | 3.141 ± 0.002 | 3.142 ± 0.002 | 3.139 ± 0.002 | 3.139 ± 0.002 | 3.139 ± 0.002 |
|  | Median | 3.103 | 3.136 | 3.139 | 3.134 | 3.137 | 3.137 |
|  | Std dev. | 0.252 | 0.269 | 0.273 | 0.275 | 0.274 | 0.271 |

Table S4. Distribution statistics for Si-O, Si-Si and -O-Si bonding under ambient and laser modified conditions in CAS20.60

| Parameter |  | Ambient | 10 eV | 15 eV | 25 eV | 50 eV | 100 eV |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Si-O-Si | Mean | 148.0 ± 0.08 | 146.6 ± 0.08 | 146.1 ± 0.08 | 145.8 ± 0.08 | 145.7 ± 0.08 | 145.4 ± 0.08 |
|  | Median | 148.1 | 146.4 | 145.8 | 145.4 | 145.5 | 145.4 |
|  | Std. dev. | 14.1 | 14.8 | 15.0 | 15.0 | 15.2 | 15.1 |
| O-Si-O | Mean | 109.3 ± 0.01 | 109.2 ± 0.02 | 109.2 ± 0.02 | 109.2 ± 0.02 | 109.2 ± 0.02 | 109.2 ± 0.02 |
|  | Median | 108.9 | 108.6 | 108.6 | 108.6 | 108.5 | 108.5 |
|  | Std. dev. | 6.45 | 8.34 | 8.68 | 8.82 | 8.93 | 8.97 |
| d(Si-O) | Mean | 1.610 ± 0.000 | 1.621 ± 0.000 | 1.621 ± 0.000 | 1.621 ± 0.000 | 1.621 ± 0.000 | 1.621 ± 0.000 |
|  | Median | 1.606 | 1.613 | 1.613 | 1.613 | 1.613 | 1.613 |
|  | Std. dev. | 0.053 | 0.074 | 0.075 | 0.075 | 0.075 | 0.074 |
| d(Si-Si) | Mean | 3.100 ± 0.000 | 3.116 ± 0.001 | 3.114 ± 0.001 | 3.112 ± 0.001 | 3.112 ± 0.001 | 3.111 ± 0.001 |
|  | Median | 3.106 | 3.117 | 3.114 | 3.111 | 3.112 | 3.111 |
|  | Std dev. | 0.110 | 0.134 | 0.137 | 0.138 | 0.139 | 0.140 |

Figure S6. Running coordination for Al-Al, Si-Si and Al-Si (CAS20.60) after exposure to various pulse energies

Figure S7. Distribution of CAS25.50 units (at x = 3, 4, 5 and 6) as a function of shell number. Shell zero represents the combine statistics within the focal volume (shells one through five).

Table S5. Distribution statistics for Al-O, Al-Al, Al-O-Si bonding under ambient and laser modified conditions in CAS25.50

| Parameter |  | Ambient | 10 eV | 15 eV | 25 eV | 50 eV | 100 eV |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al-O-Al | Mean | 119.8 ± 0.09 | 118.4 ± 0.10 | 117.8 ± 0.09 | 117.5 ± 0.10 | 116.5 ± 0.11 | 117.6 ± 0.10 |
|  | Median | 118.9 | 117.4 | 116.8 | 116.5 | 116.2 | 116.4 |
|  | Std. dev. | 18.8 | 19.6 | 19.9 | 19.9 | 19.8 | 20.0 |
| Al-O-Si | Mean | 136.4 ± 0.07 | 134.8 ± 0.07 | 134.0 ± 0.07 | 133.7 ± 0.07 | 132.2 ± 0.09 | 133.4 ± 0.07 |
|  | Median | 134.7 | 133.5 | 132.6 | 132.3 | 131.8 | 132.1 |
|  | Std. dev. | 16.8 | 17.6 | 17.6 | 17.7 | 20.4 | 17.8 |
| O-Al-O | Mean | 108.5 ± 0.04 | 108.1 ± 0.04 | 108.0 ± 0.04 | 107.9 ± 0.05 | 107.6 ± 0.05 | 107.6 ± 0.05 |
|  | Median | 106.7 | 105.4 | 104.9 | 104.7 | 104.2 | 104.1 |
|  | Std. dev. | 15.6 | 18.3 | 19.1 | 19.3 | 20.3 | 20.4 |
| d(Al-O) | Mean | 1.772 ± 0.000 | 1.799 ± 0.000 | 1.802 ± 0.000 | 1.803 ± 0.000 | 1.804 ± 0.000 | 1.805 ± 0.000 |
|  | Median | 1.753 | 1.776 | 1.778 | 1.779 | 1.780 | 1.780 |
|  | Std. dev. | 0.100 | 0.125 | 0.126 | 0.127 | 0.123 | 0.124 |
| d(Al-Al) | Mean | 3.112 ± 0.001 | 3.146 ± 0.001 | 3.146 ± 0.001 | 3.145 ± 0.001 | 3.145 ± 0.001 | 3.144 ± 0.001 |
|  | Median | 3.110 | 3.141 | 3.140 | 3.140 | 3.140 | 3.139 |
|  | Std dev. | 0.251 | 0.268 | 0.273 | 0.2274 | 0.274 | 0.272 |

Table S6. Distribution statistics for Si-O, Si-Si and -O-Si bonding under ambient and laser modified conditions in CAS25.50

| Parameter |  | Ambient | 10 eV | 15 eV | 25 eV | 50 eV | 100 eV |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Si-O-Si | Mean | 147.7 ± 0.09 | 146.2 ± 0.10 | 145.6 ± 0.10 | 145.4 ± 0.10 | 142.3 ± 0.10 | 145.2 ± 0.10 |
|  | Median | 147.4 | 146.1 | 145.2 | 145.0 | 143.5 | 144.8 |
|  | Std. dev. | 14.1 | 14.9 | 15.1 | 15.0 | 20.1 | 15.2 |
| O-Si-O | Mean | 109.3 ± 0.02 | 109.2 ± 0.02 | 109.2 ± 0.02 | 109.2 ± 0.02 | 109.2 ± .02 | 109.2 ± .02 |
|  | Median | 108.9 | 108.6 | 108.6 | 108.5 | 108.5 | 108.5 |
|  | Std. dev. | 6.45 | 8.40 | 8.61 | 8.67 | 8.74 | 8.78 |
| d(Si-O) | Mean | 1.609 ± 0.000 | 1.620 ± 0.000 | 1.620 ± 0.000 | 1.620 ± 0.000 | 1.620 ± 0.000 | 1.620 ± 0.000 |
|  | Median | 1.605 | 1.613 | 1.612 | 1.612 | 1.612 | 1.612 |
|  | Std. dev. | 0.053 | 0.075 | 0.075 | 0.074 | 0.075 | 0.074 |
| d(Si-Si) | Mean | 3.101 ± 0.001 | 3.117 ± 0.001 | 3.117 ± 0.001 | 3.115 ± 0.001 | 3.114 ± 0.001 | 3.115 ± 0.001 |
|  | Median | 3.107 | 3.118 | 3.116 | 3.115 | 3.112 | 3.114 |
|  | Std dev. | 0.111 | 0.136 | 0.139 | 0.140 | 0.141 | 0.140 |

Figure S8. Running coordination for Al-Al, Si-Si and Al-Si (CAS25.50) after exposure to various pulse energies

Figure S9. Fractional change in non-bridging oxygen (NBO) content as a function of silica concentration and pulse energy

Figure S10. Fractional change in triclustered oxygen (TBO) content as a function of silica concentration and pulse energy.

Figure S11. AlV in CAS10.80

Figure S12. 2-membered ring in CAS10.80 between AlIV and AV

Figure S13. TBO formed in CAS10.80 between Al- and Si-tetrahedra and AlV