In-situ formed and low-temperature deposited Nb: TiO2 compact-mesoporous layer for hysteresis-less perovskite solar cells with high performance

Miao Yu1, Haoxuan Sun1, Xiaona Huang2, Yichao Yan1,*, Wanli Zhang1

(1State Key Laboratory of Electronic Thin Films and Integrated Devices, University of Electronic Science and Technology of China, Chengdu, 611731, China；

2Chengdu Technological University, Chengdu, 611730, China)

Miao Yu: yumiao@uestc.edu.cn

Haoxuan Sun: 2577187880@qq.com

Xiaonan Huang: 504251083@qq.com

Yichao Yan: yanyichao@uestc.edu.cn

Wanli Zhang: wlzhang@uestc.edu.cn

Fig. S1 The light permeation comparison of TiO2 and Nb:TiO2 based ETL

Fig. S2 SEM images of (a) perovskite deposited on the pure TiO2 and (b) perovskite deposited on the TiO2 layer doped with 2% Nb

Fig. S3 Absorbance spectra of perovskite film deposited on pure TiO2 and 2%Nb:TiO2 layer

| Device | Rs (Ω) | Rct (Ω) | Rrec (kΩ) |
| --- | --- | --- | --- |
| TiO2 | 27.1 | 216 | 5.23 |
| 2% Nb:TiO2 | 26.2 | 178 | 119 |

Table S1 Parameters employed for the fitting of the impedance spectra of devices based on the pure TiO2 and 2%Nb:TiO2