Supporting Information

Synthesis and characterization of Ru-doped ZnO thin films from novel perimidine ruthenium complexes

Gokhan Demircana*, Abuzer Acikgoza, Serife Yalcinb, Emine Aytarc, Bulent Aktasa,

a Department of Mechanical Engineering, Engineering Faculty, Harran University, Sanliurfa, Turkey

b Department of Physics, Art and Science Faculty, Harran University, Sanliurfa, Turkey

c  Department of Chemistry, Art and Science Faculty, Harran University, Sanliurfa, Turkey

# Content:

General procedure for the synthesis of the ligands (L1-L2) 	2

General procedure for the synthesis of the metal complexes	3

Spectroscopic characterization	4

Table	5

Figures	7

References	10

- General procedure for the synthesis of the ligands (L1-L2)

The ligands (L1) [1,2] and (L2) [3,4] was synthesized by a modification of the method in the published procedure. The ligands were synthesized by procedure as follow:

In a two-necked, 100 mL round-bottom flask and equipped with a blanket of nitrogen (N2) was placed 30 mL of anhydrous ethanol (EtOH) at room temperature for each ligand. 1,8-diaminonaphthalene (1.58 g, 10.0 mmol) was added to these solution, followed by the 2-pyridinecarboxaldehyde (1.07 g, 10.0 mmol) for ligand (L1), the quinoline-2-carboxaldehyde (1.57 g, 10.0 mmol) for ligand (L2) was slowly added and stirred at reflux. To the solutions, a few drops of acetic acid were added, and then heated under reflux for 24 h. The volatiles were evaporated in vacuum to dryness. The residue was dissolved in CH2Cl2 and filtered via cannula on celite. The solution was concentrated to 15 mL and then the desired product was precipitated in 30 mL n-hexane.

For (L1): Color: brown, yield (%): 80, m.p: 96-100 oC. Anal. Calc. for [C16H11N3] (M.W: 245 g/mol): C, 78.35; H, 4.52; N, 17.13; found: C, 78.01; H, 4.36; N, 17.00. 1H NMR (300 MHz, DMSO-d6, δ ppm): 6.92-6.89 (t, J = 4.2 Hz, 1H, Ar-CH); 7.12-7.07 (t, J = 7.2 Hz, 2H, Ar-CH); 7.71 (d, J = 4.2 Hz, 2H, Ar-CH); 8.02 (d, J = 1.8 Hz, 2H, Ar-CH); 8.31 (d, J = 7.2 Hz, 1H, Ar-CH); 8.74 (d, J = 4.2 Hz, 1H, Ar-CH); 10.20 (s, 1H, Ar-CH); 10.99 (s, 1H, N-H). 13C NMR (100.56 MHz, DMSO-d6, δ ppm): 103.5; 106.2; 114.1; 114.6; 117.7; 121.6; 126.1; 128.1; 128.8; 137.5; 137.9; 148.4 and 149.3 (Ar-CH). LC-MS/MS (Scan ES+): m/z (%) 246 [M]+. UV-Vis (ʎmax/(nm), * shoulder peak): 359, 273, 237 and 206* (in C2H5OH).

For (L2): Color: red, yield (%): 85, m.p: 132-136 oC. Anal. Calc. for [C20H13N3] (M.W: 295 g/mol): C, 81.34; H, 4.44; N, 14.23; found: C, 81.07; H, 4.03; N, 14.08. 1H NMR (300 MHz, CDCl3, δ ppm): 6.86 (d, J = 7.2 Hz, 2H, Ar-CH); 7.72-7.77 (t, J = 7.5 Hz, 2H, Ar-CH); 7.88-7.94 (t, J = 8.4 Hz, 2H, Ar-CH); 8.12 (d, J = 8.4 Hz, 2H, Ar-CH); 8.26 (d, J = 8.4 Hz, 2H, Ar-CH); 8.41 (d, J = 8.4 Hz, 1H, Ar-CH); 8.57 (d, J = 8.7 Hz, 2H, Ar-CH); 10.95 (s, 1H, N- H). 13C NMR (75.48 MHz, CDCl3, δ ppm): 100.0; 103.6; 106.3; 114.5; 117.8; 118.6; 128.1; 128.2; 128.6; 128.8; 129.0;130.4; 137.3; 137.9 and 144.7 (Ar-CH). LC-MS/MS (Scan ES+): m/z (%) 296 [M]+. UV-Vis (ʎmax/(nm), * shoulder peak): 445, 305, 253, 235 and 210* (in C2H5OH).

- General procedure for the synthesis of the metal complexes

The complexes ([Ru(L1-2)(p-cymene)Cl]Cl) [2] were synthesized by the procedure as follows:

In a two-necked, 50 mL round-bottom flask equipped with a blanket of nitrogen (N2) was placed 15 mL of anhydrous tetrahydrofuran (THF) at room temperature for each metal complex synthesis. The solution of each ligand (L1-L2) (1.0 mmol) in 7 mL of anhydrous tetrahydrofuran (THF) was added to the round-bottom flask and after the reaction mixtures were stirred for 20 min, this was followed by the addition of [RuCl2(p-cymene)]2 (1.2 g, 0.5 mmol) for Ru complexes, respectively, for each solution. Once the metal salts were added, the color of the mixtures was immediately developed. The reaction mixtures were stirred at 60 °C temperature and between 2-24 h. for all metal complexes. Subsequently, 25 mL n-hexane was added to the mixtures to precipitate the metal complex and the precipitate was filtered off, washed with THF and filtered off again, to remove un-reacted ligands. The resulting solids were re-dissolved in CH2Cl2 (5 mL) and then precipitated with diethyl ether (10 mL) to give the clear crystal solid.

[Ru(L1)(p-cymene)Cl]Cl: Color: yellow, yield (%): 85, m.p: >350 oC. Anal. Calc. for [C27H28N3Cl2Ru] (M.W: 566 g/mol): C, 57.24; H, 4.98; N, 7.42; found: C, 57.04; H, 4.63; N, 7.05. 1H NMR (300 MHz, DMSO-d6, δ ppm): 1.17 (d, J = 7.2 Hz, 6H, p-cym-CH3) 2.09 (s, 3H, p-cym-CH3); 2.88-2.78 (m, 1H, p-cym-CHCH3); 5.87 (m, 2H, Ar-CH); 7.09 (m, 2H, Ar-CH); 8.08 (d, J = 8.7 Hz, 2H, Ar-CH); 9.06 (d, J = 7.2 Hz, 2H, Ar-CH); 9.26 (d, J = 5.4 Hz, 1H, Ar-CH); 9.55 (d, J = 4.2 Hz, 1H, Ar-CH). 13C NMR (75.48 MHz, DMSO-d6, δ ppm): 17.8; 21.5; 23.9 (CH3); 29.9 CH(CH3)2; 85. 5 and 86.3 (Ar CH of p-cym); 100.0; 106.3; 114.2; 114.6; 117.8; 126.1; 128.0; 128.8; 137.5; 137.9; 148.4; 148.9 and 149.3 (Ar CH). LC-MS/MS (Scan ES+): m/z (%) 567 [M]+. UV-Vis (ʎmax/(nm), * shoulder peak): 282 and 233* (in C2H5OH).

[Ru(L2)( p-cymene)Cl]Cl: Color: yellow, yield (%): 87, m.p: 295-299 oC. Anal. Calc. for [C30H27N3Cl2Ru] (M.W: 616 g/mol): C, 60.39; H, 4.90; N, 6.82; found: C, 60.01; H, 4.28; N, 6.35. 1H NMR (400 MHz, DMSO-d6, δ ppm): 1.19 (d, J = 6.9 Hz, 6H, p-cym-CH3); 2.09 (s, 3H, p-cym-CH3); 2.88-2.78 (m, 1H, p-cym-CHCH3); 6.81 (d, J = 7.2 Hz, 2H, Ar-CH); 7.75-7.70 (t, J = 7.5 Hz, 2H, Ar-CH); 7.92-7.87 (t, J = 7.7 Hz, 2H, Ar-CH); 8.09 (d, J = 7.8 Hz, 2H, Ar-CH); 8.25 (d, J = 8.4 Hz, 2H, Ar-CH); 8.39 (d, J = 8.7 Hz, 1H, Ar-CH); 8.56 (d, J = 8.4 Hz, 1H, Ar- CH). 13C NMR (100.56 MHz, DMSO-d6, δ ppm): 17.8; 21.5; 23.9 and 22.3 (CH3); 29.9 (CHCH3); 85.5 and 86.3 (Ar CH of p-cym); 100.0; 106.3; 114.5; 117.8; 118.6; 122.3; 128.1; 128.5; 128.6; 128.9; 130.4; 135.1;137.3; 144.7 and 146.1 (Ar-CH). LC-MS/MS (Scan ES+): m/z (%) 617 [M]+. UV-Vis (ʎmax/(nm), * shoulder peak): 530, 430, 336, 298, 254 and 232* (in C2H5OH).

- Spectroscopic characterization

The perimidine ligands (L1-2) were fully characterized by IR, 1H and 13C NMR spectroscopy elemental analysis, melting point measurements, mass spectrometry and UV-Vis spectroscopy. The IR spectra of perimidine ligands showed peaks in the υC=N stretching frequency region at 1627-1629 cm-1 given in Table 1. The coordination of perimidine ligands to M(II) through the nitrogen atom was expected to lower the (C=N) frequency (1615-1625 cm-1) [5].

The NMR spectra of ligands (L1-2) and their diamagnetic ([Ru(L1-2)(p-cymene)Cl]Cl) complexes have been recorded in DMSO-d6 or CDCl3 at room temperature and the assignments made for the observed chemical shifts are listed. All NMR data showed good agreement with their proposed structures. By a comparison of the chemical shifts of the aromatic protons and carbons of the perimidine ligands (L1-2) with their [Ru(L1-2)(p-cymene)Cl]Cl complexes, the chemical shift to low magnetic field due to the formation of dative M←N bond as expected was observed. This result is confirmed the participation of the nitrogen atoms in coordination for metal complexes. Notably, in the 1H NMR spectrum of L1 and L2 ligands, perimidyl N-H proton was observed 10.99 ppm for L1 and at 10.95 ppm for L2 as singlets, respectively.

Table 1. Selected IR bands ( υ C=N cm-1 ) of the synthesized compounds as KBr pellets.

| x | Lx | [Ru(Lx)(p-cymene)Cl]Cl |
| --- | --- | --- |
| 1 | 1627 | 1615 |
| 2 | 1629 | 1625 |

To investigate the electronic properties of the perimidine ligand system to have a high conjugation (L1 and L2) and their Ru(II) metal complexes, the UV-Vis absorption spectra of all complexes in C2H5OH were measured at room temperature. Regarding the absorption spectroscopy, there are some obvious bands clearly separated from the other transition in the electronic spectrum of the ligands (L1-2) and their metal complexes ([Ru(L1-2)(p-cymene)Cl]Cl). The ligands (L1-2) spectra exhibit absorption bands in the region 206-445 nm. These bands can be assigned to the * or n * charge transfer transitions of LM ligand-to-metal charge transfer (LMCT) transition. For some complexes the d-d transition was not observed due to their poor solubility in the spectra. Appearance of this band is due to π→π* transition associated with the azomethine linkage and L→M charge transfer transition. The metal complexes spectra exhibit absorption bands in the region 530-232 nm.

The LC–MS/MS spectra for the high conjugated perimidine ligand systems (L1-2) and their metal complexes ([Ru(L1-2)(p-cymene)Cl]Cl) were investigated. The Mass (LC–MS/MS) spectral data of all compounds (L1, L2 and [Ru(L1-2)(p-cymene)Cl]Cl) supported the proposed structures due to the molecular ion peaks consistent with the molecular weight of the compounds. The designated results for peak positions are given in the fig. 1-4. The m/z corresponding to perimidine ligands (L1-2) appeared at 246 for L1, at 296 for L2, at 567 for complex [Ru(L1)(p-cymene)Cl]Cl, at 617 for complex [Ru(L2)(p-cymene)Cl]Cl, consecutively. These mass results are in a good agreement with the proposed molecular formula for these compounds.

Fig. 1. The LC-MS/MS spectra of L1 ligand.

Fig. 2. The LC-MS/MS spectra of [Ru(L1)(p-cymene)Cl]Cl complex.

Fig. 3. The LC-MS/MS spectra of L2 ligand complex.

Fig. 4. The LC-MS/MS spectra of [Ru(L2)(p-cymene)Cl]Cl complex.

REFERENCES

[1] A.M. Giani, M. Lamperti, A. Maspero, A. Cimino, R. Negri, G.B. Giovenzana, G. Palmisano, L. Nardo, Fluorescence studies on 2-(het)aryl perimidine derivatives, J. Lumin. 179 (2016) 384–392. https://doi.org/10.1016/j.jlumin.2016.07.033.

[2] E. Aytar, Konjuge nn kompleks bileşikleri ve katalitik uygulamaları, Harran University, 2019, PhD Thesis.

[3] V. A. Anisimova, A. F. Pozharskii, L. E. Nivorozhkin, , & V. I. Minkin, Heterocyclic analogs of pleiadiene. Chemistry of Heterocyclic Compounds. 14 (1978) 89-92. https://doi.org/10.1007/BF00635953

[4] E. Aytar, V. Kasim, Sübstitüe Perimidin Ligantları ile Metal Klorürlerin Varlığında CO2’in Organik Ürünlere Dönüşümü, Selçuk Üniversitesi Fen Fakültesi Fen Derg. 45 (2019) 60–70.

[5] M. Ulusoy, E. Çetinkaya, B. Çetinkaya, Conversion of carbon dioxide to cyclic carbonates using diimine Ru (II) complexes as catalysts, Appl. Organomet. Chem. 23 (2009) 68-74. https://doi.org/10.1002/aoc.1473