Table 1:  Molar concentrations a and extinction coeﬀicients (ε)b of gold nanoparticle solutions.

Sample	AuNP s’ Molar conc.  (M)	ε (M−1.cm−1)	Drug conc.

| AuNP s with Alen. | 3.97×10−8 | (3.02±0.39) ×104 | 3.69 mM |
| --- | --- | --- | --- |
| AuNP s with Mem. | 3.67×10−8 | (2.22±0.029)×106 | 55.77 µM |
| AuNP s with Tobr. | 3.22×10−8 | (5.35±0.047)×106 | 213.90 µM |
| AuNP s with Tobr. | 3.33×10−8 | ———c | 21.39 µM |

AuNP s	3.68×10−8	———

- molar concentrations calculated from Equation  2.

- extinction coeﬀicients calculated from the slope of regression line in Figure 3.

- extinction coeﬀicient not calculated due to aggregation of AuNP s and unstable λmax.

2:  Mean core diameter, hydrodynamic diameter and Zeta Potential * of gold nanoparticles   in absence and presence of alendronate, memantine, and   tobramycin.

| Gold-nanoparticles | Core D ± SD (nm) | Hydrodynamic D | Zeta Potential |
| --- | --- | --- | --- |
|  |  | ± SD (nm) | (mV) |
| AuNP s | 9.58 ± 1.27 | 52.08 ± 3.54 | -24.56 |
| AuNP s with Alen. (micro) | 9.34 ± 1.07 | 58.94 ± 7.3 | -30.23 |
| AuNP s with Mem. (nano) | ————— | 64.99 ± 2.32 | 0.26 |
| AuNP s with Mem. (micro) | 9.59 ± 0.87 | 98.41 ± 1.05 | 0.53 |
| AuNP s with Tobr. (nano) | 10.01 ± 0.95 | 135.3 ± 4.75 | -23.63 |
| AuNP s with Tobr. (micro) | 9.90 ± 1.05 | 332.16 ± 38.54 | -1.64 |
| D = diameter. |  |  |  |

*The average core diameter, hydrodynamic diameter and Zeta Potential were calculated from multiple HRTEM images and DLS measures.