Supporting information of

Fabrication of near-invisible solar cell with monolayer WS2

Xing He1, Yuta Iwamoto1, Toshiro Kaneko1, and Toshiaki Kato1,*

1Graduate School of Engineering, Tohoku University, Sendai 980-8579, Japan

*Corresponding Author. e-mail: kato12@tohoku.ac.jp

Table S1| Types and basic features of solar cells with thick TMD.

| Type | Material | Layer number | PCE | Device size | Optical transparency | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| PN (Dual gate) | MoSe2 | 10L | 14% (solar simulator) | m-scale | X (Si substrate) | S1 |
| PN (Plasma doping) | MoS2 | ~120 nm | 2.8% (Solar simulator) | m-scale | X (Au substrate) | S2 |
| Hetero (Lateral) | MoS2/WSe2 | 7.06/4.51 nm (10L/6L) | ~10% (19.1 W/m2) | m-scale | O (glass substrate) | S3 |
| Hetero (Lateral) | n-MoS2/p-InP | 6L (MoS2)/- | 0.11% (solar simulator) | mm-scale | X (Si substrate) | S4 |
| PN (MoOx Doping) | WS2 | < 90 nm | 1.55% (solar simulator) | m-scale | X (Si substrate) | S5 |
| Schottky | MoS2 | 50 nm | 2.5% (532 nm, 1000W/m2) | m-scale | X (Si substrate) | S6 |
| Schottky | WSe2 | 25 ~ 185 nm | 1.7% (solar simulator) | m-scale | X (Si substrate) | S7 |

Table S2| Types and basic features of solar cells with monolayer and TMD with a few layers.

| Type | Material | Layer number | Total power | Device size | Optical transparency | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| PN (Dual gate) | WSe2 | 1L | 170 pW (Laser, 640 nm, 48000 W/m2) | m-scale | X (Si substrate) | S8 |
| PN (Dual gate) | WSe2 | 1L | 9 pW (halogen lamp, 1400 W/m2) | m-scale | X (Si substrate) | S9 |
| Liquid junction (Vertical) | MoS2, WSe2 | 1L (MoS2) 1L (MoS2)/1L (WSe2) 1L (WSe2) | – (532 nm, 20.8 W/m2) | m-scale | X (ITO substrate, Pt electrode) | S10 |
| Schottky (lateral) | WSe2, WS2 | 2L, 3L | 0.023 pW (solar simulator, 1000 W/m2) | cm-scale | O (PEN substrate, Sparse scattered pattern) | S11 |
| Schottky | WS2 | 1L | 420 pW (solar simulator, 1000 W/m2) | cm-scale | O (Quartz substrate， Dense integrated pattern) | This work |

Table S3| Schottky barrier height of Mx/ITO, as measured by the SPCM method.

| Electrode | ØB [meV] |
| --- | --- |
| WO3/Cu/ ITO | ~ 220 |
| Cu/ITO | ~ 100 |
| Ni/ITO | ~ 60 |
| Ag/ITO | ~ 20 |
| Au/ITO | ~ 10 |
| ITO | ~ 5 |

Figure S1| (i–v) Potential profile of WO3/Cu/ITO contact with WS2 with an inverse bias applied, VDS, and flat band forms when VDS = –220 mV shown in (iv), indicating ΦB is 220 meV between the contact of WO3/Cu/ITO and WS2.

Figure captions:

Figure S1| (i–v) Potential profile of WO3/Cu/ITO contact with WS2 with an inverse bias applied, VDS, and flat band forms when VDS = –220 mV shown in (iv), indicating ΦB is 220 meV between the contact of WO3/Cu/ITO and WS2.

Figure S2| Performance of solar cells in um2 scale. (a–d) Typical I-V curves of the solar cell with electrodes of ITO–ITO, WO3/ITO–ITO, Cu/ITO–ITO, and WO3/Cu/ITO–ITO, respectively. Scale bars in inset images represent 50 um. (e–g) Comparison of open circuit voltage, short circuit current, and fill factor, respectively, of the solar cells shown in (a–d).

Figure S3| Devices with a simple enlarged pattern. (a) Images of the devices, (b) device area calculation method, (c) normalized PT, and (d) open circuit voltage (VOC) of the devices with increasing area.

Figure S4| Parallel connection equivalent circuit for the unit device. (a) Unit device treated as many small channels (i, ii, iii, …) connected in parallel. (b) Total resistance (Rsh) calculated from the equation 1/Rsh =Σ(1/Rsh (i)). (c) Schematic diagram of the device with a low parallel resistance part, which may come from impurities or metallic-like 1T phase.

Figure S5| Dependency on the number of parallel connections (Ndev) of unit device module A (UDM-A). (a) Images of the device structure. (b, c) Images of the devices with same channel length and width, but different Ndev. (d, e) Plots of normalized PT and Voc versus Ndev; black line in (d) is the ideal tendency of normalized PT and black dash line in (e) is the fitting curve of VOC.

Figure S6| Design of UDM-B: seriers connection of UDM-A. (a, b) Diagram of Nse designed for the device. (c, d, e) PT, VOC, ISC of the devices with Nse values.

Figure S7| Comparision of designed patteren and simple pattern. (a) PT of designed and simple patterns. (b–e) Typical I–V curve of the solar cells as shown in (a) (1)–(4). (f, g) Voc and ISC of designed pattern and simple pattern.

Figure S8| Images of (a) quartz, (b) electrodes on quartz, and (c) solar cell on quartz combined with electrodes and WS2.

Figure S9| Photoluminencent intensity of CVD grown WS2. (a) Schematic illustration of PL intensity testing and mapping. (b) PL mapping of WS2 sheet on SiO2/Si substrate, green dots represent monolayer WS2. (c) Image and (d) PL mapping of single crystal monolayer WS2 at the red cross in (b). (e) PL intensity of WS2 in (d).

Figure S1| (i–v) Potential profile of WO3/Cu/ITO contact with WS2 with an inverse bias applied, VDS, and flat band forms when VDS = –220 mV shown in (iv), indicating ΦB is 220 meV between the contact of WO3/Cu/ITO and WS2.

Figure captions:

Figure S1| (i–v) Potential profile of WO3/Cu/ITO contact with WS2 with an inverse bias applied, VDS, and flat band forms when VDS = –220 mV shown in (iv), indicating ΦB is 220 meV between the contact of WO3/Cu/ITO and WS2.

Figure S2| Performance of solar cells in um2 scale. (a–d) Typical I-V curves of the solar cell with electrodes of ITO–ITO, WO3/ITO–ITO, Cu/ITO–ITO, and WO3/Cu/ITO–ITO, respectively. Scale bars in inset images represent 50 um. (e–g) Comparison of open circuit voltage, short circuit current, and fill factor, respectively, of the solar cells shown in (a–d).

Figure S3| Devices with a simple enlarged pattern. (a) Images of the devices, (b) device area calculation method, (c) normalized PT, and (d) open circuit voltage (VOC) of the devices with increasing area.

Figure S4| Parallel connection equivalent circuit for the unit device. (a) Unit device treated as many small channels (i, ii, iii, …) connected in parallel. (b) Total resistance (Rsh) calculated from the equation 1/Rsh =Σ(1/Rsh (i)). (c) Schematic diagram of the device with a low parallel resistance part, which may come from impurities or metallic-like 1T phase.

Figure S5| Dependency on the number of parallel connections (Ndev) of unit device module A (UDM-A). (a) Images of the device structure. (b, c) Images of the devices with same channel length and width, but different Ndev. (d, e) Plots of normalized PT and Voc versus Ndev; black line in (d) is the ideal tendency of normalized PT and black dash line in (e) is the fitting curve of VOC.

Figure S6| Design of UDM-B: seriers connection of UDM-A. (a, b) Diagram of Nse designed for the device. (c, d, e) PT, VOC, ISC of the devices with Nse values.

Figure S7| Comparision of designed patteren and simple pattern. (a) PT of designed and simple patterns. (b–e) Typical I–V curve of the solar cells as shown in (a) (1)–(4). (f, g) Voc and ISC of designed pattern and simple pattern.

Figure S8| Images of (a) quartz, (b) electrodes on quartz, and (c) solar cell on quartz combined with electrodes and WS2.

Figure S9| Photoluminencent intensity of CVD grown WS2. (a) Schematic illustration of PL intensity testing and mapping. (b) PL mapping of WS2 sheet on SiO2/Si substrate, green dots represent monolayer WS2. (c) Image and (d) PL mapping of single crystal monolayer WS2 at the red cross in (b). (e) PL intensity of WS2 in (d).

Figure S2| Performance of solar cells in um2 scale. (a–d) Typical I-V curves of the solar cell with electrodes of ITO–ITO, WO3/ITO–ITO, Cu/ITO–ITO, and WO3/Cu/ITO–ITO, respectively. Scale bars in inset images represent 50 um. (e–g) Comparison of open circuit voltage, short circuit current, and fill factor, respectively, of the solar cells shown in (a–d).

Figure S2| Performance of solar cells in um2 scale. (a–d) Typical I-V curves of the solar cell with electrodes of ITO–ITO, WO3/ITO–ITO, Cu/ITO–ITO, and WO3/Cu/ITO–ITO, respectively. Scale bars in inset images represent 50 um. (e–g) Comparison of open circuit voltage, short circuit current, and fill factor, respectively, of the solar cells shown in (a–d).

Figure S3| Devices with a simple enlarged pattern. (a) Images of the devices, (b) device area calculation method, (c) normalized PT, and (d) VOC of the devices with increasing area.

Figure S4| Parallel connection equivalent circuit for the unit device. (a) Unit device treated as many small channels (i, ii, iii, …) connected in parallel. (b) Total parallel (shunt) resistance (Rsh) calculated from the equation 1/Rsh =Σ(1/Rsh (i)). (c) Schematic diagram of the device with a low parallel resistance part, which may come from impurities or metallic-like 1T phase.

Figure S5| Dependency on the number of parallel connections (Npa) of unit device module A (UDM-A). (a) Images of the device structure. (b, c) Images of the devices with same channel length and width, but different Npa. (d, e) Plots of normalized PT and VOC versus Npa; black line in (d) is the ideal tendency of normalized PT and black dash line in (e) is the fitting curve of VOC.

Figure S6| Design of UDM-B: seriers connection of UDM-A. (a, b) Diagram of Nse designed for the device. (c, d, e) PT, VOC, ISC of the devices with Nse values.

Figure S6| Design of UDM-B: seriers connection of UDM-A. (a, b) Diagram of Nse designed for the device. (c, d, e) PT, VOC, ISC of the devices with Nse values.

Figure S7| Comparision of designed patteren and simple pattern. (a) PT of designed and simple patterns. (b–e) Typical I–V curve of the solar cells as shown in (a) (1)–(4). (f, g) VOC and ISC of designed pattern and simple pattern.

Figure S8| Images of (a) quartz, (b) electrodes on quartz, and (c) solar cell on quartz combined with electrodes and WS2.

Figure S8| Images of (a) quartz, (b) electrodes on quartz, and (c) solar cell on quartz combined with electrodes and WS2.

Figure S9| Photoluminencent intensity of CVD grown WS2. (a) Schematic illustration of PL intensity testing and mapping. (b) PL mapping of WS2 sheet on SiO2/Si substrate, green dots represent monolayer WS2. (c) Image and (d) PL mapping of single crystal monolayer WS2 at the red cross in (b). (e) PL spectrum of WS2 in (d).

References

S1.	Memaran, S. et al. Pronounced photovoltaic response from multilayered transition-metal dichalcogenides pn-junctions. Nano Lett. 15, 7532–7538 (2015).

S2.	Wi, S. et al. Enhancement of photovoltaic response in multilayer MoS2 induced by plasma doping. ACS Nano 8, 5270–5281 (2014).

S3.	Cho, A. J., Song, M. K., Kang, D. W. & Kwon, J. Y. Two-dimensional WSe2/MoS2 p-n heterojunction-based transparent photovoltaic cell and its performance enhancement by fluoropolymer passivation. ACS Appl. Mater. Interfaces 10, 35972–35977 (2018).

S4.	Pawar, S. A. et al. Heterojunction solar cell based on n-MoS2/p-InP. Opt. Mater. 86, 576–581 (2018).

S5.	Nazif, N. K. et al. High-performance p-n junction transition metal dichalcogenide photovoltaic cells enabled by MoOx doping and passivation. Nano Lett. 21, 3443–3450 (2021).

S6.	Fontana, M. et al. Electron-hole transport and photovoltaic effect in gated MoS2 Schottky junctions. Sci. Rep. 3, 1634–8–13 (2013).

S7.	McVay, E., Zubair, A., Lin, Y., Nourbakhsh, A. & Palacios, T. Impact of Al2O3 passivation on the photovoltaic performance of vertical WSe2 Schottky junction solar cells. ACS Appl. Mater. Interfaces 12, 57987–57995 (2020).

S8.	Groenendijk, D. J. et al. Photovoltaic and photothermoelectric effect in a double-gated WSe2 device. Nano Lett. 14, 5846–5852 (2014).

S9.	Pospischil, A., Furchi, M. M. & Mueller, T. Solar-energy conversion and light emission in an atomic monolayer p-n diode. Nat. Nanotechnol. 9, 257–261 (2014).

S10.	Wang, L. & Sambur, J. B. Efficient ultrathin liquid junction photovoltaics based on transition metal dichalcogenides. Nano Lett. 19, 2960–2967 (2019).

S11.	Akama, T. et al. Schottky solar cell using few-layered transition metal dichalcogenides toward large-scale fabrication of semitransparent and flexible power generator. Sci. Rep. 7, 11967–1–10 (2017).