The use of Uio-66 Metal-Organic Frameworks as a high-performance catalyst for the isomerization process of endo- to exo-dicyclopentadiene in a solvent-free condition

Narjes Khaton Maghsoodi and Mohammad Hossein Keshavarz*

Faculty of Applied Sciences, Malek Ashtar University of Technology, Iran

# *Corresponding Author: Mohammad Hossein Keshavarz

E-mail: mhkeshavarz@mut-es.ac.ir; keshavarz7@gmail.com

Characterization of catalysts

The X-ray diffraction (XRD) patterns were recorded with AW-XDM300 X-ray Diffractometer at a step size of 0.05° with a Cu Ka radiation (λ=1.5406Å). BET surface area was analyzed by N2 sorption/desorption using at 77k with a Belsorp mini instrument and degassing at 200 °C under vacuum. The Fourier transform infrared (FT-IR) spectra were recorded on an Infralum-08 spectrophotometer in the range of 400–4000 cm−1. Gas chromatography–mass spectrometry (GC-MS) were analyzed using Agilent 6890 by 30 m length packed HP5((5%-phenyl)-methylpolysiloxane) column and mass selective  detector.

531

111

Figure S1. XRD patterns of UiO-66 and UiO-66-vac

Figure S2. FT-IR spectra of UiO-66 and UiO-66-vac

Figure S3. N2 adsorption-desorption isotherm of UiO-66 & UiO-66-vac.

- b)

c)

Figure S4. Effects of main factors on the yield of exo-DCPD: a) Temperature, b) Time and c) Wt% cat.

c)

a)

b)

Figure S5. Contours plots for main factors interactions on the isomerization endo-DCPD in the presence of UiO-66: a) Time-%Wt cat., b) Temperature-%Wt cat., and c) Temperature-Time

Table S1. ANOVA results of Response Surface model for yield in the isomerization of endo-DCPD to exo-DCPD using UiO-66 and UiO-66-vac

|  |  |  | a) UiO-66 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Source | Sum of Squares | df | Mean Square | F Value |  | p-value Prob > F |  |
| Model | 116.55 | 9 | 12.95 | 53.97 |  | < 0.0001 | significant |
| Temperature | 2.97 | 1 | 2.97 | 12.36 |  | 0.0056 | significant |
| Time | 39.04 | 1 | 39.04 | 162.69 |  | < 0.0001 | significant |
| Wt% Cat. | 7.86 | 1 | 7.86 | 32.77 |  | 0.0002 | significant |
| TemperatureTime | 0.13 | 1 | 0.13 | 0.52 |  | 0.4870 | not significant |
| TemperatureWt% Cat. | 28.12 | 1 | 28.12 | 117.20 |  | < 0.0001 | significant |
| TimeWt% Cat. | 10.12 | 1 | 10.12 | 42.19 |  | < 0.0001 | significant |
| Temperature 2 | 8.04 | 1 | 8.04 | 33.50 |  | 0.0002 | significant |
| Time 2 | 17.45 | 1 | 17.45 | 72.72 |  | < 0.0001 | significant |
| Wt% Cat.2 | 8.04 | 1 | 8.04 | 33.50 |  | 0.0002 | significant |
| Residual | 2.40 | 10 | 0.24 |  |  |  |  |
| Lack of Fit | 1.07 | 5 | 0.21 | 0.80 |  | 0.5939 | not significant |
| Pure Error | 1.33 | 5 | 0.27 |  |  |  |  |
| Cor Total | 118.95 | 19 |  |  |  |  |  |

b)UiO-66-vac

| Source | Sum of Squares | df | Mean Square | F Value | p-value Prob > F |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 1021.55 | 9 | 113.51 | 89.71 | < 0.0001 | significant |
| Temperature | 25.80 | 1 | 25.80 | 20.40 | 0.0011 | significant |
| Time | 371.96 | 1 | 371.96 | 293.99 | < 0.0001 | significant |
| Wt% Cat. | 32.57 | 1 | 32.57 | 25.74 | 0.0005 | significant |
| TemperatureTime | 0.13 | 1 | 0.13 | 0.099 | 0.7597 | not significant |
| TemperatureWt% Cat. | 190.12 | 1 | 190.12 | 150.27 | < 0.0001 | significant |
| TimeWt% Cat. | 78.12 | 1 | 78.12 | 61.75 | < 0.0001 | significant |
| Temperature 2 | 71.26 | 1 | 71.26 | 56.33 | < 0.0001 | significant |
| Time 2 | 172.64 | 1 | 172.64 | 136.45 | < 0.0001 | significant |
| Wt% Cat.2 | 139.17 | 1 | 139.17 | 110.00 | < 0.0001 | significant |
| Residual | 12.65 | 10 | 1.27 |  |  |  |
| Lack of Fit | 9.32 | 5 | 1.86 | 2.80 | 0.1418 | not significant |
| Pure Error | 3.33 | 5 | 0.67 |  |  |  |
| Cor Total | 1034.20 | 19 |  |  |  |  |