- Supporting Information

- Multilevel resistive switching memory based on a
CH3NH3PbI3-xClx film with potassium chloride
additives

- Fengzhen Lv*, Kang Ling†, Tingting Zhong, Fuchi Liu*, Xiaoguang Liang, Changming Zhu, Jun Liu and Wenjie Kong

- College of Physics and Technology, Guangxi Normal University, Yucai Road, Guilin 541000, China

*Corresponding author: E-mail:

lvfzh17@mailbox.gxnu.edu.cn, liufuchi@gxnu.edu.cn

- Fig. S1 Characteristic peak binding energy of Cl 2p3/2 and Cl 2p1/2 (199.0 eV and 200.4 eV) highlighted by the arrows.

Fig. S2 The top-view SEM image of the MAPIC films without the KCl additive.

Fig. S3 (a) The I-V characteristic of Au/MAPIC/ITO/Glass under the sweeping voltage of 0 V→1 V→0 V→-1 V→0 V. (b) The semi-logarithmic plots of the I-V curve of the Au/MAPIC/ITO/Glass devices under different VSETs (0.8 V and 1 V). The numbers and arrows represent the voltage sweeping sequences and directions, respectively.