Supporting Information

Tailoring Water Dissociation Energy by Platinum Single-Atom Catalyst Coupled with Transition Metal/metal Oxide Heterostructure for Accelerating Alkaline Hydrogen Evolution Reaction

Kai Ling Zhou,a Zelin Wang,a Chang Bao Han,*a Xiaoxing Ke,*a Changhao Wang,a Yuhong Jin,a Qianqian Zhang,a Jingbing Liu, a Hao Wang*a and Hui Yana

a. Faculty of Materials and Manufacturing, Beijing University of Technology, Beijing 100124, P. R. China

E-mail: cbhan@bjut.edu; kexiaoxing@bjut.edu.cn.cn; haowang@bjut.edu.cn

Figure S1. The electrochemical process with -3.0 V versus SCE for the deposition of NiO/Ni composite on the Ag NWs network.

Figure S2. The scanning electron microscopy (SEM) images of NiO/Ni on Ag NWs with different magnifications.

Figure S3. (a-b) Transmission electron microscopy (TEM) images, (c) high-resolution TEM (HRTEM) and (d) fast Fourier transform (FFT) images of Ag NWs supported NiO/Ni.

Figure S4. The elements mapping of Ag, Ni, and O in Ag NWs supported NiO/Ni.

Figure S5. The X-ray diffraction (XRD) patterns of NiO/Ni and NiO on Ag NWs.

Figure S6. X-ray photoelectron spectroscopy spectra of NiO/Ni and NiO.

Figure S7. The electrochemical process with -1.0 V versus SCE for the deposition of NiO on the Ag NWs network.

Figure S8. The SEM images of NiO on Ag NWs with different magnifications.

Figure S9. (a-b) TEM images, (c) HRTEM, and (d) FFT images of NiO on Ag NWs.

Figure S10. The electrochemical process with -1.2 V versus SCE for the deposition of metallic Ni on the Ag NWs network.

Figure S11. The SEM images of Ni on Ag NWs with different magnifications.

Figure S12. (a-b) TEM images and (c) HRTEM image of Ni.

Figure S13. XRD patterns of Ag NWs supported Ni, and the XRD patterns of Ag NWs supported NiO/Ni and NiO are given as the comparison.

Figure S14. The scanning transmission electron microscopy (STEM) images of PtSA-NiO/Ni.

Figure S15. The elements mapping of Ni, O, and Pt in PtSA-NiO/Ni.

Figure S16. HAADF-STEM images of (a) PtSA-NiO and (b) PtSA-Ni, respectively.

Figure S17. The normalized difference spectra for Pt L3-edge XANES using Pt foil as reference. The oxidation states are fitted by integrating the area of the white-line peak from 11557 to 11574 eV.

Figure S18. The DFT-optimized structure for (a) PtSA-NiO/Ni, (b) PtSA-NiO, and (c) PtSA-Ni catalysts, respectively based on the EXAFS analysis.

Figure S19. (a) Computational models of NiO/Ni heterostructure. (b) The localized electric field distribution of NiO/Ni heterostructure. (c) The localized electric field distribution of Pt atom at NiO/Ni phase junction. (d) 2D isosurface map of the cross-section consisting of Pt, Ni, and O atoms in PtSA-NiO/Ni with a unit of e A-3.

Figure S20. Highlighted total DOS of NiO/Ni and PtSA-NiO/Ni with aligned Fermi level.

Figure S21. Highlighted Pt 5d band of PtSA-NiO, PtSA-Ni, and PtSA-NiO/Ni with aligned Fermi level.

Figure S22. The optimal absorption site of metallic Ni for H, and O vacancies coupled NiO for HO.

Figure S23. O 1s spectra of NiO/Ni and NiO.

Figure S24. Calculated H2O adsorption energies of PtSA-NiO/Ni, PtSA-NiO and PtSA-Ni catalysts

Figure S25. The optimal absorption site of PtSA-NiO/Ni catalyst for the dissociation of H2O into OH and H.

Figure S26. The optimal absorption site of PtSA-NiO/Ni catalyst for the dissociated proton.

Figure S27. Cyclic voltammograms performed in 1 M KOH solution in the potential window without the participation of faradaic processes for (a) PtSA-NiO/Ni, (b) PtSA-NiO, (c) PtSA-Ni, and (d) NiO/Ni. (e) The corresponding scan rate dependence of the average currents.

Figure S28. HAADF-STEM image of PtSA-NiO/Ni after the stability test.

Figure S29. Elements mapping of PtSA-NiO/Ni after the stability test.

Figure S30. The double-layer capacitance measurement of PtSA-NiO/Ni after the stability test.

Table S1. FT-EXAFS fitting results of PtSA-NiO/Ni, PtSA-NiO and PtSA-Ni, and Pt foil was given as a reference.

|  | Shell | CN | R(Å) | σ2 | ΔE0 | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Pt foil | Pt-Pt | 12 | 2.760.01 | 0.004 | 10.40.6 | 0.0017 |
| PtSA-NiO/Ni | Pt-Ni | 5.870.5 | 2.600.01 | 0.012 | 9.22.0 | 0.0095 |
|  | Pt-O | 1.310.2 | 1.990.02 | 0.001 |  |  |
|  | Pt-Cl | 1.910.5 | 3.100.02 | 0.004 |  |  |
| PtSA-NiO | Pt-Ni | 2.140.2 | 2.700.01 | 0.005 | 18.61.8 | 0.0099 |
|  | Pt-O | 2.410.2 | 2.070.02 | 0.009 |  |  |
|  | Pt-Cl | 1.620.3 | 3.200.02 | 0.004 |  |  |
| PtSA-Ni | Pt-Ni | 4.970.5 | 2.630.01 | 0.010 | 16.92.4 | 0.0054 |
|  | Pt-Cl | 1.400.2 | 2.310.01 | 0.002 |  |  |

CN: coordination numbers of identical atoms; R: interatomic distance; σ2: Debye-Waller factors; ΔE0: energy shift. R factor: goodness of fit. Ѕ02 was set to 0.74, according to the experimental EXAFS fit of Pt foil reference by fixing CN as the known crystallographic value.

Table S2. Comparison of HER performances for Ag NWs supported PtSA-NiO/Ni with the reported HER catalysts.

|  | Electrocatalysts | Electrolyte | Overpotential at 10 mA cm-2 (mV) | Tafel slop (mV dec-1) | Reference |
| --- | --- | --- | --- | --- | --- |
| 1 | PtSA-NiO/Ni | 1.0 M KOH | 26 | 27 | This work |
| 2 | PtSA-C1N1 | 1.0 M KOH | 46 | 36.8 | Nat. Commun., 2020, 11:1029. |
| 3 | Ru-MoS2/CC | 1.0 M KOH | 41 | 114 | Appl. Catal., B, 2019, 249, 91. |
| 4 | PtSA-Co(OH)2 | 1.0 M KOH | 29 | 35 | Energy Environ. Sci., 2020, 13:3082. |
| 5 | RuCo@N-C | 1.0 M KOH | 28 | 31 | Nat. Commun., 2017, 8, 14969. |
| 6 | Ru-MoO2 | 1.0 M KOH | 29 | 44 | J. Mater. Chem. A, 2017, 5, 5475-5485. |
| 7 | PtNi NWs/C | 1.0 M KOH | 40 | - | Angew. Chem.Int. Ed., 2016, 55, 12859. |
| 8 | IrCo@N-C | 1.0 M KOH | 45 | 80 | Adv. Mater., 2018, 30,1705324. |
| 9 | Hexagonal-PtNi | 1.0 M KOH | 65 | 74 | Nat. Commun., 2017, 8, 15131. |
| 10 | Ru/C3N4/C | 0.1 M KOH | 79 | - | J. Am. Chem. Soc., 2016, 138, 16174. |
| 11 | Cu2-xS@Ru | 1.0 M KOH | 82 | 48 | Small, 2017, 13, 1700052. |
| 12 | PtNi-O/C | 0.1 M KOH | 40 | 79 | J. Am. Chem. Soc., 2018, 140, 9046. |
| 13 | Pt-Ni ASs | 1.0 M KOH | 28 | 27 | Adv. Mater., 2018,30, 1801741. |
| 14 | Pt3.6Ni-S NWs | 0.1 M KOH | 38 | - | Angew Chem. Int. Ed., 2018, 130,11852. |
| 15 | Rh2P | 1.0 M KOH | 30 | - | Adv. Energy Mater., 2018, 8,1703489. |
| 16 | hcp excavated PtNi | 0.1 M KOH | 38 | 42 | Inorg. Chem. Front., 2018,5, 1365. |
| 17 | Ni(OH)2-PtO2 NS/Ti | 0.1 M KOH | 44 | 89 | J. Mater. Chem. A, 2018, 6, 1967. |
| 18 | Pt3Ni2 NWs-S/C | 0.1 M KOH | 45 | - | Nat. Commun., 2017, 8, 14580. |
| 19 | Mo2TiC2Tx-PtSA | 0.5 M H2SO4 | 30 | 30 | Nat. Catal., 2018, 1, 985. |
| 20 | PtSA/OLC | 0.5 M H2SO4 | 38 | 36 | Nat. Energy, 2019, 4, 512. |
| 21 | Pt-MWCNTs | 0.5 M H2SO4 | 44 | 30 | Nano Energy, 2019, 63, 1038. |
| 22 | Pt-MoS2 | 0.1 M H2SO4 | 60 | 96 | Energy Environ. Sci., 2015, 8, 1594. |
| 23 | er-WS2-Pt | 0.5 M H2SO4 | 40 | 27 | Adv. Mater., 2017, 1704779. |
| 24 | Pt@PCM | 0.5 M H2SO4 | 105 | 63 | Sci. Adv., 2018, 4, 6657. |
| 25 | ALD50 Pt/NGNs | 0.5 M H2SO4 | 39 | 29 | Nat. Commun., 2016, 7, 13638. |
| 26 | PtSA/m-WO3-x | 0.5 M H2SO4 | 38 | 45 | Angew. Chem., Int. Ed., 2019, 131, 16184. |
| 27 | PtSA/S-C | 0.5 M H2SO4 | 53 | 46 | Nat. Communicat., 2019, 10, 1. |
| 28 | Ru/N-C NWs | 0.1 M H2SO4 | 47 | 14 | Nat. Communicat., 2019, 10, 1. |
| 29 | Pd-Graphdiyne | 0.5 M H2SO4 | 55 | 47 | iScience, 2019, 11, 31. |
| 30 | PtNx/TiO2 | 0.5 M H2SO4 | 67 | 34 | Nano Energy, 2020, 73, 104739 |
| 31 | PtML/Au NF/Ni foam | 0.5 M H2SO4 | 60 | 53 | Sci. Adv., 2015, 1, e1400268. |
| 32 | Rh/SiNW | 0.5 M H2SO4 | 85 | 24 | Nat. Commun., 2016, 7, 12272. |
| 33 | Pt@PM | 0.5 M H2SO4 | 106 | 65 | Sci. Adv., 2018, 4, eaao6657. |
| 34 | RuP2@NPC | 0.5 M H2SO4 | 38 | 38 | Angew. Chem., Int. Ed., 2017, 56, 11559. |
| 35 | NiO-Ni/CNT | 1.0 M KOH | 86 | 82 | Nat. Commun., 2014, 5, 4695. |
| 36 | Ni NP/Ni-NC | 1.0 M KOH | 147 | 114 | Energy Environ. Sci., 2019, 12, 149. |
| 37 | Ni/NiP | 1.0 M KOH | 130 | 58 | Adv. Funct. Mater., 2016, 26, 3314. |
| 38 | CoP/NCNHP | 1.0 M KOH | 115 | 66 | J. Am. Chem. Soc., 2018, 140, 2610. |
| 39 | Co2P | 1.0 M KOH | 160 | 61 | Adv. Mater., 2017, 29, 1606980. |
| 40 | NiCoN/C nanocages | 1.0 M KOH | 103 | - | Adv. Mater., 2019, 31, 1805541. |
| 41 | Co doped β-Mo2C | 1.0 M KOH | 141 | 62 | Adv. Funct. Mater., 2020, 30, 2000561. |
| 42 | NiP2 NS/CC | 1.0 M KOH | 102 | 64 | Nanoscale, 2014, 6, 13440. |

Supplementary Note 1. Turnover frequency (TOF) calculation of the Pt-based catalysts.

The TOF per Pt site of the fabricated Pt-based catalysts in this work was calculated by using the formula:

TOF (H2/s) =  # total hydrogen turnover per geometric area# active sites per geometric area

The total number of hydrogen turnovers could be obtained by the current density as the following formula:

# total hydrogen turnover:

= (|j|mAcm2) (1 C/s1000 mA) (1 mol e-96485.3 C) ( 1 mol2 mol e-) ( 6.022×1023 molecules H21 mol H2)

= 3.12×1015 H2/scm2  mAcm2

The number of catalytic active sites in the Pt-based catalysts was calculated according to the mass loading on the electrode, the Pt contents, and the Pt atomic weight with a hypothesis that each Pt atom accounts for one catalytic active site:

# Pt active site:

=catalyst loading per geometric area x g/cm2×Pt wt%Pt Mw (g/mol)×(6.022×1023Pt atoms1 mol Pt)

Hence, the Pt active site in PtSA-NiO/Ni can be calculated to be:

= 0.0066×10-3195.08 g/mol ×(6.022×1023Pt atoms1 mol Pt)

= 2.03×1016

So, the TOFs of per Pt site in PtSA-NiO/Ni can be calculated to be:

= 3.12×10152.03×1016×|j|

= 0.18×|j|