Supporting information

Preparation and properties of spirotetramat nanoparticles base on mesoporous silica of different particle sizes

Zhichao Wang 1, Wangjin Xu 1, Zhiyuan Meng 1, 2 *, Tianle Fan 1,

Chunmei Yang 1, Jianjun Wang 1, Xiaojun Chen 1 *

1 School of Horticulture and Plant Protection, Yangzhou University / Joint International Research Laboratory of Agriculture & Agri-Product Safety, Yangzhou University, Yangzhou 225009, China

2 College of Guangling, Yangzhou University, Yangzhou, Jiangsu 225009, China.

*Corresponding author:

Xiaojun Chen, School of Horticulture and Plant Protection, Yangzhou University / Joint International Research Laboratory of Agriculture & Agri-Product Safety, Yangzhou University, Yangzhou 225009, China

E-mail: cxj @yzu.edu.cn

Zhiyuan Meng, School of Horticulture and Plant Protection, Yangzhou University / College of Guangling, Yangzhou University, Yangzhou, Jiangsu 225009, China. E-mail: zymeng@yzu.edu.cn

Table S1 DLS analysis of MSNs(A), MSNs(B) and MSNs(C)

| Sample | Average grain diameter (nm) | PdI |
| --- | --- | --- |
| MSNs-100 | 112.5 | 0.107 |
| MSNs-200 | 200.1 | 0.002 |
| MSNs-400 | 439.4 | 0.025 |

Table S2 Physical adsorption analysis of three particle size MSNs

| Samples | Surface area (m2/g) | Pore Volume (cm3/g) | Pore diameter (nm) |
| --- | --- | --- | --- |
| MSNs-100 nm | 742 | 0.76 | 4.1 |
| MSNs-200 nm | 332 | 0.28 | 3.4 |
| MSNs-400 nm | 461 | 0.25 | 2.2 |