Ordered Mesoporous Silica (SBA-15) Anchored Tungsten and Molybdenum Aminophenolate Complexes: as Efficient and Reusable Catalysts for Selective Oxidation of Sulfides with H2O2

Iraj Saberikia1, Elham Safaei*2, Babak Karimi1

1Institute for Advanced Studies in Basic Sciences (IASBS), 45137-66731, Zanjan, Iran

2Department of Chemistry, College of Sciences, Shiraz University, Shiraz, 71454, Iran

Correspondence

Elham Safaei, Department of Chemistry, College of Sciences, Shiraz University, Shiraz, 71454, Iran

Email: e.safaei@shirazu.ac.ir

Fig. S1: FT-IR spectra of SBA-15@AP-LPro-Mo

Fig. S2: FT-IR spectra of SBA-15@AP-LPro-W

Fig. S3: Thermo-gravimetric analysis (TGA) of SBA-15@AP-LPro-Mo

Fig. S4: Thermo-gravimetric analysis (TGA) of SBA-15@AP-LPro-W

Fig. S5: SEM-EDX spectra of SBA-15@AP-LPro-Mo

Fig. S6: SEM-EDX spectra of SBA-15@AP-LPro-Mo

Table S1: Textural properties of SBA-15, SBA-15@AP, SBA-15@AP-LPro-Mo and SBA-15@AP-LPro-W

| Material | SBET a (m2g-1) | Vp b (cm3g-1) | DBJH c (nm) | Loading of M (M= Mo & W) (mmol.g-1)e |
| --- | --- | --- | --- | --- |
| SBA-15@AP | 660 | 0.9 | 7.06 | - |
| SBA-15@AP-LPro-Mo | 406 | 0.72 | 7.04 | 0.32 |
| SBA-15@AP-LPro-W | 372 | 0.57 | 9.20 | 0.41 |
| Re-SBA-15@AP-LPro-Mo | 315 | 0.56 | 7.91 | 0.29 |
| Re-SBA-15@AP-LPro-W | 197 | 0.40 | 6.18 | 0.38 |

[a] SBET = specific surface area derived from linear part of adsorbed nitrogen in  the range from 0.05 to 0.3.

[b] Vp = pore volume derived from adsorbed nitrogen from relative pressure ≈ 0.99.

[c] DBJH = pore size distributions calculated from the adsorption branch using BJH method.

[d] Calculated using elemental analysis (CHN).

[e] Estimated by ICP techniques.

[f] Estimated after 5 run.