Supplementary Information
Self-reduction assisted MXene/Silver composite Tencel cellulose-based fabric with electrothermal conversion and NIR photothermal actuation

Han Li1, Yinuo Pan1, Zhaoqun Du1*

Engineering Research Center of Technical Textiles, Ministry of Education, Donghua University, Shanghai, China 201620

E-mail: duzq@dhu.edu.cn

Figure S1. Resistance values under different dip-coating times.

Table S1. The O 1s XPS peak fitting results of MXene, in which Peak BE represents Peak Binding Energy, and FWHM represents full-widths at half maximum.

| Name | Peak BE | FWHM eV | Area (P) CPS.eV | Atomic % |
| --- | --- | --- | --- | --- |
| TiO2 | 530.02 | 1.14 | 10242.16 | 15.35 |
| C-Ti-Ox(I) | 531.06 | 1.35 | 20257.45 | 30.38 |
| C-Ti-(OH)x | 532.01 | 1.37 | 16298.48 | 24.46 |
| Al2O3 | 532.89 | 1.03 | 6676.81 | 10.03 |
| H2Oads | 533.77 | 1.19 | 8716.84 | 13.1 |
| Al (OF)x | 534.71 | 1.2 | 4453.86 | 6.7 |

Table S2. The F 1s XPS peak fitting results of MXene.

| Name | Peak BE | FWHM eV | Area (P) CPS.eV | Atomic % |
| --- | --- | --- | --- | --- |
| C-Ti-Fx(III) | 685.13 | 1.31 | 106445.19 | 32.96 |
| Al Fx | 685.86 | 1.28 | 182277.39 | 56.48 |
| Al (OF)x | 686.81 | 1.22 | 34050.05 | 10.56 |

Note S1. Reasonable and simplified equations for selective etching of Ti3AlC2 in HCl solution: (Naguib M et al., 2011)

LiF + HCl = HF + HCl                                                 (1)

Ti3AlC2 + 3HF = AlF3 + 3/2H2 + Ti3C2                                    (2)

Ti3C2 + 2H2O = Ti3C2(OH)2 + H2                                        (3)

Ti3C2 + 2HF = Ti3C2F2 + H2                                            (4)

Naguib, M., Kurtoglu, M., Presser, V., Lu, J., Niu, J., Heon, M., Hultman, L., Gogotsi, Y., Barsoum, M.W. (2011) Two‐dimensional nanocrystals produced by exfoliation of Ti3AlC2. Adv. Mater. 23: 4248-4253.