Supplementary Material

Supplementary Tables and figures

Table S1. Cycle parameters for sintering Lava™ Plus

| Cycle | Cycle stages | Cycle Parameters |
| --- | --- | --- |
| Standard sintering cycle | Drying | 2 h in open, cold furnace or at room temperature |
|  | Heating | 20 ℃/min to 800 ℃ |
|  | Heating | 10 ℃/min to 1450 ℃ |
|  | Holding time | 120 min at 1450 ℃ |
|  | Cooling off | Maximum 15 ℃/min to 800 ℃ |
|  | Cooling off | Maximum 20 ℃/min to 250 ℃ |