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Supplementary Tables and figures
Table S1. Cycle parameters for sintering Lava™ Plus
	Cycle
	Cycle stages
	Cycle Parameters

	Standard sintering cycle
	Drying
	2 h in open, cold furnace or at room temperature

	
	Heating
	20 ℃/min to 800 ℃

	
	Heating
	10 ℃/min to 1450 ℃

	
	Holding time
	120 min at 1450 ℃

	
	Cooling off
	Maximum 15 ℃/min to 800 ℃

	
	Cooling off
	Maximum 20 ℃/min to 250 ℃



