Supplementary Information

Supplementary Information for

Efficient integrated photo-charging storage device operating at

3 V

Juyeon Han†, Junyeong Lee†, Myeongjin Kim, Hyojung Cha, Sungjin Jo*, Jeeyoung Yoo*

†These authors contributed equally to this work.

*Correspondences to: sungjin@knu.ac.kr, jyoo@knu.ac.kr

This PDF file includes:

Supplementary Figures 1 to 10

Supplementary Table 1 to 6

Supplementary References 1 to 6

Supplementary Fig. 1 | Schematic of series-connected PSC. The gray color with hatch means patterned FTO electrode. Brown color means patterned layer of ETL/MAPbI3/HTL. And dark gray color means Ag electrode.

Supplementary Fig. 2 | Schematic illustration and linear sweep voltage graph of ionogel. a, Black is polymerized PUA while red and blue represent the cations and anions of EMITFSI, respectively. b, LSV of ionogel with a scan rate of 10 mV s−1.

Supplementary Fig. 3 | GCD profile of SC with different current densities.

Supplementary Fig. 4 | The performance of 4-PSCD with different discharging current densities under AM 1.5 G illumination. a, specific capacitance. b, storage efficiency.

Supplementary Fig. 5 | Ragone plot of 4-PSCD.

Supplementary Fig. 6 | Photo-charging and galvanostatic discharging profile. a, single-PCSD. b, 2-PCSD. c, 3-PCSD. d, 4-PCSD.

Supplementary Fig. 7 | Overall efficiency depending on the number of series cell at 1 mA cm−2 discharging.

Supplementary Fig. 8 | The performance of 4-PSCD with different discharging current densities under 0.1 sun illumination. a, the specific capacitance. b, storage efficiency. c, overall efficiency.

Supplementary Fig. 9 | The voltage profile of photo-charging and galvanostatic discharging of 20 mA cm−2 for 100 cycles.

Supplementary Fig. 10 | The weekly specific energy density of encapsulated 4-PCSD under ambient condition.

| Device | Jsc [mA cm−2] | Voc [V] | FF [%] | PCE [%] |
| --- | --- | --- | --- | --- |
| Small area | 21.84 | 0.99 | 69.50 | 15.07 |
| Large area | 21.56 | 1.02 | 66.33 | 14.60 |

Supplementary Table 1 | Photovoltaic performance parameters of PSC using small size electrode and large size electrode.

| Device | Isc [mA] | Voc [V] | FF [%] | PCE [%] |
| --- | --- | --- | --- | --- |
| Series | 5.74 | 4.07 | 64.40 | 14.46 |
| Individual | 5.58 | 1.02 | 66.33 | 14.60 |

Supplementary Table 2 | Photovoltaic performance parameters of series-connected PSC and single PSC.

| Light intensity | Jsc [mA cm−2] | Voc [V] | FF [%] | PCE [%] |
| --- | --- | --- | --- | --- |
| 0.1 sun | 1.97 | 0.93 | 70.15 | 12.88 |

Supplementary Table 3 | Photovoltaic performance parameters of PSC under 0.1sun illumination.

| Current density [A g−1] | Energy density [Wh kg−1] | Power density [W kg−1] |
| --- | --- | --- |
| 0.1 | 4.27 | 147.94 |
| 0.2 | 4.04 | 285.70 |
| 0.5 | 3.45 | 622.66 |
| 1 | 2.68 | 1073.30 |

Supplementary Table 4 | The specific energy density and specific power density of SC.

| Condition | Device | Rs [Ω] | Rct [Ω] | Rrec [Ω] | Cdl [F] | Wo |
| --- | --- | --- | --- | --- | --- | --- |
| Dark | PSC | 4.57×101 | 1.80×105 | 1.10×105 | - | - |
|  | SC | 3.55×101 | 1.10×102 | - | 1.65×10-6 | 8.53×10-1 |
|  | 4-PCSD | 7.69×101 | 2.04×104 | 2.13×104 | - | - |
| Light | PSC | 7.06×101 | 3.50×102 | - | - | - |
|  | SC | 3.34×101 | 8.98×101 | - | 1.30×10-6 | 3.21×10-3 |
|  | 4-PCSD | 3.56×101 | 9.53×101 | - | 1.74×10-6 | 5.70×10-3 |

Supplementary Table 5 | The parameters of EIS of PSC, SC, and 4-PCSD with light/dark condition.

| PV cell | Supercapacitor |  | Current density [mA cm–2] | Storage efficiency [%] | Conversion efficiency [%] | Overall efficiency [%] | Working Voltage [V] | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Electrode | Electrolyte |  |  |  |  |  |  |
| GaAs solar cell | MnO2@C//VN | MgSO4/PAM | 1 | 67.90 | 25.88 | 17.57 | 2.2 | 1 |
| SiNW/PEDOT:PSS solar cell | laser-scribed graphene | - M H2SO4 / porous separator | 5.48 A g–1 | - | 12.37 | 2.92 | 0.45 | 2 |
| SiNW/PEDOT:PSS hybrid solar cell | polypyrrole plate | H3PO4/PVA | 3 | - | 13.39 | 10.5 | 0.55 | 3 |
| Perovskite solar cell | PANI/CNT | H2SO4/PVA | 1 | 70.9 | 22.1 | - | 0.7 | 4 |
| Perovskite solar cell | PEDOT-carbon | 1 M LiClO4/ tetramethylammonium iodide in isopropanol | 1 | 73.77 | 6.37 | 4.70 | 0.71 | 5 |
| Perovskite solar cell | mesoporous N-doped carbon nanospheres | H2SO4/PVA | 0.5 | 92 | 12.5 | 11.5 | 1.05 | 6 |
| Perovskite solar cell | Activated carbon | EMITFSI/PUA | 1 | 94.08 | 14.46 | 13.17 | 3 | This work |

Supplementary Table 6 | Comparisons between prepared PSCD and other reported integration of solar cell-SC.

Supplementary References

- Tian, Z. et al. Printable magnesium ion quasi-solid-state asymmetric supercapacitors for flexible solar-charging integrated units. Nat. Commun. 10, 1–11 (2019).

- Liu, H., Li, M., Kaner, R. B., Chen, S. & Pei, Q. Monolithically Integrated Self-Charging Power Pack Consisting of a Silicon Nanowire Array/Conductive Polymer Hybrid Solar Cell and a Laser-Scribed Graphene Supercapacitor. ACS Appl. Mater. Interfaces 10, 15609–15615 (2018).

- Liu, R. et al. Silicon Nanowire/Polymer Hybrid Solar Cell-Supercapacitor: A Self-Charging Power Unit with a Total Efficiency of 10.5%. Nano Lett. 17, 4240–4247 (2017).

- Liu, R., Liu, C. & Fan, S. A photocapacitor based on organometal halide perovskite and PANI/CNT composites integrated using a CNT bridge. J. Mater. Chem. A 5, 23078–23084 (2017).

- Xu, J., Ku, Z., Zhang, Y., Chao, D. & Fan, H. J. Integrated Photo-Supercapacitor Based on PEDOT Modified Printable Perovskite Solar Cell. Adv. Mater. Technol. 1, 1–5 (2016).

- Berestok, T. et al. High-Efficiency Monolithic Photosupercapacitors: Smart Integration of a Perovskite Solar Cell with a Mesoporous Carbon Double-Layer Capacitor. Sol. RRL 5, 1–13 (2021).