Supporting Information

Multiple valence bands convergence and strong phonon scattering lead to high thermoelectric performance in p-type PbSe

Yingcai Zhu,1 Dongyang Wang,1 Tao Hong,1 Lei Hu,2 Toshiaki Ina,3 Shaoping, Zhan,1 Bingchao Qin,1 Haonan Shi,1 Lizhong Su,1 Xiang Gao,4 Li-Dong Zhao1*

1School of Materials Science and Engineering, Beihang University, Beijing 100191, China

2State Key Laboratory for Mechanical Behavior of Materials, Xi’an Jiaotong University, Xi’an 710049, China

3Research and Utilization Division, Japan Synchrotron Radiation Research Institute (JASRI/SPring-8), Sayo, Hyogo, Japan

4Center for High Pressure Science and Technology Advanced Research (HPSTAR), Beijing, 100094, China

*zhaolidong@buaa.edu.cn (L.-D. Zhao).

Transport properties estimation. In single parabolic band (SPB) model, the Seebeck coefficient can be expressed as:[1]

S=kBe2F1(η)F0(η)-η                                                       (S1)

where kB is the Boltzmann constant, e is the electron charge, Fj is the Fermi-Dirac integral Fj(η)=0∞ξjdξ1+exp⁡(ξ-η), and η is the reduced Fermi level EFkBT. Here, we assume that the acoustic-phonon scattering (APS) is the dominating scattering mechanism for the carriers.

Under this condition, the chemical carrier concentration (n) can be described as:

n=4π2m*kBTh23/2F1/2η                                                  (S2)

The Hall carrier concentration (nH) is related to n via nH = n/rH, where rH is the Hall factor and it is given by:

rH=34F1/2η F-1/2ηF02η                                                     (S3)

For a given reduced Fermi level η, the Seebeck coefficient and Hall factor will be determined. Then, the effective mass (m*) will be obtained via measuring nH through Hall measurement. Therefore, the Seebeck coefficient (S) versus Hall carrier concentration (nH) (Pisarenko plot) will be obtained with varying η for a constant m*.

Within the APS assumption, the Hall carrier mobility (μH) is represented as:

μH=em*πħ4vL2ρ2Edef2m*kT3/2 F-1/2η2F0η                                            (S4)

where vL is the longitudinal sound velocity, ρ is the density of sample, Edef is the deformation potential. The Edef can be expressed as:

ǀEdefǀ=hkB23π2vL2ρTm*κLB1/2                                                  (S5)

B is the quality factor and it is given by: [2]

B=kBe2σE0TκL                                                         (S6)

σE0= σ/F0η                                                          (S7)

Therefore, the relation between μH and nH can be estimated via equation (S1-S7).

Lorenz number calculation. The electronic contribution to the thermal conductivity was calculated via the Wiedemann-Franz law (κe = LσT), where the Lozenz number (L) is given by:

L=kB2e23F0ηF2η-4F12ηF02(η)                                            (S8)

Callaway model. We can estimate the lattice thermal conductivity considering the effect of defects using the Callaway model: [3]

κLκ0=tan-1uu                                                        (S9)

Here, κ0 is the lattice conductivity of purity sample without considering defects, while the κL is the lattice thermal conductivity of doping material with defects. The u is a disorder parameter and it depends on the properties of pure material:

u2=6π5V21/32kBvavgκ0Γ                                                  (S10)

where V, vavg, Γ are the average volume per atom, average speed of sound, and the disorder scattering parameter, respectively. We use the Callaway model to estimate the lattice thermal conductivity of Pb0.98Na0.02Se-x%AgInSe2. To simplify, we assume the  Pb0.98Na0.02 as a whole and term it as PN. Then, the chemical formula can be written as PN2-2y AgyInySe2 (y = 2x/(100+2x)). Only considering the mass variation, the Γ can be expressed as:

Γ=1-yMPN-M12+yMAg-M12+1-yMPN-M22+yMIn-M12/42MSe+M1+M2/42         (S11)

MPN=0.98MPb+0.02MNa                             (S12)

M1=1-yMPN+yMAg                               (S13)

M2=1-yMPN+yMIn                               (S14)

For a given y, the values of V, vavg and κ0 are determined as the linear interpolation between the values of the end-member species (Pb0.98Na0.02Se and AgInSe2), respectively.

Figure S1. Hall carrier concentrations of Pb0.98Na0.02Se-x%AgInSe2 (LISS) with increasing AgInSe2 content at 303K.

Figure S2. Electronic band structures of (a) Pb26AgSe27 and (b) Pb26InSe27. (c) The energy offset (ΔE1-2) between L and Σ valence band. (d) Theoretical bandgaps (Eg) for pristine, Ag-doped, In-doped and Ag-In co-doped PbSe.

Figure S3. (a) Temperature-dependent synchrotron radiation x-ray diffraction (SR-XRD) patterns for Pb0.98Na0.02Se-2% AgInSe2. (b) The refined lattice parameters as a function of temperature.

Figure S4. The electronic band structures of Pb25AgInSe27 at various temperature: (a) 373 K, (b) 473 K, (c) 573 K, (d) 623 K, (e) 673 K, (f) 773 K.

Figure S5. (a) Temperature dependence of Hall coefficient (RH) of Pb0.98Na0.02Se-2.05% AgInSe2. (b) Effective mass as a function of temperature for Pb0.98Na0.02Se-2.05% AgInSe2 and Pb1-xNaxSe.

Figure S6. Temperature-dependent (a) Lorenz number (L) and (b) electronic contribution to the thermal conductivity (κe) for Pb0.98Na0.02Se-x% AgInSe2 (LISS).

Figure S7. (a) Heat capacities of Pb0.98Na0.02Se - x% AgInSe2 calculated by Dulong-Petit law and the empirical equation (Cp/kB atom-1 = 3.07 + 4.7 × 10-4 (T/K-300)). (b) The figure-of-merit ZT of Pb0.98Na0.02Se - x% AgInSe2 with different Cp.

Figure S8. Temperature-dependent (a) electrical conductivity, (b) Seebeck coefficient, (c) total thermal conductivity, and (d) figure-of-merit ZT for several x=2.05 and x=2.1 samples, respectively.

Figure S9. Annular dark-field (ADF) STEM image (a, b) of Pb0.98Na0.02Se-2.05%AgInSe2 sample and the corresponding energy dispersive X-ray spectroscopy (EDS) elements distribution mappings for (c) Ag, (d) In, (e) Na, (f) Se and (g) Pb elements, respectively.

Figure S10. Comparison of experimental XANES spectra of (a) Se K-edge and (b) Pb L3-edge between PbSe and Pb0.98Na0.02Se-2%AgInSe2.

Figure S11. Experimental XANES spectra of Ag K-edge for Pb0.98Na0.02Se-2% AgInSe2 (red dots), and AgInSe2 (orange line), respectively. Theoretical XANES spectrum of Ag K-edge for Ag-doped PbSe assuming that Ag occupy the Pb site. The black line represents a linear combination fitting result of Ag K-edge of Pb0.98Na0.02Se-2% AgInSe2 considering that the Ag K-edge of AgInSe2 and Ag-doped PbSe serves as standards.

Table S1. Longitudinal, transverse and average sound velocity of Pb0.98Na0.02Se - x% AgInSe2. The Poisson ration (vp) is calculated by vp= 1-2vtvl22-2vtvl2, and then the Grüneisen parameter (γ) is obtained using γ = 321+vp2-3vp.

| Sample | vl (m/s) | vt (m/s) | vavg (m/s) | vp | γ |
| --- | --- | --- | --- | --- | --- |
| x=0 | 3165.6 | 1708.6 | 1907.1 | 0.294 | 1.74 |
| x=0.5 | 3192.9 | 1726.9 | 1927.3 | 0.293 | 1.73 |
| x=1 | 3214.7 | 1726.1 | 1927.4 | 0.297 | 1.75 |
| x=1.5 | 3151.7 | 1715.4 | 1913.5 | 0.289 | 1.71 |
| x=2 | 3217.4 | 1720.9 | 1922.1 | 0.299 | 1.77 |
| x=2.05 | 3148.7 | 1718.3 | 1916.4 | 0.288 | 1.70 |
| x=2.1 | 3179.8 | 1720.3 | 1919.9 | 0.293 | 1.73 |
| x=2.15 | 3149.7 | 1718.8 | 1916.9 | 0.288 | 1.70 |

Table S2. LCF fitting results of In K-edge and Ag K-edge of Pb0.98Na0.02Se - 2% AgInSe2.

| Atom | Atomic occupied ratio in standards |  |
| --- | --- | --- |
|  | @ Pb site in PbSe | AgInSe2 |
| In | 13.7% | 86.3% |
| Ag | 16.0% | 84.0% |

References

[1]	A. F. May, G. J. Snyder, CRC Press: Boca Raton, FL 2012, Vol. 1, pp 231.

[2]	S. D. Kang, Snyder, G. J., Nat. Mater. 2017, 16, 252.

[3]	C. Joseph, v. B. Hans C., Phys. Rev. 1960, 120, 1149.