Table 2. Oxidation of sulfides to sulfoxides with 30% H2O2 catalyzed by Cell/Bent@V Complex nanocomposite at room temperature a
	Entry

	Sulfide
	Product
	Time (h)
	Yield (%)b

	

1
	


	

	

2

	

90

	

2
	


	

	

2
	

90

	


3
	

	

	


2
	


85

	

4
	

	

	

2
	

90

	

5
	

	

	

2
	

85

	

6
	


	

	

2
	

90

	

7c
	

	

	

2
	

82

	
8c
	

	

	
2.5
	
85

	

9c
	

	

	

2.5
	

83


	

10c
	


	

	

2.5
	

83








[bookmark: _Hlk96937325]a Reaction conditions: sulfide (1 mmol), EtOH (2 ml), 30% H2O2 (3 mmol), catalyst (20 mg). b Isolated yields. c Yields determined by GC.
[bookmark: _GoBack]
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