Table 2. Oxidation of sulfides to sulfoxides with 30% H2O2 catalyzed by Cell/Bent@V Complex nanocomposite at room temperature a

| Entry | Sulfide | Product | Time (h) | Yield (%)b |
| --- | --- | --- | --- | --- |
| 1 |  |  | 2 | 90 |
| 2 |  |  | 2 | 90 |
| 3 |  |  | 2 | 85 |
| 4 |  |  | 2 | 90 |
| 5 |  |  | 2 | 85 |
| 6 |  |  | 2 | 90 |
| 7c |  |  | 2 | 82 |
| 8c |  |  | 2.5 | 85 |
| 9c |  |  | 2.5 | 83 |
| 10c |  |  | 2.5 | 83 |

a Reaction conditions: sulfide (1 mmol), EtOH (2 ml), 30% H2O2 (3 mmol), catalyst (20 mg). b Isolated yields. c Yields determined by GC.