Table 4. Oxidative coupling of thiols into disulfides by urea/H2O2 catalyzed by Cell/Bent@V Complex nanocomposite at room temperature a

| Entry | Thiol | Product | Time (h) | Yield (%)b |
| --- | --- | --- | --- | --- |
| 1 |  |  | 1.25 | 95 |
| 2 |  |  | 1.25 | 85 |
| 3 |  |  | 1.25 | 92 |
| 4 |  |  | 1.25 | 90 |
| 5 |  |  | 1.5 | 87 |
| 6c |  |  | 1.5 | 68 |

a Reaction conditions: thiol (1 mmol), CH3CN (2 ml), UHP (5 mmol), catalyst (20 mg). b Isolated yields. c Yield determined by GC.