Supporting Information

Improvement of the functional properties of cellulose acetate film by incorporating with glycerol and n-propanol

Wei Dai1, Xiaoyan Li1, Yangfeng Wu, Kairong Zang, Zhengqiu Yuan*, Jianxian Zeng, Jian Jian, Hu Zhou*

(School of Chemistry and Chemical Engineering, Hunan University of Science and Technology, Xiangtan, 411201, China)

Corresponding author:

*E-mail: yuanzhengqiu@126.com (Z. Yuan), hnustchemzhou@163.com (H. Zhou)

1: These authors contributed equally to this work.

Fig. S1. Films prepared with different concentration of glycerol as plasticizer. (a) CAF; (b) CAF-5G; (c) CAF-10G; (d) CAF-15G. The solutions were casted into petri dishes, and the mixtures were solvent vapor annealed in a drying chamber under an acetone vapor atmosphere.

Fig. S2. Films prepared with different alcohols as proposed transparent agent. (a) methanol; (b) ethanol; (c) n-propanol; (d) 1-butanol; (e) 1-pentanol.

Fig. S3. Hydrophobic and hydrophilic performance of the prepared films.

Table S1. The compositions of cast solution for different films

| Samples | Cast solution |  |  |  |
| --- | --- | --- | --- | --- |
|  | CA (g) | THF (mL) | Glycerol (g) | n-Propanol (mL) |
| CAF | 6 | 45 | 0 | 0 |
| CAF-5G | 6 | 45 | 0.3 | 0 |
| CAF-10G | 6 | 45 | 0.6 | 0 |
| CAF-15G | 6 | 45 | 0.9 | 0 |
| CAGF-0.6P | 6 | 45 | 0.3 | 0.27 |
| CAGF-1.2P | 6 | 45 | 0.3 | 0.54 |
| CAGF-1.8P | 6 | 45 | 0.3 | 0.80 |
| CAGF-2.4P | 6 | 45 | 0.3 | 1.08 |