Supporting Information

ML-guided discovery of La-Co-Pb ternary compounds involving immiscible pairs of Co and Pb elements

Renhai Wang1,3, Weiyi Xia2,3, Tyler J. Slade2,3, Xinyu Fan4, Huafeng Dong1, Kai-Ming Ho2,3, Paul C. Canfield2,3, Cai-Zhuang Wang2,3*

1School of Physics and Optoelectronic Engineering, Guangdong University of Technology, Guangzhou 510006, China

2Ames Laboratory-USDOE, Iowa State University, Ames, Iowa 50011, USA

3Department of Physics and Astronomy, Iowa State University, Ames, Iowa 50011, United States

4Department of Physics, University of Science and Technology of China, Hefei 230026, China

Figure S1. The Co-Pb binary phase diagram from ASM Alloy Phase Diagram DatabaseTM.

Figure S2. The La5CoPb3, La12Co6Pb and La6Co13Pb structures predicted by our ML approach after DFT optimization (top raw) that are the same as the three known La-Co-Pb compounds (bottom raw).

Figure S3. Calculated PXRD spectrum of the newly predicted La3CoPb phase with the lattice constant reduced by 2.0% is compared with the experimental powder diffraction patterns obtained from pieces of the arc melted La-Co-Pb pellet (left: 3:1:1 sample, right: 18:28:3 sample). The experimental samples are annealed at 650°C for one week.

Figure S4. Powder diffraction patterns obtained from pieces of the arc melted La-Co-Pb pellet (left column: the 3:1:1 sample; right column: the 18:28:3 sample) before annealing. Calculated PXRD of the predicted La3CoPb and La18Co28Pb3 ternary phases, and the known La6Co13Pb phases are also shown in the top, middle, and bottom rows respectively for comparison.

Figure S5. Powder diffraction patterns obtained from pieces of the arc melted La-Co-Pb pellet (left column: the 3:1:1 sample; right column: the 18:28:3 sample) after annealing 700°C for two week. Calculated PXRD of the predicted La3CoPb and La18Co28Pb3 ternary phases, and the known La6Co13Pb phases are also shown in the top, middle, and bottom rows respectively for comparison.

Figure S6. Calculated PXRD of the known La5CoPb3 phase is compared with the powder diffraction patterns obtained from pieces of the arc melted La-Co-Pb pellet (left column: the 3:1:1 sample; right column: the 18:28:3 sample).

Figure S7. Calculated PXRD of the known La12Co6Pb3 phase is compared with the powder diffraction patterns obtained from pieces of the arc melted La-Co-Pb pellet (left column: the 3:1:1 sample; right column: the 18:28:3 sample).

Figure S8. Calculated PXRD of binary La5Pb3 phase is compared with the powder diffraction patterns obtained from pieces of the arc melted La-Co-Pb pellet (left column: the 3:1:1 sample; right column: the 18:28:3 sample).

Figure S9. Calculated PXRD of binary La3Co phase is compared with the powder diffraction patterns obtained from pieces of the arc melted La-Co-Pb pellet (left column: the 3:1:1 sample; right column: the 18:28:3 sample).

Figure S10. Experimental PXRD data (black) from the 3:1:1 sample synthesized under pressure (see the text for more details). Calculated PXRD patterns of some known ternary and binary phases are also shown for comparison.

Table S1. Structure database of the La-Co-Pb system, including existing phases, CGCNN predicted stable phases and metastable phases. The formation energies (H) are referenced to the stable phases that form Gibbs triangles. The phases in bold are thermodynamically stable. The results are based on GGA calculation.

|  | Phases | Symmetry | a (Å) | b (Å) | c (Å) | H (meV/atom) |
| --- | --- | --- | --- | --- | --- | --- |
| Existing stable phases | La | P63/mmc | 3.75 | 3.75 | 12.12 | 0 |
|  | Co | P63/mmc | 2.49 | 2.49 | 4.02 | 0 |
|  | Pb | Fm-3m | 5.0 | 5.0 | 5.0 | 0 |
|  | La3Co | Pnma | 7.10 | 10.13 | 6.60 | 0 |
|  | LaCo13 | Fm-3c | 11.26 | 11.26 | 11.26 | 0 |
|  | LaPb3 | Pm-3m | 4.98 | 4.98 | 4.98 | 0 |
|  | La5Pb4 | Pnma | 8.66 | 16.47 | 8.77 | 0 |
|  | La4Pb3 | I-43d | 9.94 | 9.94 | 9.94 | 0 |
|  | La5Pb3 | P63/mcm | 9.64 | 9.64 | 7.04 | 0 |
|  | La3Pb | Pm-3m | 5.08 | 5.08 | 5.08 | 0 |
|  | La6Co13Pb | I4/mcm | 8.08 | 8.08 | 23.43 | 0 |
|  | La12Co6Pb | Im-3 | 10.20 | 10.20 | 10.20 | 0 |
| ML+DFT predicted stable phase | La3CoPb | Pm-3m | 5.33 | 5.33 | 5.33 | 0 |
| Existing metastable phases | La5CoPb3 | P63/mcm | 9.71 | 9.71 | 9.71 | 35 |
| ML+DFT predicted metastable phases | La18Co28Pb3 | I4/mmm | 14.05 | 14.05 | 9.92 | 7 |
|  | La13Co4Pb5 | C/2m | 7.30 | 7.31 | 25.87 | 11 |
|  | La24CoPb8 | Pm-3m | 10.23 | 10.23 | 10.23 | 14 |
|  | La12CoPb4 | Im-3m | 10.31 | 10.31 | 10.31 | 22 |
|  | La5CoPb | Cmcm | 13.77 | 11.79 | 11.19 | 22 |
|  | La5Co2Pb | C2/c | 16.05 | 7.83 | 7.83 | 31 |

| ML+DFT predicted metastable phases (continued) | La23Co7Pb4 | P63mc | 10.10 | 10.10 | 22.69 | 36 |
| --- | --- | --- | --- | --- | --- | --- |
|  | La12Co7Pb | I4/mcm | 12.10 | 12.10 | 13.74 | 38 |
|  | La11Co4Pb6 | P1 | 4.53 | 9.96 | 15.04 | 46 |
|  | La18Co2Pb9 | Pmma | 23.21 | 4.58 | 18.33 | 47 |
|  | La10Co2Pb11 | C2/m | 21.87 | 4.82 | 14.55 | 48 |
|  | La17Co6Pb3 | C2/m | 43.89 | 3.84 | 17.88 | 48 |
|  | La13Co3Pb7 | Pnma | 13.52 | 25.08 | 8.88 | 50 |
|  | La26Co10Pb7 | P4/mbm | 12.54 | 12.54 | 15.64 | 53 |
|  | La23Co14Pb4 | P1 | 11.78 | 13.96 | 14.55 | 54 |
|  | La26Co11Pb6 | P4/mbm | 12.38 | 12.38 | 15.71 | 54 |
|  | La14CoPb11 | C2/c | 22.22 | 24.98 | 16.76 | 55 |
|  | La6Co13Pb | I4/mcm | 8.01 | 8.01 | 23.41 | 57 |
|  | La11Co6Pb4 | R-3c | 10.13 | 10.13 | 36.68 | 62 |
|  | La16Co5Pb6 | Cm | 6.79 | 19.91 | 12.80 | 62 |
|  | La17Co3Pb4 | P21/c | 10.15 | 28.26 | 12.04 | 62 |
|  | La23Co6Pb4 | C2/m | 20.22 | 4.91 | 20.86 | 62 |
|  | La7Co3Pb | I41/amd | 10.26 | 10.26 | 22.76 | 62 |
|  | La11CoPb9 | Iba2 | 12.33 | 12.79 | 17.66 | 64 |
|  | La18Co5Pb4 | P1 | 4.83 | 10.55 | 17.00 | 69 |
|  | La14Co5Pb3 | Pm | 11.02 | 10.81 | 21.17 | 70 |
|  | La8CoPb2 | P4/mmm | 4.99 | 4.99 | 14.11 | 70 |
|  | La13Co12Pb3 | R-3 | 10.24 | 10.24 | 46.02 | 75 |
|  | La18Co11Pb3 | P1 | 4.09 | 12.06 | 18.29 | 77 |
|  | La7Co5Pb | P21/m | 8.70 | 4.17 | 18.46 | 77 |
|  | La7CoPb4 | Pba2 | 13.13 | 13.13 | 9.18 | 77 |
|  | La7Co6Pb | R3 | 10.23 | 10.23 | 23.45 | 78 |
|  | La9Co5Pb | P4/n | 10.80 | 10.80 | 6.64 | 78 |
|  | La17Co15Pb3 | P63/m | 10.20 | 10.20 | 19.51 | 79 |
|  | La19Co15Pb2 | R-3c | 10.57 | 10.57 | 58.28 | 79 |
|  | La20Co9Pb7 | P21 | 8.54 | 24.98 | 9.69 | 79 |
|  | La23Co21Pb5 | P63/m | 10.24 | 10.24 | 26.91 | 79 |
|  | La8Co5Pb | C2/m | 20.39 | 4.10 | 9.52 | 79 |
|  | La8CoPb24 | Pm-3m | 10.00 | 10.00 | 10.00 | 79 |
|  | La2CoPb2 | P4/mmm | 5.28 | 5.28 | 5.02 | 80 |
|  | La31Co27Pb5 | P63/m | 10.25 | 10.25 | 35.01 | 80 |
|  | La10Co9Pb2 | P-1 | 10.24 | 10.24 | 13.04 | 81 |
|  | La12Co3Pb5 | Amm2 | 4.57 | 22.62 | 13.05 | 85 |
|  | La3Co2Pb7 | Cmmm | 28.45 | 4.82 | 4.77 | 85 |
|  | La23Co4Pb7 | Cmc21 | 10.44 | 18.08 | 23.38 | 87 |
|  | La24Co9Pb4 | P1 | 8.92 | 9.16 | 14.74 | 87 |
|  | La15Co8Pb3 | C2/c | 14.28 | 11.14 | 18.58 | 88 |
|  | La17Co9Pb4 | Pbam | 25.31 | 16.98 | 4.03 | 88 |
|  | La21Co13Pb3 | Cm | 22.53 | 21.20 | 8.80 | 89 |
|  | La7Co2Pb | R-3m | 7.68 | 7.68 | 18.81 | 90 |
|  | La8Co3Pb5 | I4/mmm | 16.71 | 16.71 | 6.99 | 90 |
|  | La12Co4Pb | Im-3 | 10.35 | 10.35 | 10.35 | 91 |
|  | La13Co4Pb7 | P4/m | 11.95 | 11.95 | 5.02 | 95 |
|  | La21Co4Pb18 | C2/m | 17.79 | 17.29 | 17.65 | 96 |
|  | La9Co3Pb2 | Cmcm | 15.46 | 9.28 | 11.28 | 97 |
|  | La8Co3Pb4 | P1 | 10.76 | 10.76 | 10.76 | 98 |
|  | La11Co9Pb2 | R-3c | 10.48 | 10.48 | 36.18 | 99 |

Table S2. Crystallographic data of La3CoPb (space group of Pm-3m).

| phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La3CoPb | a =5.331 α=90° | 3c | La | 0.0 | 0.5 | 0.5 |
|  |  | 1b | Co | 0.5 | 0.5 | 0.5 |
|  |  | 1a | Pb | 0.0 | 0.0 | 0.0 |

Table S3. Crystallographic data of La18Co28Pb3 (space group of I4/mmm). E_hull = 7meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La28Co18Pb3 | a=14.049 b=14.049 c=9.918 α=β=γ=90° | 4c | La | 0 | 0.5 | 0 |
|  |  | 8i | La | 0.23636 | 0 | 0 |
|  |  | 16m | La | 0.33361 | 0.33361 | 0.23933 |
|  |  | 8j | La | 0.75076 | 0.5 | 0 |
|  |  | 32o | Co | 0.35595 | 0.8514 | 0.37739 |
|  |  | 16n | Co | 0 | 0.6238 | 0.25083 |
|  |  | 8h | Co | 0.75585 | 0.75585 | 0 |
|  |  | 2b | Pb | 0 | 0 | 0.5 |
|  |  | 4e | Pb | 0 | 0 | 0.83897 |
|  |  | 4c | La | 0 | 0.5 | 0 |

Table S4. Crystallographic data of La13Co4Pb5 (space group of C/2m). E_hull = 11 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La13Co4Pb5 | a=7.306 b=7.325 c=25.869 α= γ=90° β=97.96° | 4i | La | 0.88576 | 0 | 0.77901 |
|  |  | 8j | La | 0.08334 | 0.25028 | 0.66902 |
|  |  | 8j | La | 0.19593 | 0.24951 | 0.88997 |
|  |  | 4i | La | 0.77495 | 0 | 0.54961 |
|  |  | 2a | La | 0 | 0 | 0 |
|  |  | 4i | Co | 0.83192 | 0 | 0.66684 |
|  |  | 4i | Co | 0.05368 | 0 | 0.1106 |
|  |  | 4i | Pb | 0.71057 | 0 | 0.42136 |
|  |  | 4i | Pb | 0.60455 | 0 | 0.21691 |
|  |  | 2b | Pb | 0 | 0.5 | 0 |

Table S5. Crystallographic data of La24CoPb8 (space group of Pm-3m). E_hull = 14 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La24CoPb8 | a=10.232 b=10.232 c=10.232 α=β=γ=90° | 4i | La | 0.74756 | 0.5 | 0.5 |
|  |  | 8j | La | 0.74045 | 0 | 0 |
|  |  | 8j | La | 0.25493 | 0.5 | 0 |
|  |  | 4i | Co | 0 | 0 | 0 |
|  |  | 2a | Pb | 0.7483 | 0.7483 | 0.7483 |

Table S6. Crystallographic data of La12CoPb4 (space group of Im-3m). E_hull = 22 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La12CoPb4 | a=10.308 b=10.308 c=10.308 α=β=γ=90° | 12d | La | 0.25 | 0 | 0.5 |
|  |  | 12e | La | 0.25861 | 0 | 0 |
|  |  | 2a | La | 0 | 0 | 0 |
|  |  | 8c | Pb | 0.25 | 0.25 | 0.25 |

Table S7. Crystallographic data of La5CoPb (space group of Cmcm). E_hull = 22 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La5CoPb | a=13.768 b=11.786 c=11.189 α=β=γ=90° | 16h | La | 0.87012 | 0.33042 | 0.44825 |
|  |  | 4c | La | 0.00000 | 0.54813 | 0.25000 |
|  |  | 4c | La | 0.00000 | 0.11795 | 0.25000 |
|  |  | 8e | La | 0.13139 | 0.00000 | 0.00000 |
|  |  | 8g | La | 0.37049 | 0.31916 | 0.25000 |
|  |  | 8f | Co | 0.00000 | 0.18440 | 0.53823 |
|  |  | 8g | Pb | 0.74490 | 0.07658 | 0.25000 |

Table S8. Crystallographic data of La5Co2Pb (space group of C2/c). E_hull = 31 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La5Co2Pb | a=16.054 b=7.833 c=7.834 α=γ=90° β=119.05° | 8f | La | 0.88204 | 0.40526 | -0.02258 |
|  |  | 8f | La | 0.61849 | 0.40689 | 0.71088 |
|  |  | 4c | La | 0.25 | 0.25 | 0 |
|  |  | 8f | Co | 0.24992 | 0.3894 | 0.36059 |
|  |  | 4e | Pb | 0 | 0.75 | 0.25 |

Table S9. Crystallographic data of La23Co7Pb4 (space group of P63mc). E_hull = 36 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La23Co7Pb4 | a=10.105 b=10.105 c=22.691 α= β =90° γ =120° | 6c | La | 0.1274 | 0.8726 | 0.37299 |
|  |  | 6c | La | 0.20417 | 0.79583 | 0.21853 |
|  |  | 6c | La | 0.2055 | 0.7945 | 0.05119 |
|  |  | 6c | La | 0.21608 | 0.78392 | 0.50469 |
|  |  | 6c | La | 0.5405 | 0.4595 | 0.41271 |
|  |  | 6c | La | 0.53617 | 0.46383 | 0.14794 |
|  |  | 2b | La | 0.33333 | 0.66667 | 0.34761 |
|  |  | 2a | La | 0 | 0 | 0.50387 |
|  |  | 6c | La | 0.79588 | 0.20412 | 0.28042 |
|  |  | 6c | Co | 0.48386 | 0.51614 | 0.2843 |
|  |  | 6c | Co | 0.85533 | 0.14467 | 0.44144 |
|  |  | 2b | Co | 0.33333 | 0.66667 | 0.13071 |
|  |  | 6c | Pb | 0.88412 | 0.11588 | 0.13319 |
|  |  | 2a | Pb | 0 | 0 | 0.25913 |

Table S10. Crystallographic data of La12Co7Pb1 (space group of I4/mcm). E_hull = 38 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La12Co7Pb | a=12.104 b=12.104 c=13.745 α=β=γ=90° | 32m | La | 0.57452 | 0.71431 | 0.3531 |
|  |  | 8h | La | 0.82583 | 0.32583 | 0 |
|  |  | 8g | La | 0 | 0.5 | 0.36717 |
|  |  | 16l | Co | 0.31736 | 0.81736 | 0.31187 |
|  |  | 8h | Co | 0.37459 | 0.87459 | 0 |
|  |  | 4a | Co | 0 | 0 | 0.25 |
|  |  | 4c | Pb | 0 | 0 | 0 |

Table S11. Crystallographic data of La10Co2Pb11 (space group of C2/m). E_hull = 48 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La10Co2Pb11 | a=21.874 b=4.820 c=14.554 α= γ =90° | 4i | La | 0.18365 | 0 | 0.54056 |
|  |  | 4i | La | 0.59724 | 0 | 0.24272 |
|  |  | 4i | La | 0.75683 | 0 | 0.1625 |
|  |  | 4i | La | -0.03704 | 0 | 0.35765 |
|  |  | 4i | La | 0.37017 | 0 | 0.08016 |
|  | β =109.4° | 4i | Co | 0.76477 | 0 | -0.00734 |
|  |  | 4i | Pb | 0.78659 | 0 | 0.66729 |
|  |  | 4i | Pb | 0.01529 | 0 | 0.84939 |
|  |  | 4i | Pb | 0.64933 | 0 | 0.69359 |
|  |  | 4i | Pb | 0.56623 | 0 | 0.46876 |
|  |  | 4i | Pb | 0.87026 | 0 | -0.08978 |
|  |  | 2b | Pb | 0 | 0.5 | 0 |

Table S12. Crystallographic data of La17Co6Pb3 (space group of C2/m). E_hull = 48 meV

| Phase | Lattice param. | Wyckoff site | Atom | x | y | z |
| --- | --- | --- | --- | --- | --- | --- |
| La10Co2Pb11 | a=43.886 b=3.841 c=17.882 α= γ =90° | 4i | La | 0.18365 | 0 | 0.54056 |
|  |  | 4i | La | 0.59724 | 0 | 0.24272 |
|  |  | 4i | La | 0.75683 | 0 | 0.1625 |
|  |  | 4i | La | -0.03704 | 0 | 0.35765 |
|  |  | 4i | La | 0.37017 | 0 | 0.08016 |
|  | β =93.58° | 4i | Co | 0.76477 | 0 | -0.00734 |
|  |  | 4i | Pb | 0.78659 | 0 | 0.66729 |
|  |  | 4i | Pb | 0.01529 | 0 | 0.84939 |
|  |  | 4i | Pb | 0.64933 | 0 | 0.69359 |
|  |  | 4i | Pb | 0.56623 | 0 | 0.46876 |
|  |  | 4i | Pb | 0.87026 | 0 | -0.08978 |
|  |  | 2b | Pb | 0 | 0.5 | 0 |