Supplementary Information

for

Two-dimensional multiferroic material of metallic p-doped SnSe

Ruofan Du1,#, Yuzhu Wang1,#, Mo Cheng1, Peng Wang1, Hui Li1, Wang Feng1, Luying Song1, Jianping Shi1*, Jun He2*

1The Institute for Advanced Studies, Wuhan University, Wuhan 430072, China

2Key Laboratory of Artificial Micro- and Nano-structures of Ministry of Education, School of Physics and Technology, Wuhan University, Wuhan, 430072, China

*Address correspondences: jianpingshi@whu.edu.cn, He-jun@whu.edu.cn

#These authors contributed equally to this work.

Supplementary Figure 1 | OM images of PVD-synthesized 2D SnSe nanosheets on different substrates (e.g., Au foil, soda-lime glass, SiO2/Si, and sapphire).

Supplementary Figure 2 | XRD characterization of transferred 2D SnSe nanosheets on SiO2/Si, revealing its orthorhombic phase and high crystal quality.

Supplementary Figure 3 | Raman intensity (B2 3g) mapping image of a tetragonal SnSe nanosheet, showing its high thickness uniformity.

Supplementary Figure 4 | AFM images and corresponding height profiles analysis of as-grown 2D SnSe nanosheets with different thicknesses.

Supplementary Figure 5 | FFT pattern of a transferred tetragonal SnSe nanosheet, showing its single crystalline feature.

Supplementary Figure 6 | Corresponding STEM intensity line profiles capture from Fig. 2g.

Supplementary Figure 7 | Thickness-depedent conductivity of PVD-synthesized 2D p-doped metallic SnSe with the electrode direction along zigzag orientation.

Supplementary Figure 8 | Valence band photoemission spectrum of PVD-synthesized 2D SnSe on mica, indicating its metallic feature.

Supplementary Figure 9 | XPS spectrum of transferred 2D p-doped SnSe2 nanosheets on SiO2/Si.

Supplementary Figure 10 | Raman characterizations of transfer flipped SnSe nanosheets, revealing the presence of SnSe2 microdomains.

Supplementary Figure 11 | Temperature-dependent magnetoresistance of PVD-synthesized 2D metallic p-doped SnSe nanosheet (thickness of ~46 nm) with a parallel magnetic field, a sharp dip around zero magnetic field suggestes the appearance of weak antilocalization (WAL) effect.

Supplementary Figure 12 | ZFC derivative curves of PVD-synthesized 2D metallic p-doped SnSe, showing the Curie temperature of ~337 K. The magnetic field (100 Oe) is vertical and parallel to c-axis, respectively.

Supplementary Figure 13 | OM image of transferred 2D metallic p-doped SnSe nanosheets with top Au electrodes.

Supplementary Figure 14 | AFM images and corresponding height profiles analysis of transferred tetragonal SnSe nanosheets with top Au electrodes.

Supplementary Figure 15 | The single-well potential of SnSe/SnSe2 interface. A and B represent the nonpolar and polar phase, respectively.

Supplementary Figure 16 | Schematic diagram of the distorted degenerate polar structure (B) and high symmetry nonpolar phase (A).