Investigation of Synthesis of Biogenic Hematite Nanocubes for environmental Assessment and its innovative Applications associated with Antibacterial, Antifungal, and Antioxidant activity

1Debasmita Das, 1Salim Ali, 1Biplab Rajbanshi, 1Samapika Ray, 1Sanjoy Barman, 2Divya Chouhan, 2Md Salman Haydar, 2Palash Mandal, 3Kanak Roy, 1, 3* Mahendra Nath Roy

# 1Department of Chemistry, University of North Bengal, Darjeeling, India.

# 2Nanobiology and Phytotherapy Laboratory, Department of Botany, University of North Bengal, Siliguri, West Bengal, India.

3Department of Chemistry, Alipurduar University, Alipurduar-736122, India

*Corresponding Authors: Mahendra Nath Roy, mahendraroy2002@yahoo.co.in

# SUPPLEMENTARY MATERIALS

TABLE

| tABLE S1 | PAGE 2 |
| --- | --- |
| tABLE S2 | PAGE 2 |

FIGURE

| fIGURE S1 | PAGE 3 |
| --- | --- |
| FIGURE S2 | PAGE 4 |
| FIGURE S3 | PAGE 5 |
| FIGURE S4 | PAGE 6 |
| Figure S5 | PAGE 7 |
| fIGURE s6 | PAGE 8 |
| fIGURE s7 | PAGE 8 |
| fIGURE s8 | PAGE 9 |
| fIGURE S9 | PAGE 10 |
| FIGURE s10 | PAGE 10 |
| Figure s11 | PAGE 11 |
| Figure s12 | PAGE 11 |

Table S1 Phytochemical screening of Lemon Peel Extract

| Sl. No. | Phytochemicals | Lemon peel |
| --- | --- | --- |
| 1 | Carbohydrates | + |
| 2 | Protein | + |
| 3 | Phenols and tanins | + |
| 4 | Saponins | + |
| 5 | Flavonoids | - |
| 6 | Steroids | + |
| 7 | Glycosides | + |
| 8 | Terpenoids | - |
| 9 | Alkaloids | - |

Table S2 XRD diffraction data of IONPs (2θ, FWHM, Crystalline size (d. nm), Micro-strain, Dislocation Density)

| 2θ |  | θ |  | FWHM |  | Crystalline size (dnm) |  | Average size |  | Micro-strain(ε×10-3) | Dislocation Density (δ×10-3 (nm-2) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 24.49671 |  | 12.24836 |  | 0.15463 |  | 52.38233578 |  | 41.8203 |  | 3.392458284 |  | 3.6444356 |
| 33.22285 |  | 16.61143 |  | 0.32023 |  | 25.88851428 |  |  |  | 4.683627409 |  | 4.683627409 |
| 35.71506 |  | 17.85753 |  | 0.23782 |  | 35.09545979 |  |  |  | 3.220897066 |  | 3.220897066 |
| 40.93499 |  | 20.4675 |  | 0.20163 |  | 42.0552501 |  |  |  | 2.357145817 |  | 2.357145817 |
| 49.55147 |  | 24.77574 |  | 0.28193 |  | 31.03483222 |  |  |  | 2.665255988 |  | 2.665255988 |
| 54.14106 |  | 27.07053 |  | 0.28322 |  | 31.50090594 |  |  |  | 2.41799261 |  | 2.41799261 |

Fig. S1 Mechanism of interaction of phytochemicals of LPE and metal salt

Fig. S2 First order reaction kinetics for the decolorization of MB dye by the Fenton like reactions with (a) variation of H2O2 concentration at constant pH and amount of catalyst (b) Variation of pH with the constant amount of H2O2 and catalyst (c) variation of catalyst amount at constant pH and constant amount of H2O2.

Fig. S3 Plots for rate constant of first order reaction with (a) variation of catalyst amount at constant pH and constant amount of H2O2 (b) Variation of pH with constant amount of H2O2 and catalyst (c) variation of H2O2 concentration at constant pH and amount of catalyst

(d)

(b)

Fig. S4 Seed germination and seedling vigor evaluation of wheat seedlings through (a) germination index, (b) mean germination time, (c) co-efficient velocity of germination and (d) promptness index

(e)

(d)

(c)

(b)

(a)

Fig. S5 Evaluation of biochemical attributes of treated wheat seedlings through (a) Total Phenol content, (b) Total ortho-dihydric phenol, (c) Total Chlorophyll content, (d) Total reducing sugar and (e) Total flavonoid content estimation.

Fig. S6 Bar graph showing Zone of inhibition of introduced by IONPs against B Subtilis, B megaterium, S typhimurium, S aureus, E coli

Fig. S7 Visual representations of the proposed mechanisms of antibacterial activity of IONPs

Fig. S8 Concentration-response curve on DPPH radical scavenging capacity of  IONPs synthesized from LPE. Ascorbic acid was used as antioxidant reference.

Fig. S9 Effect of IONPs on mycelium radial growth of F. solani. (a) Mycelium radial growth of F. solani with different concentrations (0, 100, 250, 500, 1000, 2000, 3000 µg/mL) of IONPs on PDA plate; (b) Graph showing Percent Inhibition of Radial Growth (PIRG) of F. solani under tested concentrations of IONPs. Values are averages of three replicates (n=3), error bars indicate standard deviation (SD).

Fig. S10 Effect of IONPs on inhibition percentage of spore germination of F. solani.

0

10

20

30

0.1

1

10

100

1000

10000

Intensity (%)

Size (d.nm)

Fig. S11 DLS of recovered catalyst after third cycles

0

50000

100000

150000

200000

250000

-100

0

100

200

Total     Counts

Apparent Zeta Potential (mV)

Fig. S12 Zeta potential of recovered catalyst after third cycle