Supplementary Information for;

A Greener Mechanochemical Approach to the Synthesis of Urea-Hydroxyapatite Nanohybrids for Slow Release of Plant Nutrients

Madhavi de Silva1, Chanaka Sandaruwan2, Francisco C. Robles Hernandez3,4, Onur Sahin4, Meiyazhagan Ashokkumar4, Pulickel M. Ajayan4, Veranja Karunaratne5, Gehan A. J. Amaratunga6, Nilwala Kottegoda1*

1Department of Chemistry/Center for Advanced Materials Research, University of Sri Jayewardenepura, Sri Soartha Mawatha, Nugegoda 10250, Sri Lanka

2Nanotechnology and Science Park, Center for Excellence in Nanotechnology, Sri Lanka Institute of Nanotechnology (SLINTEC), Mahenawatta, Pitipana, Homagama 10206, Sri Lanka

3College of Engineering Technology, University of Houston, Houston, TX, U.S.A. 77204-4020

4Department of Materials Science & NanoEngineering, Rice, University, Houston, Texas, U.S.A.  77005

5Department of Chemistry, University of Peradeniya, Peradeniya 20400, Sri Lanka

6Department of Engineering, University of Cambridge, Trumpington Street, Cambridge CB2 1PZ, United Kingdom

*Corresponding author: Nilwala Kottegoda (nilwala@sjp.ac.lk)

- X-Ray Photoelectronic Spectral Analysis

Table S1: Quantitative results from the XPS analysis of HA

| Electronic core-level | Binding Energy (eV) | Atomic Weight Percentage (%) | FWHM (eV) |
| --- | --- | --- | --- |
| Ca 2p | 347.73 | 67.86 | 1.78 |
| P 2p | 133.85 | 100 | 1.99 |
| O 1s | 531.53 | 45.39 | 1.51 |

Table S2: Quantitative results from the XPS analysis of Urea

| Electronic core-level | Binding Energy | Atomic Weight Percentage | FWHM |
| --- | --- | --- | --- |
| N 1s | 400.04 | 56.87 | 1.36 |
| O 1s | 531.95 | 10.35 | 1.42 |

Table S3: Quantitative results from the XPS analysis of Urea-HA nanohybrids

| Electronic core-level | Binding Energy | Atomic Weight Percentage | FWHM |
| --- | --- | --- | --- |
| N 1s | 399.45 | 100 | 2.33 |
| Ca 2p | 347.11 | 68.05 | 1.62 |
| P 2p | 132.8 | 32.94 | 1.42 |
| O 1s | 530.99 | 40.29 | 1.53 |

- Fourier Transmission Infrared (FTIR) Spectral Analysis

Table S4: Peak shifts in the C=O stretching and -NH2 bending regions of the Urea-HA   nanohybrids

|  | C=O stretching/ cm-1 | Peak Shift /cm-1 | -NH2 bending/cm-1 | Peak Shift/ cm-1 |
| --- | --- | --- | --- | --- |
| Urea | 1663 | - | 1612 | - |
| 10: 1 U-HA | 1682 | 19 | 1626 | 14 |

Table S5: Peak shift in the N-C-N stretching region of the Urea-HA   nanohybrids

|  | N-C-N stretching / cm-1 | Peak Shift / cm-1 |
| --- | --- | --- |
| Urea | 1454 | - |
| 10: 1 U-HA | 1464 | 10 |

Table S6: Peak shifts in the -NH2 stretching regions of the Urea-HA nanohybrids

|  | -NH2 stretching / cm-1 | Peak shift / cm-1 | - NH2 stretching / cm-1 | Peak Shift / cm-1 |
| --- | --- | --- | --- | --- |
| Urea | 3440 | - | 3336 | - |
| 10: 1 U-HA | 3438 | 2 | 3343 | 6 |

Table S7: Peak shift in the PO43- stretching regions of the Urea-HA nanohybrids

|  | PO43- stretching/ cm-1 | Peak Shift / cm-1 |
| --- | --- | --- |
| Urea | 1039 | - |
| 10: 1 U-HA | 1041 | 2 |

- Release Kinetic Modeling of Urea-HA nanohybrids in Water

The data received from the nitrogen release behavioral studies in water were fitted into the below-mentioned kinetic models to determine R2 values and release exponent (n) values.

i)  Zeroth-order rate model,

Q0 − Qt = k0t

Q0 = Initial amount of the active compound

Qt =  Amount of active compound dissolved at time t

K0 = Zero-order rate constant

t = Time

ii) First-order rate model,

Log Ct = Log C0 + kt/2.303

C0 = Initial concentration of the active compound

Ct =  Concentration of the active compound released after time t

K =  First-order rate constant

t = Time

3. Higuchi model,

Log Q =1/2 log t + log kH

Q = Amount of active compound released

kH = Higuchi dissociation constant

t = time

4. Korsmeyer-Peppas model

Mt/M∞ = ktn

Mt/M∞ - Fraction of active compound released at time t

n = diffusion exponent

k = kinetic constant

Assumptions: Infinite time

5. Hixson-Crowell model

Q01/3 – Qt 1/3 = KHCt

Qt = Remaining weight of nitrogen at time t

Q0 = Initial weight of solid at time t = 0

t = Time

KHC = Dissolution rate constant

6. The Avrami-Erofe’ev model,

ln[-ln(Ct/C0 )] = n ln (kd) + n ln (t-t0)

C0 = Amount of nitrogen in Urea-HA Nanohybrids at t=0,

Ct = Amount of nitrogen remaining in the Urea-HA nanohybrids at time t

kd = Rate of release

n = Constant

Table S8: The R2 values obtained from the applying various kinetic models

| Kinetic Model | R2 Values |
| --- | --- |
| Zeroth Order | 0.667 |
| First Order | 0.806 |
| Higuchi | 0.748 |
| Korsmeyer-Peppas | 0.88 |
| Hixson-Crowell | 0.96 |
| Avrami-Erofe’ev | 0.993 |

- Plant Plot Trials

Figure S1: Plant plot trials experiments

- Calculation of Nitrogen Agronomic Use Efficiency (NAE)

Nitrogen Agronomic Use Efficiency was calculated using the below-mentioned equation;

[Yield from Nitrogen Treatment (kg ha-1) / Yield from no nitrogen treatment(kg ha-1)]

NAE (kg N kg-1)

=

Total Nitrogen Applied (kg ha-1)

Table S9: Nitrogen Agronomic Use Efficiencies (NAE)s calculated for urea and Urea-HA nanohybrids

|  | Nitrogen Agronomic Use Efficiencies (NAE) (kg N kg-1) |
| --- | --- |
| Urea | ~ 8% |
| Urea-HA nanohybrid | ~16 % |

- Proposed Scale-Up Process and Financial Calculations

(i) Industrial Manufacturing Process Layout

Figure S3: Proposed process layout diagram. Alternatively, the stored ammonia can be bubbled through phosphoric acid to regenerate the phosphorus source used: Diammonium Hydrogen Phosphate

Ammonia is the only by-product coming out from the reaction between Calcium Hydroxide and Diammonium Hydrogen Phosphate and will be collected and stored as Ammonia gas. This ammonia gas could be used to regenerate the starting material Diammonium Hydrogen Phosphate by bubbling phosphoric acid.

iii) Cost Estimation and Financial Analysis

The following calculations present the variable costs that will incur in producing urea-HA nanohybrids and therefore cost of production for 1 kg of the nanofertilizer.

NB: These calculations are made based on the utility, infrastructure, economic conditions of Sri Lanka as of  March 2021 (Exchange Rate - 1 USD = LKR 200)

Total Production Capacity per Day: 140 mt per day

Table S10: Operational costs (Per day)

| Direct labor (LKR) | 20000 |
| --- | --- |
| Utilities (LKR) | 100000 |

Table S11: Raw materials costs (Required for 140 MT/day)

|  | Required amount (kg) | Cost per 1 kg (LKR) | Total cost (LKR) |
| --- | --- | --- | --- |
| Di Ammonium Hydrogen Phosphate | 127260 | 60 | 7635600 |
| Calcium Hydroxide | 9427.6 | 35 | 329966 |
| Urea | 8943.48 | 30 | 268304.4 |
|  |  |  | 8233870.4 |

Packaging & transportation  - LKR 2000000

Total variable costs to produce 140 MT Production cost)  = LKR 10533870.4

Total variable costs to produce 1 kg = LKR 75

The cost to produce one kilogram of the nanofertilizer = USD 0.38