Supporting Information

Rational design of direct Z–scheme magnetic ZnIn2S4/ZnFe2O4 heterojunction toward enhanced photocatalytic wastewater remediation

Qiang Gao a,b,*, Zhi Wang a, Junxi Li b, Bin Liu b,*, Chenguang Liu b

a School of Chemistry and Chemical Engineering, Qinghai Normal University, Xining 810008,

P. R. China

b State Key Laboratory of Heavy Oil Processing, China University of Petroleum (East China), Qingdao 266580, P. R. China

*Corresponding authors: Professor B. Liu; E-mail addresses: liubin@upc.edu.cn

Chemicals and Materials

All the used chemicals in this work were analytical grade without further purification. Zinc sulfate heptahydrate (ZnSO4·7H2O), ferrous ammonia sulfate hexahydrate ((NH4)Fe(SO4)·6H2O), zinc chloride (ZnCl2), ethylene glycol (C2H6O2), oxalic acid dihydrate (C2H2O4·2H2O), and hydrochloric acid (HCl, 35%) were purchased from Sinopharm Chemical Reagent Co., Ltd. Indium chloride hydrate (InCl3·4H2O, 97%), thioacetamide (C2H5NS, 99%), methanol (MeOH), and ethyl alcohol (EtOH) were acquired from Aladdin. Deionized distilled water was used throughout in the experiment.

Characterization

X−ray diffraction (XRD) patterns were taken with a D8 Advance X−ray diffractometer system using a Cu−Kα source. N2 adsorption−desorption analysis was performed at 77 K with Micromeritics ASAP 2420 in a relative pressure (P/P0) range from 10−6 to 1. The field emission scanning electron microscopy (FESEM) analysis was collected with an S−4800 accelerating voltage of 15 kV. Transmission electron microscopy (TEM) was carried out with JEOL−2100F system at an acceleration voltage of 200 kV. The high angle annular dark field scanning transmission electron microscopy image (HAADF−STEM) mapping was acquired on FEI TITAN G2 (200 kV). X−ray photoelectron spectroscopy (XPS) was analyzed by an AMICUS ESCA 3400 using Al Kα radiation. UV−visible diffuse reflectance spectroscopy (DRS) was examined on Hitachi U−4100 using with BaSO4 as reference material. The photocurrent tests and electrochemical impedance spectroscopy (EIS) were carried out via a CHI760 electrochemical workstation with a standard three-electrode probe. Magnetism of samples was measured at room temperature using vibrating sample magnetometers (VSM, Quantum Design PPMS-9) in the field range of -30000 ~ +30000 Oe.