Supplementary information

Sustainable and color-indicated tannic acid@high amylose starch/polyvinyl alcohol (TA@HAS/PVA) fibers for adsorbing uranium from aqueous solutions

Qun Liua, Xiaoyang Wangb, Meiyan Baib, Jiayi Guob, Zhengjie Qianb, Jihui Lib, Zhifen Wangc, Yucang Zhanga,

aCollege of Ocean Food and Biological Engineering, Jimei University, Xiamen 361021, Fujian, China

bSchool of Chemical Engineering and Technology, Hainan University, Haikou 570228, China

cSchool of Materials Science and Engineering, Hainan University, Haikou 570228, China

| Pseudo-first-order model |  |  | Pseudo-second-order model |  |  |
| --- | --- | --- | --- | --- | --- |
| kI (min−1) | qe (mg g−1) | R2 | kII (g mg−1 min−1) | qe (mg g−1) | R2 |
| 0.0078 | 74.0518 | 0.8243 | 1.5587×10−4 | 81.0422 | 0.9299 |

Table S1. Fitted parameters and correlation coefficients (R2) from the two models for U(VI) adsorption (200 mg L−1) onto the TA@HAS/PVA fibers.

| Langmuir model |  |  | Freundlich model |  |  |
| --- | --- | --- | --- | --- | --- |
| qm (mg g−1) | KL(L mg−1) | R2 | KF (mg g−1) | n | R2 |
| 504.2677 | 0.0105 | 0.9492 | 60.2126 | -0.3032 | 0.8133 |

Table S2. Langmuir and Freundlich isotherm parameters and correlation coefficients (R2) for U(VI) adsorption onto the TA@HAS/PVA fibers.

Figure S1. Morphology of TA@HAS/PVA fibers.

Figure S2. Stretch ability of TA@HAS/PVA fiber.

Corresponding author.

E-mail address: yczhang@jmu.edu.cn (Y. Zhang)