Cost-Effective Fabrication, Antibacterial Application and Cell Viability Studies of Modified Nonwoven Cotton Fabric

Rahat Nawaz,a Sayed Tayyab Raza Naqvi,a Batool Fatima,b Nazia Zulfiqar, a  Muhammad Umar Farooq, a Asghar Javeed, c Waheed Qamar Khan,d Azhar Rasul,e Laila Jafri,f Dilshad Hussain,g Saadat Majeed ⃰ a

aDivision of Analytical Chemistry, Institute of Chemical Sciences, Bahauddin Zakariya University, Multan 60800, Pakistan

bDepartment of Biochemistry, Bahauddin Zakariya University, Multan 60800, Pakistan

c Department of Pathology, Nishtar Medical University, Multan 60800, Pakistan

d Institute of Advanced Materials, Bahauddin Zakariya University, Multan 60800, Pakistan

e Department of Zoology, Govt. College University Faisalabad, Faisalabad

f Department of Life sciences, Abasyn University, Peshawar, Pakistan

g International Centre for Chemical and Biological Sciences, HEJ Research Institute of Chemistry, University of Karachi, Karachi 75270, Pakistan

*E-mail:saadat.majeed@bzu.edu.pk

Figure S1. Photostability and shelf-life stability of N-halamines-chitosan@AgNPs-nonwoven fabric under dark and UVA light conditions for upto 12 weeks.

Table S1. Percentage loading of chlorine on Non-Woven Cotton Fabric samples

| Samples | Non-Woven Cotton Fabric | Weight | Chitosan (2% sol.) | Chlorination Time (mint.) | Volume (mL) | Loaded chlorine (%) |
| --- | --- | --- | --- | --- | --- | --- |
| AgNPs-NWCF (0.85 cm ×1.0cm) | Unchlorinated (control-I) | 0.06g | - | - | 0.01 | 0 |
| Chitosan@ AgNPs-NWCF(0.85 cm ×1.0cm) | Unchlorinated (control-II) | 0.06g | Double coating | - | 0.01 | 0 |
| N-halamine/ chitosan@ AgNPs-NWCF (0.85 cm ×1.0cm) | Chlorinated | 0.06g | Double coating | 30 | 0.01 | 0.295 |

Antibacterial Testing

Bacterial reduction (%) =  (B- A)/ B × 100 %

Where, A is the number of surviving bacterial colonies of the test sample and B is that of the control.

Table S2. Growth inhibition zone of AgNPs-nonwoven fabric, chitosan@AgNPs-nonwoven fabric, and N-halamines-chitosan@AgNPs-nonwoven fabric for Micrococcus lutes, Staphylococcus aureus, Enterobacter aerogenes and E.coli bacteria.

| Sr. | Sample | Zone of inhibition with 6mm solid disk sample |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Micrococcus lutes | Staphylococcus aureus | Enterobacter aerogenes | Escherichia coli |
| 1 | AgNPs-NWCF | 6.7 | 6.6 | 5.6 | 5.4 |
| 2 | Chitosan/@AgNPs-NWCF | 7.8 | 7.7 | 7.5 | 7.3 |
| 3 | N-halamines - chitosan@AgNPs-NWCF | 11.8 | 11.9 | 11.2 | 11.6 |