Supporting Information for

Role of weak magnetic field for enhanced oxidation of orange G by magnetic Fenton

Zhenyu Shi1,2, Ruijia Zhang3, Jing Zhang1*

- College of Environment & Ecology, Chongqing University, Chongqing 400045, P. R. China

- Environment Monitoring Center of Jiangsu Province, Nanjing 210036, PR China

- Xuzhou Municipal Engineering Design Institute Co., Ltd., Xuzhou 221000, P. R. China

*Corresponding author address:

Jing Zhang

College of Environment & Ecology, Chongqing University, Chongqing 400045, P. R. China

E-mail: zhangjing2018@cqu.edu.cn

# Fig. S1 Diagram of the experimental setup.

# Fig. S2 Removal of OG by H2O2 or Fe3O4 alone without WMF (a) and with WMF (b), Reaction conditions: [OG]=0.1 mM, pH=3.0, T=25 oC.

Fig. S3 The first-order kinetic fitting of OG degradation by Fe3O4/H2O2 as a function of MF intensity. Reaction conditions: [OG]=0.1 mM, [H2O2]=20 mM, [Fe3O4]=1 mM as Fe, pH=3.0, T=25 oC.

# Fig. S4 XRD patterns for virgin Fe3O4, spent Fe3O4 used in heterogeneous Fenton with and without WMF.

Fig. S5 Degradation of OG in homogeneous Fe(II)/H2O2 process with and without WMF. The dosage of Fe(II) was set according the maximum dissolved Fe ions at the end of reactions. Reaction conditions: [OG]=0.1 mM, [H2O2] =20 mM, pH=3.0, T=25 oC.

# Table S1 XPS analysis for Fe3O4

| Samples | XPS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | FeII peak position |  | FeIII peak position |  | Satellite peak position |  | surface FeII/FeIII molar ratio |
|  | 2p1/2 | 2p3/2 | 2p1/2 | 2p3/2 | 2p1/2 | 2p3/2 |  |
| Virgin Fe3O4 | 723.9 | 710.7 | 725.4 | 712.4 | 718.8 | 715.5 | 1.00 |
| Spent Fe3O4 without WMF | 723.9 | 710.7 | 725.4 | 712.4 | 718.8 | 715.5 | 0.76 |
| Spent Fe3O4 with WMF | 723.9 | 710.7 | 725.4 | 712.4 | 718.8 | 715.5 | 0.22 |