Table SM- 1 Properties of Amaranth Red (E123)

| Empirical formula | C20H11N2Na3O10S3 |
| --- | --- |
| IUPAC name | Trisodium (4E)-3-oxo-4-[(4-sulfonato-1-naphthyl) hydrazono]naphthalene-2,7-disulfonate |
| Color and aspect | The coloration is attributed to azo groups accountable to the red-brown dye (E123) with bond absorption in the visible region (λ = 520 nm) |
| Molecular weight (g.mol-1) | 606.48 |
| Classification | Anionic Sulphonated Azo Dye |
| Use and toxicity | Colorant used in the food sector then its application was banned because of its carcinogenic effect. |
| water solubility | 60 g. L-1 (at 25°C) |

Table SM-2 Quantification of the dissolution of Pb2 + (±0,002 mg.L-1) from SS/PbO2 obtained during the removal of 10 mg.L-1 of Amaranth Red (E123) by AO and AO coupling biosorption

| SS/PbO2/Time (min) | AO | Coupling AO with biosorption |
| --- | --- | --- |
| 5 | 0 | 0 |
| 10 | 0 | 0 |
| 15 | 0 | 0 |
| 20 | 0 | 0 |
| 25 | 0 | 0 |
| 30 | 0.0001 | 0 |
| 35 | 0.0009 | 0 |
| 40 | 0.012 | 0.010 |
| 45 | 0.018 | 0.015 |
| 60 | 0.021 | 0.020 |
| 65 | 0.029 | - |
| 70 | 0.034 | - |
| 75 | 0.047 | - |
| 80 | 0.051 | - |

(Note: - means the end of the time required for the total removal of Amaranth)

Table SM-3 Evaluation of the efficiency of the coupling process: A comparative study with works dealing with the doping methods

| Electrodes | Contaminants |  | Conditions |  | Achievement |  | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al doped PbO2 | chloramphenicol (CAP) |  | C0 =100 mg.L-1 Acid conditions J = 30 mA cm-2 Cathode: Al Electrolyte:0.2M Na2SO4 |  | The removal rates of CAP and TOC reached respectively 87.30% and 52.06% after 604 min of electrolysis |  | (Chen et al. 2015) |
| Co doped Ti/Ti nanotube/PbO2 |  | MB |  | C0 =30 mg.L-1 pH=3 t=120min J = 50 mA cm-2 Cathode: Ti Electrolyte:0.2M Na2SO4 |  | 100% and 74.0% of MB and COD were removed respectively after 120 min | (Wang et al. 2015) |
| TiO2-NTs/Co-PbO2 (P) and TiO2-NTs/Co-PbO2 (G) |  | MB |  | Cathode: SS C0 [10-50] mg.L-1 S=5cm2 d=20 mm Electrolyte: 0.2M Na2SO4 |  | Best results were achieved on the NTs / Co-PbO2 after 120 min J = 50 mA.cm-2, pH=3 | (Moura et al. 2016) |
| SS/SiOx/PbO2 |  | Amaranth |  | pH=2 Cathode: SS C0 = 10 mg.L-1 J=30 mA.cm-2 Electrolyte: 0.2M Na2SO4 |  | 100% of Color and 84% of COD were removed after 300min | (Elaissaoui et al. 2019) |
| SS/PbO2 |  | MB |  | Cathode :SS C0=10 mg.L-1, pH=7 S=4 cm2 Electrolyte: 0.1 M NaCl,0.1M Na2SO4, and 0.1 M NaNO3 |  | The % color removal MB reached 89.5% and under AC and 80.2% under DC after 150 min in NaCl | (Othmani et al. 2019) |
| SS/PbO2 (P) |  | MB |  | Cathode :SS C0=[10-140] mg.L-1 pH=7, S=4 cm2 Electrolyte:0.1 M NaCl, 0.1 M NaNO3 |  | The % of color removal of MB reached 98.7 % and 80.02% after 60 and 120 min under AC and DC in NaNO3 | (Othmani et al. 2020) |
| SS/PbO2 (P) |  | Amaranth |  | Cathode :SS C0=[10-100]mg.L-1, pH=2, S=12.56 cm2 Electrolyte:0.2 M Na2SO4 t=120 min |  | 97.8, and 99.9% of 50 mg.L-1 of Amaranth were removed respectively after, 65, and 50 min by AO and AO coupling biosorption | This study |

Table 1 Elementary analysis of L.C

|  | C | O | Na | Mg | Al | Si | P | S | Cl | Ca | Mo |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| L.C | 54.46 | 40.60 | 0.45 | 0.38 | 0.8 | 1.1 | 0.29 | 0.0 | 0.35 | 1.4 | 0.17 |