Supplementary Material:

Synergistic effect of titanium dioxide (TiO2) and ionizing radiation on thermal and mechanical properties of carboxymethyl cellulose (CMC) for potential application in removal of basic dye from wastewater

Yasser H. Gad1, Hussein E.Ali2and El-Sayed A. Hegazy1

1Polymer Chemistry Department, National Center for Radiation Research and Technology, Atomic Energy Authority P.O. Box 29, Nasr City, Cairo, Egypt

2Radiation Chemistry department, National Center for Radiation Research and Technology, Egyptian Atomic Energy Authority P.O. Box 29, Nasr City, Cairo, Egypt.

Contents

1. Figure (1):- FTIR spectra of CMC-20% Glycerol, CMC/1.5% TiO2 and CMC/1.5% TiO2 - 10kGy.

2. Scheme (1):- The suggested scheme for preparation of CMC/TiO2 composite film by 60Co g-irradiation.

3. Figure (2):- Effect of Irradiation dose (kGy) and TiO2 (%) content on the Tensile strength (MPa) of carboxymethyl cellulose (CMC) films.

4. Figure (3):- Effect of Irradiation dose (kGy) and TiO2 (%) content on the Elongation at break (%) of carboxymethyl cellulose (CMC) films.

5. Figure (4):- The X-ray diffraction patterns of CMC-20% Glycerol, CMC/1.5% TiO2and

CMC/1.5%TiO2-10kGy.

6. Figure (5):- SEM of CMC films:(a) CMC-20% Glycerol, (b) CMC/1.5%TiO2 and (c) CMC/1.5%TiO2 - 10kGy.

7. Figure (6):- (A)TGA and (B) DTG thermograms of CMC-20%Glycerol, CMC/1.5%TiO2 and

CMC-1.5% TiO2 at 10kGy.

8. Table (1):- The weight loss (%) of different prepared samples

9. Figure (7A):- shows the change in the absorbance of the basic violet 7 dye solutions  onto

blank CMC, irradiated and unirradiated CMC/TiO2 composite after 24h.

10. Figure (7b):- Effect of adsorbent type[ (A) pure CMC, (B) Unirradiated CMC/TiO2 and (C) CMC/1.5% TiO2-10 kGy]  on the removal of the basic violet dye after 24h.

11. Figure (8):- Effect of pH and initial concentration (mg/l) on the removal (%) and amount

adsorbed (mg/g) of basic Violet 7 dye onto CMC/1.5 TiO2- 10 kGy at conditions;

adsorbent dosage = 0.2 g and contact time = 420 min at room temperature = 298 oK.

12. Figure (9):- Effect of  contact time (min.) and temperature (oK) on the amount adsorbed

(qt)(mg/g) of Basic Violet 7 dye onto CMC/1.5 % TiO2- 10 kGy composite film

at the conditions; initial concentration = 100 mg/l, adsorbent dose = 0.02 g,

solution volume 50 ml and pH = 8.

13. Figure (10):- amount adsorbed of basic violet 7 dye fitted with the Langmuir model and  Freundlich models.

14. Table (2):- Parameters fitted from the Langmuir and Freundlich isotherm models, the pseudo-first order and pseudo-second order for the adsorption of basic violet 7 dye onto irradiated CMC/1.5% TiO2 composite film.

15. Figure (11):- Fitted plots of the pseudo-first-order and pseudo-second-order kinetics of adsorption

for basic violet dye onto CMC/1.5% TiO2- 10 kGy.

16. Table (3):- of Adsorption Capacities of dyes by CMC polymeric nanocomposite film as Adsorbents.

| Figure (5):- SEM of CMC films:(a) CMC-20% Glycerol, (b) CMC/1.5%TiO2 and (c) CMC/1.5%TiO2 - 10kGy. |  |
| --- | --- |

Table (1):- The weight loss (%) of different prepared samples

| Sample | Dose (kGy) | Weight Loss (%) |  |  |  |  | Tmax |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 100 oC | 200 oC | 300 oC | 400oC | 500oC |  |
| PLSTCMC | 0 | 12 | 17 | 56.6 | 67.6 | 70.4 | 284.4 |
| PLSTCMC/TiO2 | 0 | 9.4 | 14.3 | 54.2 | 67.8 | 70.2 | 287.5 |
| PLSTCMC/TiO2(10 kGy) | 10 | 9.1 | 13.9 | 53.7 | 64.5 | 67.4 | 289.9 |

Figure (7b):- Effect of adsorbent type[ (A) pure CMC, (B) Unirradiated CMC/TiO2 and (C) CMC/1.5% TiO2-10 kGy]  on the removal of the basic violet dye after 24h.

Table (2):- Parameters fitted from the Langmuir and Freundlich isotherm models, the pseudo-first order and pseudo-second order for the adsorption of basic violet 7 dye onto irradiated CMC/1.5% TiO2 hydrogel composite

| Model | Parameters | Temperature (oK) |  |  |
| --- | --- | --- | --- | --- |
|  |  | 298 (oK) | 308 (oK) | 318 (oK) |
| Langmuir | R2 | 0.9962 | 0.9969 | 0.9972 |
|  | qe, exp (mg/g) | 123.6 | 137.8 | 142.9 |
|  | qe, cal (mg/g) | 137.6 | 112.2 | 101.4 |
|  | KL (mg/g) | 0.012 | 0.018 | 0.023 |
| Freundlich | R2 | 0.7173 | 0.6268 | 0.6878 |
|  | 1/n | 0.653 | 0.416 | 0.386 |
|  | KF (L/g) | 3.53 | 22.47 | 24.31 |
| The pseudo-first order | R2 | 0.5049 | 0.9141 | 0.9256 |
|  | K1 x10-2 | 0.0145 | 0.0245 | 0.0115 |
|  | qe, cal (mg/g) | 57.8 | 89.6 | 193.6 |
| The pseudo-second order | R2 | 0.9911 | 0.9971 | 0.9909 |
|  | K2 x10-3 (g/mg.min.) | 0.413 | 0.303 | 0.198 |
|  | qe, cal (mg/g) | 129.8 | 179.8 | 148.9 |