Supplementary materials

Effective and Reproducible Biosynthesis of Nanogold-composite Catalyst for Paracetamol Oxidation

Veronika Krbečkováa,b, Zuzana Šimonováa,c, Petr Langera, Pavlína Peikertováa, Kateřina Mamulová Kutlákováa, Barbora Thomasováa, Daniela Placháa,c

a Nanotechnology Centre, CEET, VŠB – Technical University of Ostrava, 17. listopadu 2172/15, 708 00, Ostrava, Czech Republic

b Laboratory of Growth Regulators, Palacký University & Institute of Experimental Botany ASCR, Šlechtitelů 27, 783 71 Olomouc, Czech Republic

c ENET Centre, CEET, VŠB – Technical University of Ostrava, 17. listopadu 2172/15, Ostrava, 
708 00, Czech Republic

Table S1: XRFS analysis of the WDE.

|  | SiO2 | Al2O3 | K2O | CaO | P2O5 |
| --- | --- | --- | --- | --- | --- |
| [wt. %] |  |  |  |  |  |
| 1WDE | 81.2±4.1 | 1.89±0.15 | 0.285±0.029 | 0.280±0.022 | 0.245±0.029 |
| 2WDE | 81.5±4.1 | 1.68±0.13 | 0.291±0.029 | 0.258±0.021 | 0.277±0.033 |
| 3WDE | 80.9±4.0 | 1.84±0.15 | 0.274±0.027 | 0.262±0.021 | 0.267±0.032 |
| 4WDE | 81.2±4.1 | 1.90±0.15 | 0.276±0.028 | 0.265±0.021 | 0.239±0.029 |
| 5WDE | 81.2±4.1 | 1.84±0.15 | 0.282±0.028 | 0.268±0.021 | 0.244±0.029 |
|  | SO3 | TiO2 | Fe2O3 | MnO |  |
| 1WDE | 0.194±0.023 | 0.125±0.009 | 0.932±0.047 | 0.008±0.001 |  |
| 2WDE | 0.237±0.028 | 0.121±0.008 | 0.965±0.048 | 0.007±0.001 |  |
| 3WDE | 0.198±0.024 | 0.121±0.008 | 0.918±0.046 | 0.008±0.001 |  |
| 4WDE | 0.194±0.023 | 0.121±0.008 | 0.919±0.046 | 0.007±0.001 |  |
| 5WDE | 0.204±0.024 | 0.123±0.009 | 0.935±0.047 | 0.008±0.001 |  |

Figure S1: A) and B) SEM analysis of the WDE from beer filtration.

Table S2: The average size with standard deviation of Au NPs for Au/WDE samples.

| Sample | Average size [nm] |
| --- | --- |
| 1Au/ WDE | 30±8 |
| 2Au/ WDE | 31±8 |
| 3Au/ WDE | 28±7 |
| 4Au/ WDE | 32±7 |
| 5Au/ WDE | 32±10 |

Table S3: The determination of Au content by ICP-AES method.

| Sample number | Au/WDE [wt. %] | Au/WDE After washing [wt. %] | Efficiency of Au NPs preparation after washing [%] |
| --- | --- | --- | --- |
| 1 | 1.22±0.12 | 1.11±0.11 | 72 |
| 2 | 1.08±0.11 | 1.16±0.12 | 75 |
| 3 | 1.17±0.12 | 1.14±0.11 | 74 |
| 4 | 1.17±0.12 | 1.09±0.10 | 70 |
| 5 | 1.18±0.12 | 1.15±0.12 | 74 |

Figure S2: Size distribution histograms of Au NPs for A) 1Au/WDE, B) 2Au/WDE, C) 3Au/WDE, D) 4Au/WDE a E) 5Au/WDE.

Table S4: XRFS analysis of the WDE with Au NPs.

|  | SiO2 | Al2O3 | CaO | K2O | P2O5 |
| --- | --- | --- | --- | --- | --- |
| [wt. %] |  |  |  |  |  |
| 1Au/ WDE | 81.8±4.1 | 2.41±0.19 | 0.162±0.013 | 0.096±0.010 | <0.001 |
| 2Au/ WDE | 81.5±4.1 | 2.47±0.20 | 0.162±0.013 | 0.098±0.010 | <0.001 |
| 3Au/ WDE | 81.9±4.1 | 2.37±0.19 | 0.150±0.012 | 0.088±0.009 | <0.001 |
| 4Au/ WDE | 82.1±4.1 | 2.35±0.19 | 0.154±0.012 | 0.089±0.009 | <0.001 |
| 5Au/ WDE | 81.9±4.1 | 2.36±0.19 | 0.150±0.012 | 0.091±0.009 | <0.001 |
|  | SO3 | TiO2 | Fe2O3 | MnO |  |
| 1Au/ WDE | <0.005 | 0.078±0.005 | 0.545±0.027 | 0.0040±0.0004 |  |
| 2Au/ WDE | <0.005 | 0.078±0.005 | 0.567±0.028 | 0.004±0.0004 |  |
| 3Au/ WDE | <0.005 | 0.074±0.005 | 0.551±0.028 | 0.004±0.0004 |  |
| 4Au/ WDE | <0.005 | 0.077±0.005 | 0.568±0.028 | 0.004±0.0004 |  |
| 5Au/ WDE | <0.005 | 0.076±0.005 | 0.541±0.028 | 0.004±0.0004 |  |

Figure S3: FTIR spectra of yeast before and after adding of Au precursor.

Figure S4: FTIR spectra of filter DE, L_DE, M_DE and mixtures after addition of Au precursor.

1Corresponding authors

E-mail addresses: holisovaveronika@seznam.cz