Supplementary Information for

Regulating bimetallic active centers for exploring the structure-activity relationship upon high-performance photocatalytic nitrogen reduction

Supplementary Figures

Supplementary Fig. 1 a SEM image and b diameter distribution of TiO2 NFs. c TEM image of the m-TiO2 NRs. d XRD patterns of m-TiO2 NRs and se-Pd/m-TiO2 NRs.

Supplementary Fig. 2 HAADF-TEM image of se-Au/m-TiO2 NRs (a), and the TEM EDS elemental mapping of Ti (b), O (c), and Au (d) elements for se-Au/m-TiO2 NRs.

Supplementary Fig. 3 HAADF-TEM image of se-Pt/m-TiO2 NRs (a), and the TEM EDS elemental mapping of Ti (b), O (c), and Pt (d) elements for se-Pt/m-TiO2 NRs.

Supplementary Fig. 4 TEM (a) and HRTEM (b) images of fe-Pd/m-TiO2 NRs. TEM (c) and HRTEM (d) images of fe-Au/m-TiO2 NRs. TEM (e) and HRTEM (f) images of fe-Pt/m-TiO2 NRs. The insets of (a), (c), and (e) are the particle size distribution of fe-Pd, Au, and Pt NPs. Spatial distribution of the LSPR-induced enhancement of the electric field intensity from the FDTD simulations for the fe-Pd/m-TiO2 NRs (g), fe-Au/m-TiO2 NRs (h) and fe-Pt/m-TiO2 NRs (i) at excitation wavelengths of 550 nm.

Supplementary Fig. 5 Time-resolved PL decay spectra of (a) m-TiO2 NRs, (b) se-Pd/m-TiO2 NRs, (c) se-Au/m-TiO2 NRs, (d) se-Pt/m-TiO2 NRs, (e) fe-Pd/m-TiO2 NRs, (f) fe-Au/m-TiO2 NRs and (g) fe-Pt/m-TiO2 NRs.

Supplementary Fig. 6 N2 adsorption-desorption isotherms and the corresponding pore size distribution curves (insert) of (a) m-TiO2 NRs, (b) se-Pd/m-TiO2 NRs, (c) se-Au/m-TiO2 NRs, (d) se-Pt/m-TiO2 NRs, (e) fe-Pd/m-TiO2 NRs, (f) fe-Au/m-TiO2 NRs and (g) fe-Pt/m-TiO2 NRs.

Supplementary Fig. 7 Absolute calibration of the indophenol blue method using NH4Cl solutions of known concentration as standards. a UV-vis curves of indophenol assays with NH4+ after incubated for 0.5 h at room temperature. b Calibration curve used for estimation of NH3 by NH4+ concentration. The absorbance at 630 nm was measured by UV-vis spectrophotometer, and the fitting curve shows good linear relation of absorbance with NH4+ concentration (y = 0.01293x + 0.03735, R2 = 0.99991) of calibration curves. c Calibration curve of NH4+ with indophenol indicator (y = 0.7185x + 0.03735, R2 = 0.99991).

Supplementary Fig. 8 Absolute calibration of the Watt and Chrisp (para-dimethylaminobenzaldehyde) method for the estimating of N2H4 concentration using N2H4·H2O solutions with known concentration as standards. a UV-Vis absorption spectra of various N2H4 concentrations after incubated for 20 min at room temperature. b Calibration curve used for estimation of N2H4 concentration. The absorbance at 458 nm was measured by UV-vis spectrophotometer, and the fitting curve shows good linear relation of absorbance with N2H4 concentration (y = 1.042x + 0.01433, R2 = 0.99996) of calibration curves. c UV-vis absorption spectra of reaction solution by different catalysts in the first 1 h. No N2H4 was detected at 458 nm.

Supplementary Fig. 9 The schematic of the photochemical setup for N2 fixation.

Supplementary Fig. 10 a AQEs (green pentagram) for pNRR over se-Pd/m-TiO2 NRs in pure water under monochromatic light irradiation in regard to its UV–vis DRS spectrum (cyan line). b Schematic illustration of the in situ FTIR instrument with a cold white light LED illumination.

Supplementary Fig. 11 Mass spectral illustrations of the indophenol from (a) 14N2 and (b) 15N2 atmospheric conditions; the insets of (a) and (b) show the chemical structure of the indophenol anion responsible for the signals at m/z 198 (containing 14N) and 199 (containing 15N).

Supplementary Fig. 12 The optimized geometric structures of TiO2 (101), Pd (111), OVs-TiO2 (101)/Pd (111), TiO2 (101)/Pd (111) interface. Color code: Gray, red, dark cyan, and yellow spheres represent Ti atoms, O atoms, Pd atoms, and OVs, respectively.

Supplementary Fig. 13 The optimized geometric structures of Au (111), OVs-TiO2 (101)/Au (111) and TiO2 (101)/Au (111) interface. Color code: Gray, red, auratus, and yellow spheres represent Ti atoms, O atoms, Pd atoms, and OVs, respectively.

Supplementary Fig. 14 The optimized adsorption configuration of N2 molecule on Au (111), OVs-TiO2 (101)/Au (111) and TiO2 (101)/Au (111) interface.

Supplementary Fig. 15 The number of electrons transferred to N2 molecules on (a) Au (111), (b) OVs-TiO2 (101)/Au (111) and (c) TiO2 (101)/Au (111) interface model are illustrated by first-principles simulations.

Supplementary Fig. 16 Differential charge density of N2-TiO2 (101)/Au (111) interface (yellow and orange red colors illustrate an enhancement and reduction in electron density, accordingly).

Supplementary Fig. 17 The optimized geometric structures of Pt (111), OVs-TiO2 (101)/Pt (111) and TiO2 (101)/Pt (111) interface. Color code: Gray, red, blue, and yellow spheres represent Ti atoms, O atoms, Pd atoms, and OVs, respectively.

Supplementary Fig. 18 The optimized adsorption configuration of N2 molecule on Pt (111), OVs-TiO2 (101)/Pt (111) and TiO2 (101)/Pt (111) interface.

Supplementary Fig. 19 The number of electrons transferred to N2 molecules on (a) N2-Pt (111), (b) N2-OVs-TiO2 (101)/Pt (111), and (c) N2-Pt (111)/TiO2 (101) interface model are illustrated by first-principles simulations.

Supplementary Fig. 20 Differential charge density of N2-Pt (111)/TiO2 (101) interface (yellow and orange red colors illustrate an enhancement and reduction in electron density, accordingly).

Supplementary Fig. 21 Adsorption energies of N2 on single site of Au, Pt, OVs of TiO2 (101)/Au (111), Ti site of TiO2 (101)/Au (111) interface, OVs of TiO2 (101)/Pt (111), and on Pt sites at TiO2 (101)/Pt (111) interface.

Supplementary Fig. 22 N−N distance of *NN on Au (111), Pt (111), OVs in TiO2 (101)/Au (111), the Ti site at the TiO2 (101)/Au (111) interface, OVs in TiO2 (101)/Pt (111), and Pt site at the TiO2 (101)/Pd (111) interface.

Supplementary Fig. 23 Catalytic measurements for light-driven N2 fixation using various catalysts. a Photocatalytic NH3 production rate over the x%-Pd/m-TiO2 NRs in the first 1 h. b Comparison of NH3 production rates over m-TiO2 NRs, se-Pd/m-TiO2 NRs (2.71%), se-Au/m-TiO2 NRs (2.92%), se-Pt/m-TiO2 NRs (2.84%), fe-Pd/m-TiO2 NRs (2.62%), fe-Au/m-TiO2 NRs (2.76%) and fe-Pt/m-TiO2 NRs (2.86%) in N2-saturated water under light irradiation.

Supplementary Tables

Supplementary Table 1. The amount of noble metal loaded on the m-TiO2 NRs samples determined by ICP-OES.

| Samples | se-Pd/m-TiO2 NRs (0%) | se-Pd/m-TiO2 NRs (1%) | noble metal/m-TiO2 NRs (3%) |  |  |  |  |  |  |  |  |  |  | se-Pd/m-TiO2 NRs (5%) | se-Pd/m-TiO2 NRs (7%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | se-Pd | se-Au |  |  | se-Pt | fe-Pd |  |  | fe-Au | fe-Pt |  |  |  |
| Metal content (wt.%) | 0.00 | 1.02 | 2.71 |  | 2.92 | 2.84 |  |  | 2.62 | 2.76 |  |  | 2.86 | 4.76 | 6.66 |

Supplementary Table 2. EXAFS fitting parameters at the Pd K-edge for various samples (Ѕ02 = 0.87)

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Pd foil | Pd-Pd | 12.00 | 2.74 | 0.0052 | -6.15 | 0.0041 |
| PdO | Pd-O | 4.35 | 2.03 | 0.0021 | -0.46 | 0.0188 |
|  | Pd-O-Pd | 4.00 | 3.05 | 0.0034 | -1.22 |  |
|  | Pd-Pd | 8.00 | 3.44 | 0.0034 | -1.22 |  |
|  | Pd-O | 8.00 | 3.69 | 0.0021 | -0.46 |  |
| se-Pd/TiO2 NRs | Pd-O | 3.80 | 2.07 | 0.0036 | -7.73 | 0.0177 |
|  | Pd-Ti | 2.20 | 3.14 | 0.0024 | -0.34 |  |
|  | Pd-Pd | 7.40 | 3.39 | 0.0109 | -3.59 |  |

a)CN, coordination number; bR(Å), distance between absorber and backscatter atoms; cσ2, Debye-Waller factor to account for both thermal and structural disorders; dΔE0, inner potential correction; R factor indicates the goodness of the fit. Fitting range: 3.0 ≤ k (/Å) ≤ 12.4 and 1.0 ≤ R (Å) ≤ 3.0 (Pd foil); 3.0 ≤ k (/Å) ≤ 12.0 and 1.1 ≤ R (Å) ≤ 3.5 (PdO); 3.3 ≤ k (/Å) ≤ 10.0 and 1.2 ≤ R (Å) ≤ 3.4 (se-Pd/TiO2 NRs).

Supplementary Table 3. The fitted photoluminescence decay components of m-TiO2 NRs, se-Pd/m-TiO2 NRs, se-Au/m-TiO2 NRs, se-Pt/m-TiO2 NRs, fe-Pd/m-TiO2 NRs, fe-Au/m-TiO2 NRs, and fe-Pt/m-TiO2 NRs.

| Samples | Decay Time (ns) |  | Relative amplitude (%) |  | Average lifetime (ns) |
| --- | --- | --- | --- | --- | --- |
|  | τ1 | τ2 | A1 | A2 | τAa |
| m-TiO2 NRs | 1.011 | 5.04 | 42.49 | 57.51 | 4.52 |
| se-Pd/m-TiO2 NRs | 1.004 | 10.97 | 37.96 | 62.04 | 10.44 |
| se-Au/m-TiO2 NRs | 1.002 | 9.903 | 40.17 | 59.83 | 9.34 |
| se-Pt/m-TiO2 NRs | 1.07 | 10.00 | 50.99 | 49.01 | 9.10 |
| fe-Pd/m-TiO2 NRs | 0.69 | 11.04 | 87.99 | 12.01 | 7.79 |
| fe-Au/m-TiO2 NRs | 0.298 | 9.05 | 68.25 | 31.75 | 8.47 |
| fe-Pt/m-TiO2 NRs | 0.6 | 10.01 | 91.06 | 8.94 | 6.44 |

aτA = (A1τ12 + A2τ22)/(A1τ1 + A2τ2)

Supplementary Table 4. The noble metal mean particle size, BET surface area and average pore size of different samples.

| Samples | Mean metal particle sizea (nm) | BET surface areab (m2 g-1) | Average pore sizec (nm) |
| --- | --- | --- | --- |
| m-TiO2 NRs | - | 45.18 | 12.7 |
| se-Pd/m-TiO2 NRs | 12.2 | 32.78 | 14.2 |
| se-Au/m-TiO2 NRs | 10.1 | 35.49 | 13.4 |
| se-Pt/m-TiO2 NRs | 9.6 | 40.60 | 12.1 |
| fe-Pd/m-TiO2 NRs | 4.7 | 44.14 | 13.1 |
| fe-Au/m-TiO2 NRs | 6.2 | 43.15 | 11.6 |
| fe-Pt/m-TiO2 NRs | 3.5 | 44.86 | 12.6 |

aMean metal particle size statisticsed according to the TEM image.

bSBET, BET surface areas calculated by the adsorption branch of the N2 isotherm.

cDBJH, pore diameter determined by BJH model.

Supplementary Table 5. The AQE for photocatalytic N2 fixation in recent reports.

| Catalysts | AQE | References |
| --- | --- | --- |
| Se-Pd/m-TiO2 NRs | 0.37% at 375 nm | This work |
| Mo-doped WO3 | 0.33% at 400 nm | 13 |
| TiO2/Au/a-TiO2 | 0.005% at 254 nm | 14 |
| CuCr-LDH | 0.44% at 380 nm | 15 |
| Bi5O7Br | 2.3% at 420 nm | 16 |
| BiOCl NSs-Fe-5% | 1.8% at 420 nm | 17 |
| BiOBr | 0.23% at 420 nm | 18 |

Supplementary Table 6. Performance comparison of various photocatalysts for N2 reduction.

| Catalysts | Reaction medium | Scavenger | Light source | Detection Method | Ammonia generation rate (μg gcat.-1 h-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Se-Pd/m-TiO2 NRs | H2O (l) | No | Full-spectrum | Indophenol blue method | 635.73 | This work |
| TiO2 (P25) | H2O (l), | No | Full-spectrum | IC | 27 | 19 |
| Ti3C2 MXene-P25 | H2O (l) | No | Full-spectrum | IC | 193.32 | 20 |
| JRC-TiO-6 | H2O, 38 ℃ | 2-PrOH | λ > 280 nm | IC | 62 | 21 |
| Ti-MOF | H2O (l), | No | λ > 400 nm | Indophenol blue method and IC | 221.40 | 22 |
| SA Ru/TiO2-NS | H2O (l) | CH3OH | Full-spectrum | Indophenol blue method | 56.34 | 23 |
| Sb/TiO2 | H2O (l) | No | Full-spectrum | Indophenol blue method | 579.60 | 24 |
| Fe-Al@graphene | 311 K | No | Full spectrum | Indophenol blue method | 430.1 | 25 |

Supplementary Methods

Determination of NH3

The NH3 in the photocatalytic reaction solution was quantified by the indophenol method according to previous work1. For calibration in aqueous electrolytes, a known concentration of NH4Cl was added to 0.1 M KOH, and then neutralized by adding 0.5 M H2SO4. 0.5 mL of phenol nitroprusside solution and 0.5 mL of alkaline hypochlorite solution was then added to 2.0 ml of the neutralized sample. The solution was incubated for 30 min at room temperature in the dark, and the sample absorbance was analyzed by UV-vis spectroscopy (UV-17800, Shimadzu). The calibration curve was constructed for NH3 with the following concentrations:

a: 0 μmol L-1 (0 μg mL-1), b: 0.1 μmol L-1 (0.0018 μg mL-1), c: 0.2 μmol L-1 (0.0036 μg mL-1), d: 0.5 μmol L-1 (0.009 μg mL-1), e: 1.0 μmol L-1 (0.018 μg mL-1), f: 2.0 μmol L-1 (0.036 μg mL-1), g: 5.0 μmol L-1 (0.09 μg mL-1), h: 10 μmol L-1 (0.18 μg mL-1), i: 20 μmol L-1 (0.36 μg mL-1), j: 50 μmol L-1 (0.9 μg mL-1), and a fitted curve of the absorbance peak of each concentration showed a linear regression with an R2 value of 0.99991 (see Supplementary Fig. 7).

Determination of hydrazine (N2H4)

The hydrazine presented in the photocatalytic reaction solution was estimated by the method of Watt and Chrisp with some modification2-4, which contains the following steps: (ⅰ) 2.0 mL post-pNRR solution was collected from photochemical reactor with further removal of the photocatalyst by using the 0.22 μm filter. (ⅱ) 2.0 mL of color agent was added into post-pNRR solution. The color reagent solution consists of 5.99 g of para-(dimethylamino) benzaldehyde, 30 mL of HCl, and 300 mL ethanol. After reacting in a dark condition at room temperature for 20 min, the sample absorbance was investigated by UV-vis spectroscopy (UV-17800, Shimadzu). The correction curve was established for N2H4 with the following concentrations:

a: 0 μg mL-1, b: 0.05 μg mL-1), c: 0.1 μg mL-1, d: 0.2 μg mL-1, e: 0.4 μg mL-1, f: 0.6 μg mL-1, g: 0.8 μg mL-1), h: 1.0 μg mL-1, and a fitted curve of the absorbance peak at λ = 458 nm of each concentration showed a linear regression with an R2 value of 0.99996 (see Supplementary Fig. 8).

Photocatalytic nitrogen fixation

The photocatalytic nitrogen-fixing ammonia synthesis experiment was carried out in self-assembled photocatalytic reaction platform as shown in Supplementary Fig. 9. The photocatalytic N2 fixation is achieved on the three-phase interface, including N2 in the gas, H2O in the liquid and the catalyst in the solid phase. Synthetic ammonia performance experiments were conducted at room temperature and atmospheric pressure. A 300 W Xe lamp (Full-spectrum, 400 mW·cm-2) was used as light source and 10 cm away from the light source to the liquid surface. Firstly, 40 mg photocatalyst were dispersed in 100 mL deionized water in a cell equipped with water circulation. Secondly, the mixture was continuously stirred in the dark with high-purity N2 bubbled at a flow rate of 200 mL·min-1 for 30 min, then turn on the light and 4.0 mL of reaction solution was taken out from the reaction in every 30 min. The reaction mixture was purified by removing the photocatalyst by using the 0.22 μm filter. The obtained solution was used for further analysis.

Determination of apparent quantum efficiency (AQE)

The catalytic experiments for determining AQE were performed in 100 mL pure water, and the irradiation area was 19.63 cm2. 40 mg of se-Pd/m-TiO2 NRs was used as the photocatalyst. To obtain the AQE, the light was filtered by different monochromatic filters (i.e., 320, 375, and 520 nm), and the reaction time was 1 h. The light intensities were measured to be 5.10, 12.32, and 42.20 mW cm-2, respectively. The AQE was calculated through the following equation:

AQE = NeNp = 3NAMNp = 3nAMNAWAthν × 100 %

where Ne, Np and NAM represent the number of reacted electrons, incident photons and generated ammonia, respectively; nAM represents the molar number of generated ammonia; ν, W, A and t are the incident light frequency, intensity, irradiation area and time, respectively; NA and h are the Avogadro’s constant and Planck constant, respectively.

15N2 isotope labeling experiments

Isotopic labeling experiments labeled 15N2 gas was purchased from Sigma-Aldrich Chemical Company. It was used to confirm that the detected ammonia originates form N2. A low-velocity gas flow system was adopted due to the limited supply and high expense of 15N2. Firstly, 40 mg photocatalyst were dispersed in 100 mL deionized water in a cell equipped with water circulation. Secondly, the mixture was continuously stirred in the dark with high-purity N2 bubbled at a flow rate of 100 mL·min-1 for 10 min, then turn on the light and 4.0 mL of reaction solution was taken out after 30 min illumination and further removing the photocatalyst by using the 0.22 μm filter. Estimation of obtained 15NH4+ was done indirectly using the indophenol method, owing to the low mass of 15NH4+ for LC-MS studies. The samples for LC-MS analysis were prepared as follows. 0.5 mL phenol nitroprusside solution (P6994, Sigma-Aldrich) and 0.5 mL of alkaline hypochlorite solution (A1727, Sigma-Aldrich) were then added to 2.0 mL of the resulting solution. The MS studies were carried on an Agilent 1260-6460 (LC-MS).

Finite-Difference Time-Domain simulations

To investigate the optical mechanisms behind the structure, Finite-Difference Time-Domain (FDTD) simulations were carried out using FDTD Solutions software (Lumerical Co. Ltd). Plane wave was used as the light source with different wavelength. Periodic boundary was used along the x-axis and y-axis, and the perfect match layer (PML) boundary was used along the z-axis. Mesh size was set as 0.01 nm for the structure during FDTD simulations.

N2 temperature-programmed desorption (N2-TPD)

100 mg of catalyst was placed at the bottom of the U-shaped quartz tube and preheated in Ar flow (50 mL min-1) at 300 °C for 0.5 h and then cooled down to 25 °C. After pretreatment, the feeding N2 flowed through the catalyst bed at 25 °C for 1 h. Then, the physisorption of N2 was removed by Ar flow (50 mL min-1) at 50 °C for 0.8 h. Finally, the catalyst bed was heated from 50 °C to 600 °C at 10 °C min-1. We monitored a wide range of desorbing species to identify the main products that are generated from reactions of N2 on catalyst and found that the only species desorbed from the N2-exposed samples is N2, as analyzed on-line by a thermal conductivity detector (TCD, Micromeritics AutoChem II 2920).

X-ray absorption spectra collection and data processing

The obtained XAFS data was processed in Athena (version 0.9.26) for background, pre-edge line and post-edge line calibrations5. Then Fourier transformed fitting was carried out in Artemis (version 0.9.26). The model of Pd foil and PdO were used to calculate the simulated scattering paths. The four parameters, coordination number, bond length, Debye-Waller factor and ΔE0 shift (CN, R, σ2, ΔE0) were fitted and partially fixed. For the Wavelet Transform analysis6,7, the χ(k) exported from Athena was imported into the Hama Fortran code. The parameters were listed as follow: R range, 1 – 3.5 Å, k range, 3.0 – 13.9 Å−1; k weight, 3; and Morlet function with κ = 5, σ = 1 was used as the mother wavelet to provide the overall distribution.

In-situ Fourier-transform infrared spectroscopy experiments

In-situ Fourier-transform infrared spectroscopy (FTIR) was performed by adopting a Nicolet-iS50 Fourier-transform infrared spectrometer, equipped with a Harrick Scientific in-situ cell and a mercury-cadmium-telluride (MCT) detector cooled by liquid N2. The sample (20 mg) was pressed into thin slices by a hydraulic machine and placed in the in-situ cell. Then, the system was evacuated to an internal pressure of 10-4 mbar and heated at 200 ℃ for 60 min with a heating rate of 8.5 ℃ min-1. When the temperature was cooled to 30 ℃, the molecular pump was closed and then the background was tested. After that, pure N2 with H2O vapor was pumped into the in-situ cell. At the same time, the light was turned on to drive the reaction and the IR signal was tested every 5 min.

Density functional theory simulations

The density functional theory (DFT) simulations were performed by using the Cambridge Sequential Total Energy Package (CASTEP) module implemented in the Material Studio 8.0 package8-10. The exchange correlation potential was represented by the Perdew–Burke–Ernzerhof (PBE) functional within the generalized gradient approximation (GGA)11. The TiO2 (101), Pd (111), Au (111) and Pt (111) surfaces were built. Then, TiO2 (101) with OVs and Pd (111) interface, TiO2 (101) with oxygen vacancy and Au (111) interface, TiO2 (101) with oxygen vacancy and Pt (111) interface were built, and the vacuum layer is set to 15 Å. The cutoff energy for the plane-wave-basis expansion is set to be 500 eV, and the convergence tolerances of energy, force and maximum displacement are set to 1.010-5 eV/atom, 5.010-2 eV/Å and 2.010-3 eV/Å, respectively. The k-points grid sampling of Monkhorst-Pack scheme was set as 1×2×1 in the irreducible Brillouin zone. Meanwhile, the DFT-D correction method is used to describe the long-range van der Waals interaction12. The adsorption energy (Eab) of N2 was defined as:

Eab = E(sub+N2) - E(sub) - E(N2)

E(sub+N2) and E(sub) are the total energy of the system with and without N2. E(N2) is the total energy of N2 molecules. The Gibbs free energy change (ΔG) of the elementary step was calculated by:

∆G = ∆E + ∆EZPE - T∆S

Where ∆E is the total energy difference, ΔEZPE is the change in the zero-point energy and the entropy, T is the temperature (T = 298.15 K), and ΔS is the entropy change.

Supplementary References

- Andersen, S. Z. et al. A rigorous electrochemical ammonia synthesis protocol with quantitative isotope measurements. Nature, 570, 504−508 (2019).

- Watt, G. W. & Chrisp, J. D. A spectrophotometric method for the determination of hydrazine, Anal. Chem. 24, 2006–2008 (1952).

- Zhao, J. X. et al. Defect-rich ZnS nanoparticles supported on reduced graphene oxide for high-efficiency ambient N2-to-NH3 conversion. Appl. Catal., B 284, 119746 (2021).

- Qiu,W. B. et al. High-performance artificial nitrogen fixation at ambient conditions using a metal-free electrocatalyst. Nat. Commun. 9, 3485 (2018).

- Ravel, B. & Newville, M. ATHENA, ARTEMIS, HEPHAESTUS: data analysis for X-ray absorption spectroscopy using IFEFFIT, J. Synchrotron Radiat. 12, 537–541 (2005).

- Funke, H.; Scheinost, A. C.; Chukalina, M. Wavelet analysis of extended X-ray absorption fine structure data. Phys. Rev. B, 71, 094110 (2005).

- Funke, H.; Chukalina, M.; Scheinost, A. C. A new FEFF-based wavelet for EXAFS data analysis. J. Synchrotron Radiat. 14, 426–432 (2007).

- Kresse, G. D. & Joubert, J. From ultrasoft pseudopotentials to the projector augmented wave method. Phys. Rev. 59, 1758 (1999).

- Kresse, G. & Furthmüller, J. Efficiency of ab-initio total energy calculations for metals and semiconductors using a plane-wave basis set. Comp. Mater. Sci. 6, 15–50 (1996).

- Kresse, G. & Furthmüller, J. Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. Phys. Rev. 54, 11169 (1996).

- Perdew, J. P.; Burke, K.; Ernzerhof, M. Generalized gradient approximation made simple. Phys. Rev. Lett. 77, 3865 (1996).

- Grimme, S.; Antony, J.; Ehrlich, S.; Krieg, H. A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. J. Chem. Phys. 132, 154104 (2010).

- Zhang, N. et al. Refining defect states in W18O49 by Mo doping: A strategy for tuning N2 activation towards solar driven nitrogen fixation. J. Am. Chem. Soc. 140, 9434–9443 (2018).

- Li, C. et al. Promoted fixation of molecular nitrogen with surface oxygen vacancies on plasmon-enhanced TiO2 photoelectrodes. Angew. Chem. Int. Ed. 57, 5278–5282 (2018).

- Zhao, Y. et al. Layered-double-hydroxide nanosheets as efficient visible-light-driven photocatalysts fordinitrogen fixation. Adv. Mater. 29, 1703828 (2017).

- Wang, S. et al. Light-switchable oxygen vacancies in ultrafine Bi5O7Br nanotubes for boosting solar-driven nitrogen fixation in pure water. Adv. Mater. 29, 1701774 (2017).

- Zhang, N. et al. Fe-doped BiOCl nanosheets with light-switchable oxygen vacancies for photocatalytic nitrogen fixation. ACS Appl. Energy Mater. 2, 8394−8398 (2019).

- Li, H.; Shang, J.; Ai, Z. H.; Zhang, L. Z., Efficient visible light nitrogen fixation with BiOBr nanosheets of oxygen vacancies on the exposed {001} facets. J. Am. Chem. Soc. 137, 6393–6399 (2015).

- Gao, X. et al. Interference effect of alcohol on Nessler’s reagent in photocatalytic nitrogen fixation. ACS Sustain. Chem. Eng. 6, 5342–5348 (2018).

- Liao, Y. et al. 2D-layered Ti3C2 MXenes for promoted synthesis of NH3 on P25 photocatalysts. Appl. Catal., B 273, 119054 (2020).

- Hirakawa, H.; Hashimoto, M.; Shiraishi, Y.; Hirai, T.; Photocatalytic conversion of nitrogen to ammonia with water on surface oxygen vacancies of titanium dioxide. J. Am. Chem. Soc. 139, 10929–10936 (2017).

- Huang, H. et al. Toward visible-light-assisted photocatalytic nitrogen fixation: A titanium metal organic framework with functionalized ligands. Appl. Catal., B 267, 118686 (2020).

- Liu, S.; et al. Photocatalytic fixation of nitrogen to ammonia by single Ru atom decorated TiO2 nanosheets. ACS Sustain. Chem. Eng. 7, 6813–6820 (2019).

- Zhao, Z. Q. et al. Efficient visible-light driven N2 fixation over two-dimensional Sb/TiO2 composites. Chem. Comm. 55, 7171–7174 (2019).

- Yang, Y. et al. Highly enhanced stability and efficiency for atmospheric ammonia photocatalysis by hot electrons from a graphene composite catalyst with Al2O3. Carbon 124, 72–78 (2017).