Supplementary Information

Intermediate C=O Formation Is the Bottleneck of Overall Water Splitting on Carbon Nitride

Ji Wu1, Zhonghuan Liu1, Xinyu Lin1, Enhui Jiang1, Shuai Zhang1, Pengwei Huo1, Yan Yan1*, Peng Zhou2*, Yongsheng Yan1

1Institute of Green Chemistry and Chemical Technology, School of Chemistry and Chemical Engineering, Jiangsu University, Zhenjiang 212013, PR China,

2Department of Electrical Engineering and Computer Science, University of Michigan, Ann Arbor, MI 48109, USA.

Corresponding authors:

Y. Yan (dgy5212004@163.com)

P. Zhou (dpzhou@umich.edu)

Supplementary Methods

Materials

Melamine (C3H6N6), sodium fluoride (NaF), perchloric acid (HClO4), nitric acid (HNO3) and ethanol (C2H5OH) were purchased from Sinopharm Chemical Reagent Co. Ltd. Chloroplatinic acid hexahydrate (H2PtCl6∙6H2O), deuterium oxide (D2O, 99 atom % D) and heavy oxygen water (H218O, 97 atom % 18O) were obtained from Sigma-Aldrich Company Ltd. All reagents used in the synthesis were analytical grade and used without further purified. Deionized water, with a resistivity of 18 MΩcm, was used throughout the experiments.

Preparation of pristine CN

Typically, CN was synthesized by calcining melamine powder (10 g) at 550 °C for 4 h with a ramping rate 5 °C min−1 in static air in a muffle furnace. After naturally cooling down to room temperature, the resulting product was subsequently dissolved into 0.5 M HNO3 solution bathing for 4 h at 80 °C. Then, light yellow agglomerates were gathered, cross-washed with deionized water and ethanol for several times, and then dried at 60 °C in vacuum oven for further uses.

Preparation of F-CN

FX-CN sample were prepared by a one-step hydrothermal treatment of pristine CN. In a typical procedure, the pristine CN (1 g) was mixed in aqueous solutions containing different concentrations of NaF (0.01-1 mM) with stirring for 30 min, and the pH was adjusted to 3.5 by HClO4. Then, the resulting solution was transferred to a sealed Teflon container at 180 °C for 12 h. The final sample was obtained, labeling as FX-CN (x represents the NaF concentration employed). Exfoliated CN (CN-E) sample was prepared under otherwise identical conditions without NaF.

Characterizations

In-situ diffuse reflection infrared Fourier transform spectroscopy (DRIFTS) experiments were performed on a Thermo Nicolet iS10 spectrometer equipped with a mercury cadmium telluride (MCT) detector. The near-ambient pressure X-ray photoelectron spectroscopy (NAP-XPS) experiments were conducted on a laboratory-based SPECS near-ambient pressure XPS system. The XRD patterns were examined on a Shimazu-6100 powder X-ray diffractometer using Cu Kα radiation at a scan rate of 7° min-1. Electron Microscope (TEM) analyses were performed on an H-7800 microscope with an acceleration voltage of 120 kV. The ultraviolet-visible diffuse reflectance spectroscopy (UV-vis DRS) was recorded on a Shimadzu UV-3600 spectrometer with BaSO4 as reference. The isotopic labeled experiments were carried out on a gas chromatography-mass spectrometry (GC-MS, Agilent 7890B-5977B). Transient fluorescence decay spectra were characterized on an Edinburgh FLS1000 fluorescence spectrometer. N2 adsorption-desorption isotherms were obtained on a BEL SORP mini (Microtrac BEL, Japan).

Photocatalytic water splitting experiments

Photocatalytic overall water splitting reactions were carried out in a top-irradiation Pyrex reactor connected to a glass sealed gas system with a 300 W Xenon lamp (1000 mW∙cm-2) as the white light source. 30 mg catalyst was dispersed in 100 ml of pure water and 3wt% Pt as co-catalysts was loaded via in situ photo-deposition using H2PtCl6∙6H2O without any sacrificial agents, equipped recirculating cooling water at 6 °C. The gas productions were monitored by a gas chromatography assembled with a thermal conduction detector (TCD, 5 A molecular sieve columns) using Ar as carrier gas. All reactions were carried out at 279 K in low vacuum.

In-situ DRIFTS experiments

In-situ diffuse reflection infrared Fourier transform spectroscopy (DRIFTS) experiments were implemented on a Thermo Scientific Nicolet iS10 spectrometer equipped with a mercury cadmium telluride (MCT) detector. In a typical procedure, the catalyst was housed in a sample groove inside a sealed reaction cell with two ZnSe windows and a quartz window, as well as H2O was carried into the reaction cell by N2 flow until equilibrium, and IR spectra were recorded during the in situ photoreactions with a 420 nm LED lamb (3 W) as light source though the quartz window. Prior to isotopic experiments, pristine CN and F-CN samples were heated at 423 k for 30 min under flowing N2 to remove the remaining water, which was used for IR test under identical conditions to exclude H2O/H218O exchange.

In-situ NAP-XPS experiments

The near-ambient pressure X-ray photoelectron spectroscopy (NAP-XPS) experiments were conducted on a laboratory-based SPECS near-ambient pressure XPS system (base pressure < 5 × 10 -10 mbar) with a monochromatic Al Kα X-ray source, equipped with an in-situ reaction chamber that permits specific gas to flow the reaction chamber during data acquisition. The catalyst, anchored at a Ta-based lame of the groove inside the reaction chamber as well as H2O was carried into the samples via a variable leak valve connected to a glass bulb containing MilliQ water (18 MΩ∙cm-1), and the water was freeze degassed several times using liquid nitrogen before the reaction. The NAP-XPS spectra were collected by the in-situ reaction chamber with 0.2 mbar H2O vapor pressure using a 300 W Xenon lamp as the white light source in 15 min through the quartz window. All NAP-XPS spectra were calibrated to the Ta 4d5/2 peak at 230 eV.

H2O2 quantification

The H2O2 production was quantified by the well-reported Ghormley triiodide method1. In a typical procedure, a sample volume of 0.2 mL was extracted and diluted by H2O and mixed with 0.1 mL of 1 M KI and 0.1 mL of 1 M HAc/NaAc (including a few drops of ammonium dimolybdate acting as a catalyst for the oxidation of I- by H2O2). I- was oxidized to I3- in the presence of H2O21. The absorbance of the product I3- was subsequently measured spectrophotometrically at 350 nm and compared to a linear calibration curve.

Computational methods

The free energy profiles of OER on CN and F-CN were investigated by the Vienna Ab-initio Simulation Package (VASP) with the revised Perdew-Burke-Ernzerh functional of (RPBE) of the generalized gradient approximation (GGA). PAW pseudo-potential was used to describe the interaction between ionic core and valence electrons. A 2 × 3 supercell was used to simulate the CN layer. One F atom was used to bond with the C atom in CN, formed the F-CN layer. The energy cutoff of plane-wave basis of 400 eV and the energy convergence threshold of 1.0 × 10-5 eV were used in the geometry optimization at gamma point. After geometry optimization, the projected density of states (PDOS) and the charge density difference mappings between intermediate and photocatalyst surface were calculated with energy convergence threshold of 1.0 × 10-5 eV and the energy cutoff of plane-wave basis of 400 eV at gamma point. The calculations of Gibbs free energy changes (ΔG) of all reaction steps adopted the reported standard hydrogen electrode (SHE) model2, which was obtained from the following formula:

G=E + ZPE –TS

Where E, ZPE and S are the electronic free energy, zero-point energy and entropy of model at T = 298.15 K, respectively.

References

1. Diesen, V. & Jonsson, M. Formation of H2O2 in TiO2 Photocatalysis of Oxygenated and Deoxygenated Aqueous Systems: A Probe for Photocatalytically Produced Hydroxyl Radicals. J. Phys. Chem. C. 118, 10083-10087 (2014).

2. J. K. Nørskov., J. R., A. Logadottir & L. Lindqvist. Origin of the Overpotential for Oxygen Reduction at a Fuel-Cell Cathode. J. Phys. Chem. B. 108, 17886-17892 (2004).

Supplementary Figures

Supplementary Figure 1. TEM images of (a) CN, (b) CN-E and (c) F0.1-CN.

Supplementary Figure 2. XRD patterns of CN, CN-E and different F-CN catalysts.

Supplementary Figure 3. (a) NAP-XPS C1s spectra and (b) F1s spectra on both the CN and F0.1-CN samples to show the C-F interaction.

Supplementary Figure 4. In-situ NAP-XPS observations of C1s spectra on (a) pristine CN and (b) F0.1-CN catalysts with 0.2 mbar H2O vapor pressure using a 300 W Xenon lamp as the white light source in 15 min; and in-situ NAP-XPS observation of N1s spectra on (c) pristine CN  and (d) F0.1-CN catalysts with 0.2 mbar H2O vapor pressure using a 300 W Xenon lamp as the white light source in 15 min.

Supplementary Figure 5. N2 adsorption-desorption isotherms of CN, CN-E and F0.1-CN. inset shows the BET surface area of different samples.

Supplementary Figure 6. Control experiments to demonstrate the changed hydrophilic feature of CN after fluorination. (a) Photographs to show the time-resolved sedimentation of 100 mg CN and F1-CN in 10 mL water. (b) Photographs to show the time-resolved sedimentation of 100 mg CN and F1-CN in 10 mL acetonitrile. Surface contact angle measurements on (c) the pristine CN and (d) F1-CN samples on ITO substrates.

Supplementary Figure 7. Control experiments of photocatalytic H2 and O2 production without light, without catalysts or without H2O on F0.1-CN sample.

200 nm

200 nm

200 nm

(b)

Supplementary Figure 8. GC-MS profiles of gas products with F0.1-CN catalyst in (a) deuterium-labeled D2O and (b) 18O-labeled H218O.

Supplementary Figure 9. In-situ detection of H2O2 production during continuous photocatalytic overall water splitting on F0.1-CN.

Supplementary Figure 10. Time course comparison of the white-light photocatalytic overall water splitting on F0.1-CN (a), CN (b) and CN-E catalysts.

Supplementary Figure 11. XPS valence band spectra near Fermi level of the CN and F0.1-CN samples.

Supplementary Figure 12. Simulated 2 × 3 supercell of (a) CN and (b) F-CN layers by using one F atom to bond with the C atom in CN.

Supplementary Figure 13. (a) Water adsorption and activation simulation on N site in pristine CN (denoted CN(N)). (b) Charge density difference mappings between *OH intermediate and catalyst surface on the CN(N). The blue and yellow isosurfaces stand for the negative and positive charges, respectively.

Supplementary Tables

Supplementary Table 1. Wavelength-dependent water splitting performances and AQYs on F0.1-CN catalyst.

| Wavelength (nm) | 365 | 380 | 405 | 420 | 435 | 450 | 475 | 500 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H2 evolution (μmol) | 6.3127 | 5.3863 | 2.8891 | 2.1345 | 0.4584 | 0.2695 | 0 | 0 |
| O2 evolution (μmol) | 1.5782 | 1.4879 | 0.7408 | 0.5431 | 0.1161 | 0.0842 | 0 | 0 |
| Light intensity (mW cm-2) | 10.06 | 11.64 | 101.3 | 102.9 | 97.6 | 105.1 | 78.6 | 96.9 |
| Irradiation area (cm2) | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| Irradiation time (h) | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| AQY (%) | 0.5718 | 0.3538 | 0.023 | 0.0164 | 0.0036 | 0.0019 | 0 | 0 |

Supplementary Table 2. Wavelength-dependent water splitting performances and AQYs on the CN catalyst.

| Wavelength (nm) | 365 | 380 | 405 | 420 | 435 | 450 | 475 | 500 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H2 evolution (μmol) | 1.6081 | 1.0457 | 0.1352 | 0.0678 | 0 | 0 | 0 | 0 |
| O2 evolution (μmol) | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Light intensity (mW cm-2) | 11.45 | 12.75 | 102.4 | 103.5 | 96.8 | 113.1 | 77.3 | 97.4 |
| Irradiation area (cm2) | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| Irradiation time (h) | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 |
| AQY (%) | 0.1280 | 0.0718 | 0.0011 | 0.0005 | 0 | 0 | 0 | 0 |

Reaction conditions: 30 mg catalysts, 100 ml deionized water, using 3wt% Pt as co-catalysts without any sacrificial agents. All reactions were carried out at 279 K in low vacuum.

Take λ=420 nm of the F0.1-CN as example:

The number of incident photons:

N=Eλhc= 102.9×4×10-3×5×3600×420×10-96.626×10-34×3×108=1.5654×1022

AQY:

AQY=2×the number of evolved H2 moleculesN×100%

=2×6.02×1023×2.1345×10-61.5654×1022×100%=0.0164 %