Table 9 Identification of glaze colourants and a characterization of their deterioration

| Object after restoration | Inv. No. | Glaze colour | Colouring/ opacifying agent | Identified defect | Corrosion product | Ceramic body colour |
| --- | --- | --- | --- | --- | --- | --- |
|  | 1 |  | Fe2O3, Sb2O3, CuO / ZnO | unidentified | unidentified |  |
|  | 2 |  | CuO, Fe2O3, Sb2O3 / TiO2 | delayed crazing | Calcium Lead Phosphate Hydroxide Ca5.5Pb4.5 (PO4)6 (OH)2 |  |
|  | 3 |  | CuO, Fe2O3, Sb2O3, SnO2 | delayed crazing | Lead Sulphate Pb(SO4) |  |
|  | 4 |  | Fe2O3, Sb2O3, CuO / CaO | unidentified | unidentified |  |
|  | 5 |  | Fe2O3, Sb2O3, CuO / ZnO | unidentified | unidentified |  |
|  | 6 |  | Fe2O3, Sb2O3, CuO / ZnO | unidentified | unidentified |  |
|  | 7 |  | CuO, Fe2O3, Sb2O3 | corrosion crust | Calcium Lead Phosphate Chloride Ca2Pb3(PO4)3Cl Calcium Phosphate Hydroxide Hydrate CaPO3(OH)·2H2O |  |
|  | 8 |  | Fe2O3, Sb2O3, CuO/ ZnO | instant crazing | unidentified |  |
|  | 9 |  | Fe2O3, Sb2O3, CuO | corrosion crust | Calcium Lead Phosphate Chloride Ca2Pb3 (PO4)3Cl Calcium Sulphate CaSO4 |  |
|  | 10 |  | CuO, Fe2O3 | unidentified | unidentified |  |
|  | 11 |  | Fe2O3, CuO | unidentified | unidentified |  |
|  | 12 |  | CuO, Fe2O3, Sb2O3 / SnO2 | unidentified | unidentified |  |
|  | 13 |  | CuO, Fe2O3 | unidentified | unidentified |  |
|  | 14 |  | Fe2O3 / ZnO | unidentified | unidentified |  |
|  | 15 |  | Fe2O3, CuO | unidentified | unidentified |  |
|  | 16 |  | Fe2O3, Sb2O3 / ZnO | unidentified | unidentified |  |
|  | 17 |  | Fe2O3, CuO / TiO2 | corrosion crust | noncrystalline |  |
|  | 18 |  | Fe2O3, transparent | unidentified | unidentified |  |
|  | 19 |  | Fe2O3, CuO / CaO, TiO2 | corrosion crust | Calcium Phosphate Hydroxide Ca5(PO4)3(OH) |  |
|  | 20 |  | Fe2O3, MnO / CaO, TiO2 | unidentified | unidentified |  |
|  | 21 |  | CuO, Fe2O3 | corrosion crust | noncrystalline |  |
|  | 22 |  | Fe2O3, CuO | delayed crazing | unidentified |  |
|  | 23 |  | Fe2O3, Sb2O3,CuO / ZnO Brown: Fe2O3, MnO / ZnO | peeling | unidentified |  |
|  | 24 |  | Fe2O3, Sb2O3, CuO / TiO2 | crazing | noncrystalline |  |
|  | 25 |  | Fe2O3 / TiO2 | peeling | unidentified |  |
|  | 26 |  | Fe2O3 | delayed crazing | unidentified |  |
|  | 27 |  | Fe2O3 / TiO2, ZnO | unidentified | unidentified |  |
|  | 28 |  | CuO, Fe2O3 / TiO2 | unidentified | unidentified |  |
|  | 29 |  | Fe2O3, CuO, Sb2O3 | peeling | unidentified |  |
|  | 30 |  | Fe2O3, CuO, MnO / SnO2 | corrosion crust | Lead Sulphide PbS Lead Sulphate Pb(SO4) |  |
|  | 31 |  | Fe2O3 / ZnO | corrosion crust | Calcium Sulfate Hydrate CaSO4·2H2O |  |
|  | 32 |  | Fe2O3, CuO / TiO2 | unidentified | unidentified |  |
|  | 33 |  | CuO, Fe2O3 / ZnO | corrosion crust | Calcium Sulphate Hydrate CaSO4·2H2O |  |
|  | 34 |  | CuO, Fe2O3 / SnO2 | corrosion crust | Lead Sulphate Pb(SO4) |  |
|  | 35 |  | CuO, Fe2O3 / SnO2 | corrosion crust | Lead Sulphide PbS Lead Sulphate Pb(SO4) |  |
|  | 36 |  | Fe2O3, MnO, Sb2O3 / ZnO | unidentified | unidentified |  |
|  | 37 |  | Fe2O3, Sb2O3, CuO / TiO2 | unidentified | unidentified |  |
|  | 38 |  | Fe2O3,CuO / TiO2 | specking | unidentified |  |
|  | 39 |  | CuO, Fe2O3 / TiO2 | crazing | unidentified |  |
|  | 40 |  | Sb2O3, Fe2O3 | crazing | unidentified |  |