# Supplementary Information

The Cellulose Regeneration in Imidazolium-based Ionic Liquids and Anti-solvents Mixtures: A DFT study

Lanlan Fua, Zhaoyang Jua,b,c*, Mengting Yua, Huaying Luoc, Cheng Zhangc, and Ximing Zhangb, Haixiang Chenga, Minjia Zhenga, Chengsheng Gea*

aCollege of Chemical & Material Engineering, Quzhou University, Quzhou, China

bCollege of Biosystems Engineering and Food Science, Zhejiang University, Hangzhou, China

cXianhe Co., Ltd, Quzhou, China.

Contents

- Table S 1: The binding energies (ΔEb) corrected by BSSE(ΔEBSSE) of BmimOAc-nH2O (n=0-6).

- Figure S 1-2: The optimized configurations of Cellobiose-OAc and Cellobiose-Bmim at different positions.

- Table S 2-3: H-bonds and interaction energies between cellulose and OAc/Bmim.

- Table S 4-6: The optimized coordinates of DFT calculated BmimOAc-nH2O, Cellobiose-Bmim-nH2O, and Cellobiose-Bmim-nH2O (n=0-6) clusters.

Table S 1 The binding energies (ΔEb) corrected by BSSE(ΔEBSSE) of BmimOAc-nH2O (n=0-6).

| Structures | ΔE (kcal/mol) | ΔEBSSE (a.u.) | ΔEb (kcal/mol) |
| --- | --- | --- | --- |
| CIP | -115.42 | 0.0163 | -105.18 |
| CIP+1W | -133.50 | 0.0099 | -127.29 |
| CIP+2W | -148.31 | 0.0183 | -136.85 |
| CIP+3W | -170.93 | 0.0340 | -149.58 |
| CIP+4W | -192.24 | 0.0410 | -166.48 |
| SIP+4W | -189.73 | 0.0379 | -165.94 |
| CIP+5W | -208.22 | 0.0474 | -178.50 |
| SIP+5W | -210.29 | 0.0415 | -184.25 |
| SIP+6W | -226.82 | 0.0469 | -197.39 |

Figure S 1 The optimized configurations of Cellobiose-OAc-n (n=1-7) at M062X-D3/def2SVP level. The H-bonds are indicated by dashed lines.

Table S 2 H-bonds and interaction energies between cellulose and OAc at different positions.

| Structures | H-bonding | Length [Å] | Angle [°] | ΔE (kcal/mol) | ΔΔE (kcal/mol) |
| --- | --- | --- | --- | --- | --- |
| Cel-OAc1 | O52…H15-O14 | 1.48545 | 176.28847 | -61.89 | 0.00 |
|  | O51…H13-O12 | 1.61656 | 164.60949 |  |  |
| Cel-OAc2 | O52…H13-O12 | 1.47906 | 178.06949 | -57.45 | 4.44 |
|  | O51…H20-O11 | 1.58623 | 169.09267 |  |  |
| Cel-OAc3 | O52…H20-O11 | 1.40246 | 166.14563 | -46.35 | 15.54 |
|  | O51…H19-C18 | 2.12933 | 147.67106 |  |  |
| Cel-OAc4 | O52…H22-O21 | 165.30234 | 165.30234 | -54.12 | 7.78 |
|  | O51…H35-O34 | 1.65804 | 177.25736 |  |  |
| Cel-OAc5 | O52…H22-O21 | 1.65569 | 157.77211 | -56.43 | 5.46 |
|  | O52…H35-O34 | 1.64347 | 169.73212 |  |  |
|  | O51…H37-O36 | 1.77912 | 166.55204 |  |  |
| Cel-OAc6 | O52…H37-O36 | 1.70522 | 173.80855 | -43.60 | 18.29 |
|  | O51…H39-O38 | 1.53180 | 170.50495 |  |  |
| Cel-OAc7 | O52…H44-O43 | 1.72377 | 158.04664 | -46.90 | 14.98 |
|  | O51…H15-O14 | 1.56163 | 168.43240 |  |  |

Figure S 2 The optimized configurations of Cellobiose-Bmim-n (n=1-7) at M062X-D3/def2SVP level. The H-bonds are indicated by dashed lines

Table S 3 H-bonds and interaction energies between cellulose and Bmim at different positions.

| Structures | H-bonding | Length [Å] | Angle [°] | ΔE (kcal/mol) | ΔΔE (kcal/mol) |
| --- | --- | --- | --- | --- | --- |
| Cel-Bmim1 | O14…H51-C48 | 2.10926 | 136.12038 | -26.62 | 4.18 |
|  | O12…H51-C48 | 2.33744 | 118.14374 |  |  |
| Cel-Bmim2 | O12…H51-C48 | 2.03504 | 148.39245 | -23.97 | 6.84 |
|  | O11…H51-C48 | 2.51739 | 98.11835 |  |  |
| Cel-Bmim3 | O11…H51-C48 | 2.08153 | 159.23658 | -27.62 | 3.19 |
|  | O21…H51-C48 | 2.86760 | 81.48962 |  |  |
| Cel-Bmim4 | O34…H51-C48 | 2.27202 | 141.87674 | -30.80 | 0.00 |
|  | O36…H51-C48 | 2.10432 | 125.01150 |  |  |
| Cel-Bmim5 | O36…H51-C48 | 2.09782 | 132.32727 | -26.37 | 4.43 |
|  | O38…H51-C48 | 2.46075 | 108.81000 |  |  |
| Cel-Bmim6 | O40…H51-C48 | 2.18102 | 141.74718 | -22.87 | 7.93 |
|  | O38…H51-C48 | 2.74777 | 93.04368 |  |  |
| Cel-Bmim7 | O43…H51-C48 | 2.20840 | 119.88861 | -28.70 | 2.10 |
|  | O43…H56-C54 | 2.47175 | 117.83839 |  |  |

Table S 4 The optimized geometries of DFT calculated BmimOAc-nH2O (n=0-6) clusters.

| CIP C -1.370822 -2.416160 -0.041468 C -2.572901 -1.956009 0.408283 C -1.404918 -0.221974 -0.343161 H -0.960745 -3.420972 -0.070498 H -3.417190 -2.478660 0.846386 H -1.136098 0.895350 -0.529005 N -0.670573 -1.323117 -0.504910 N -2.563726 -0.591208 0.211578 C 0.720428 -1.308820 -0.970314 H 0.845869 -2.136391 -1.684108 H 0.861935 -0.346405 -1.475008 C 1.701949 -1.388766 0.190556 H 1.384552 -0.644900 0.936056 H 1.673599 -2.390909 0.654774 C -3.602953 0.370395 0.553877 H -3.914517 0.222243 1.594894 H -3.166684 1.371320 0.435410 H -4.466476 0.254717 -0.113117 C 0.846878 3.846138 0.260991 H 1.869019 3.764689 0.647782 H 0.844586 4.488329 -0.632068 H 0.185094 4.316276 1.000331 C 0.302321 2.473244 -0.124530 O 1.087457 1.511258 -0.194232 O -0.940090 2.416680 -0.370085 C 3.114020 -1.037208 -0.263869 H 3.413596 -1.686904 -1.104657 H 3.079693 -0.002398 -0.638090 C 4.130646 -1.146429 0.865328 H 5.137197 -0.863022 0.528031 H 3.855469 -0.479533 1.695667 H 4.184386 -2.172513 1.260923 | CIP+1W C -0.247661 -2.871708 -0.051820 C 1.044600 -3.033753 -0.452972 C 0.845153 -1.003596 0.408306 H -1.099633 -3.542369 -0.103616 H 1.545906 -3.874615 -0.921556 H 1.080229 0.057687 0.738130 N -0.342180 -1.607492 0.483711 N 1.701808 -1.859074 -0.158992 C -1.573127 -0.956836 0.946986 H -2.065871 -1.639154 1.655503 H -1.261518 -0.038207 1.457065 C -2.477129 -0.580131 -0.217648 H -1.861370 -0.032819 -0.945973 H -2.880343 -1.486617 -0.703696 C 3.112530 -1.581127 -0.415157 H 3.360821 -1.924860 -1.426306 H 3.294081 -0.496286 -0.352032 H 3.732834 -2.114221 0.316835 C 0.780616 3.556569 -0.385653 H -0.047315 3.889745 -1.020925 H 0.966170 4.302201 0.401040 H 1.707408 3.457459 -0.968811 C 0.462081 2.216469 0.265371 O -0.667550 1.726764 0.158135 O 1.429922 1.663888 0.890172 O 3.680245 1.563150 -0.450621 H 4.396160 1.964289 0.052025 H 2.874385 1.711969 0.112665 C -3.608860 0.334015 0.238788 H -3.144849 1.235553 0.667671 H -4.188341 -0.154972 1.040979 C -4.532107 0.725716 -0.907760 H -5.004754 -0.158257 -1.363098 H -5.332209 1.397433 -0.567627 H -3.966693 1.247869 -1.693439 |
| --- | --- |
| CIP+2W C 1.274216 -2.427423 -1.030992 C 0.212827 -3.217408 -0.702330 C -0.379814 -1.107159 -0.406205 H 2.270554 -2.680879 -1.379311 H 0.094649 -4.296022 -0.712079 H -1.006323 -0.220303 -0.152534 N 0.880842 -1.122874 -0.844803 N -0.801943 -2.371700 -0.316369 C 1.736828 0.063046 -1.029422 H 2.540059 -0.245321 -1.713882 H 1.138769 0.848772 -1.498914 C 2.292585 0.581979 0.286471 H 2.847758 1.499107 0.036990 H 1.439621 0.909128 0.903642 C -2.140954 -2.775525 0.103441 H -2.055509 -3.496633 0.925584 H -2.713597 -1.898114 0.439574 H -2.663539 -3.242261 -0.740778 C -2.408515 3.320377 0.178343 H -1.721745 4.173202 0.139170 H -3.140336 3.404449 -0.638312 H -2.971362 3.322868 1.120730 C -1.661421 2.001926 0.027511 O -0.475009 2.014319 -0.363367 O -2.294699 0.946471 0.288460 O 1.768629 3.153907 -1.328088 H 1.467927 3.554420 -2.149658 H 0.931382 2.907593 -0.881104 O -4.302156 -0.615707 1.072632 H -3.734076 0.093097 0.701062 H -4.169409 -0.502444 2.019938 C 3.171065 -0.408621 1.041360 H 2.589145 -1.313005 1.292956 H 3.994459 -0.743688 0.385692 C 3.746559 0.191411 2.319361 H 4.378417 -0.527539 2.858954 H 4.356441 1.078035 2.092093 H 2.940039 0.510015 2.996063 | CIP+3W C 0.865347 2.821872 0.194837 C -0.321579 3.379814 -0.173830 C -0.661096 1.235908 0.222615 H 1.853307 3.258197 0.298644 H -0.576984 4.396933 -0.452008 H -1.153516 0.266884 0.362517 N 0.623978 1.490340 0.438491 N -1.258272 2.368373 -0.151581 C 1.615486 0.478106 0.809176 H 1.983801 0.721885 1.816673 H 1.069358 -0.471366 0.871631 C 2.734598 0.380876 -0.216148 H 2.269835 0.263984 -1.207016 H 3.336819 1.306478 -0.227277 C -2.676334 2.496095 -0.464390 H -2.799013 3.293457 -1.205993 H -3.015922 1.544735 -0.893257 H -3.243213 2.743497 0.442031 C -1.806917 -3.520916 -0.378305 H -1.097125 -4.350793 -0.296286 H -2.815148 -3.831936 -0.076745 H -1.854738 -3.192621 -1.429249 C -1.349120 -2.325956 0.446011 O -0.162181 -2.276311 0.815734 O -2.206682 -1.405808 0.630630 O 0.194640 -0.761163 -1.705860 H 0.286630 -1.438391 -1.019260 H -0.763456 -0.698108 -1.863174 O -0.691381 -0.259431 2.753627 H -1.561804 -0.443275 2.368327 H -0.215039 -1.024419 2.390841 O -2.665045 -0.442373 -1.713474 H -2.703748 -0.878895 -0.815313 H -3.304159 -0.903310 -2.266241 C 3.637284 -0.815006 0.075692 H 4.062951 -0.719435 1.088856 H 3.017438 -1.726596 0.088287 C 4.757319 -0.960729 -0.946713 H 5.402779 -0.069220 -0.956946 H 5.390391 -1.831392 -0.727454 H 4.345878 -1.086973 -1.958884 |
| CIP+4W C -1.649552 -2.402936 -1.028808 C -2.938421 -2.035985 -0.778055 C -1.624008 -0.363453 -0.201286 H -1.236946 -3.320935 -1.434593 H -3.873385 -2.567606 -0.920855 H -1.267692 0.603918 0.164505 N -0.855411 -1.343679 -0.661015 N -2.895755 -0.761015 -0.257207 C 0.603328 -1.267418 -0.728991 H 0.902631 -1.327186 -1.784199 H 0.861586 -0.263875 -0.380303 C 1.284049 -2.310940 0.142052 H 0.771360 -2.328171 1.115571 H 1.200292 -3.315758 -0.308033 C -4.038420 0.044654 0.162473 H -4.801800 -0.623692 0.576727 H -3.681714 0.736620 0.938798 H -4.448454 0.589510 -0.697203 C 1.538745 3.742450 -0.360750 H 1.911272 3.409186 -1.341929 H 0.849572 4.581583 -0.501637 H 2.404159 4.037665 0.245995 C 0.829313 2.556712 0.271946 O 1.568709 1.626720 0.717370 O -0.416144 2.524522 0.251900 O -2.158826 1.490173 2.180334 H -1.436707 0.866682 2.379497 H -1.686590 2.139176 1.631485 O 0.175500 -0.101986 2.119366 H 0.678230 -0.256165 2.926140 H 0.721088 0.568355 1.610252 O 2.640149 0.846364 -1.633775 H 2.494401 1.104533 -0.696192 H 3.453624 1.285733 -1.900215 O -0.147053 1.159869 -2.319020 H -0.413934 1.820897 -1.664372 H 0.821705 1.128920 -2.244395 C 2.751029 -1.946117 0.353910 H 3.233751 -1.769155 -0.620694 H 2.781074 -0.978227 0.881826 C 3.511145 -3.002460 1.144994 H 3.523400 -3.965251 0.611831 H 4.553890 -2.703251 1.319506 H 3.041407 -3.172971 2.125739 | CIP+5W C -0.722040 -2.883662 -0.996435 C -2.058134 -2.933780 -0.731881 C -1.337099 -0.913638 -0.230647 H -0.043632 -3.636245 -1.384120 H -2.778163 -3.737561 -0.843693 H -1.317255 0.123448 0.103940 N -0.299816 -1.617392 -0.671786 N -2.417966 -1.695723 -0.249542 C 1.070815 -1.112493 -0.753334 H 1.346236 -1.026390 -1.812958 H 1.040251 -0.098488 -0.346893 C 2.045897 -1.963828 0.045335 H 1.568096 -2.226128 1.001366 H 2.277375 -2.902146 -0.488295 C -3.755428 -1.303130 0.188874 H -4.368671 -2.208121 0.253102 H -3.667778 -0.828351 1.174089 H -4.178383 -0.583432 -0.520131 C 0.827213 3.856785 -0.452348 H 0.665527 3.631803 -1.517574 H 0.172984 4.696479 -0.187686 H 1.877911 4.121615 -0.286495 C 0.429608 2.624721 0.344612 O 1.347931 1.881936 0.787721 O -0.793019 2.382438 0.458135 O -2.163038 0.759765 2.236349 H -1.400525 0.184247 2.426128 H -1.694847 1.512293 1.825069 O 0.437778 -0.230601 2.122620 H 1.000260 -0.321057 2.899335 H 0.773535 0.592017 1.666982 O 2.519787 1.416373 -1.612580 H 2.371371 1.608381 -0.661619 H 3.077373 2.132150 -1.934017 O -0.282133 1.086520 -2.230229 H -0.736766 1.579068 -1.534791 H 0.662061 1.284686 -2.107633 O -3.292572 1.537717 -0.289871 H -3.249868 1.260270 0.638149 H -2.590973 2.205480 -0.311778 C 3.330164 -1.185960 0.320713 H 3.728333 -0.783829 -0.624553 H 3.061009 -0.305695 0.928612 C 4.380994 -2.022273 1.038203 H 4.687066 -2.885061 0.427108 H 5.281454 -1.433654 1.261622 H 3.990674 -2.413610 1.990299 |
| CIP+6W C -2.318440 2.293480 -0.791788 C -1.629870 3.280647 -0.155001 C -0.686639 1.358688 0.345047 H -3.175737 2.335436 -1.455500 H -1.748591 4.358537 -0.172796 H -0.033990 0.608090 0.780154 N -1.712274 1.104423 -0.458989 N -0.633159 2.668767 0.565916 C -2.142462 -0.233344 -0.866117 H -2.351747 -0.193301 -1.944985 H -1.286530 -0.899108 -0.715365 C -3.339106 -0.723150 -0.064474 H -3.081299 -0.643138 1.002045 H -4.220292 -0.087110 -0.257885 C 0.444978 3.338824 1.273779 H 0.039136 4.203189 1.811400 H 0.879937 2.626588 1.984422 H 1.208731 3.648940 0.549788 C 3.578164 -2.728970 -1.043740 H 2.857432 -2.612922 -1.868203 H 4.591489 -2.726383 -1.458175 H 3.370295 -3.677122 -0.530578 C 3.387505 -1.552642 -0.103254 O 2.335191 -1.610204 0.639968 O 4.176632 -0.613100 -0.121096 O 2.567750 1.510914 0.032456 H 2.265385 1.262346 0.923715 H 3.345075 0.915732 -0.081764 O 1.579979 0.176600 2.262571 H 1.968756 -0.549784 1.651144 H 2.102925 0.136654 3.070741 O 0.231143 -2.685599 -0.274411 H 1.117064 -2.421937 0.134407 H 0.306434 -3.608619 -0.537082 O 0.908245 -0.219896 -1.622732 H 1.534138 0.176642 -0.992600 H 0.744363 -1.121019 -1.304940 O 0.808316 2.591029 -1.897684 H 0.561154 1.713604 -2.223924 H 1.575979 2.369916 -1.344299 O -0.912181 -1.219685 1.831650 H -0.104409 -0.880470 2.247914 H -0.602579 -1.910057 1.220822 C -3.653650 -2.178407 -0.397375 H -3.875296 -2.274702 -1.473830 H -2.746168 -2.776940 -0.213866 C -4.813827 -2.726682 0.423856 H -5.733589 -2.150012 0.243662 H -5.022072 -3.776734 0.176927 H -4.588481 -2.669797 1.498791 |  |

Table S 5 The optimized geometries of DFT calculated Cellobiose-OAc-nH2O (n=0-6) clusters.

| Cellobiose-OAc C -2.849134 1.927018 0.219173 C -1.623907 2.385237 -0.561826 C -0.386449 0.493896 0.256260 C -1.558373 -0.016986 1.091032 C -2.836461 0.412657 0.371382 H -1.701239 1.983871 -1.590767 H -2.804289 2.388602 1.225500 H -0.430176 0.000525 -0.737821 H -1.510811 0.477899 2.078168 H -2.796988 -0.017896 -0.650876 O -4.004621 2.324910 -0.467178 O -4.014047 0.022689 0.997767 H -4.228713 -0.876289 0.612914 O -1.453191 -1.390525 1.264432 H -1.815647 -1.872133 0.428278 O 0.801683 0.204374 0.887802 O -0.443203 1.905480 0.070135 C -1.483259 3.896990 -0.607989 H -2.423549 4.319036 -0.989187 H -4.683551 1.710401 -0.145037 O -1.247192 4.421880 0.670802 H -0.596664 3.835931 1.080736 H -0.668139 4.158174 -1.310431 C 1.901463 -0.178341 0.096860 C 2.575307 -1.371802 0.765033 C 4.643870 -0.725913 -0.098572 C 4.106122 0.511868 -0.806460 C 2.850446 1.001973 -0.108694 H 2.905148 -1.080105 1.782046 H 1.553688 -0.503482 -0.901866 H 4.944755 -0.433888 0.933455 H 3.828793 0.203916 -1.833467 H 3.143616 1.380297 0.892650 O 2.254750 2.002366 -0.881381 H 1.379790 2.192817 -0.504121 O 5.083946 1.516400 -0.809413 H 5.872748 1.117766 -1.196904 O 5.739190 -1.169674 -0.827949 H 6.078051 -1.960179 -0.392466 O 3.693608 -1.745636 -0.024223 C 1.642752 -2.575812 0.928911 H 2.298148 -3.462732 0.973526 O 0.884767 -2.504222 2.088472 H 0.042807 -2.041720 1.878315 H 1.015364 -2.678137 0.021884 C -3.883575 -3.741098 -2.048255 H -4.963418 -3.728273 -2.235248 H -3.325511 -3.539322 -2.972560 H -3.578972 -4.737449 -1.696146 C -3.500340 -2.709449 -0.986468 O -4.423210 -2.144776 -0.370124 O -2.263232 -2.530647 -0.825753 | Cellobiose-OAc-H2O C 2.519296 2.486948 -0.073437 C 1.225039 2.763020 0.681341 C 0.269819 0.752104 -0.196560 C 1.510381 0.415299 -1.018333 C 2.712715 0.990131 -0.269963 H 1.322470 2.342050 1.700772 H 2.438700 2.966215 -1.069212 H 0.367132 0.264033 0.797227 H 1.413909 0.914917 -1.999039 H 2.726813 0.518763 0.735335 O 3.594272 3.013785 0.655314 O 3.935240 0.793750 -0.901946 H 4.262792 -0.105389 -0.616427 O 1.591029 -0.958368 -1.211415 H 2.038861 -1.386201 -0.397952 O -0.857398 0.302978 -0.846345 O 0.135178 2.154376 -0.001589 C 0.893896 4.242408 0.765338 H 1.759583 4.764606 1.195996 H 4.362421 2.525639 0.318988 O 0.641140 4.778946 -0.505354 H 0.067149 4.144786 -0.954973 H 0.027593 4.374639 1.441823 C -1.956907 -0.102959 -0.060793 C -2.378662 -1.496600 -0.514700 C -4.599572 -1.037812 0.033993 C -4.320160 0.378938 0.519872 C -3.079878 0.926971 -0.162249 H -2.633576 -1.465652 -1.592647 H -1.659869 -0.166709 1.002971 H -4.821399 -0.997455 -1.056750 H -4.111892 0.312736 1.605654 H -3.315452 1.065458 -1.237931 O -2.716388 2.133585 0.441780 H -1.798818 2.330098 0.192632 O -5.423429 1.200031 0.250194 H -6.186782 0.757368 0.640927 O -5.693260 -1.506350 0.748122 H -5.869192 -2.408105 0.455843 O -3.510571 -1.887044 0.244730 C -1.273042 -2.540641 -0.340204 H -1.770296 -3.505129 -0.156283 O -0.468748 -2.670362 -1.473366 H 0.194450 -1.941588 -1.485747 H -0.679221 -2.316715 0.566252 C 4.380060 -3.614623 1.195053 H 5.434114 -3.778003 0.944854 H 4.247021 -3.617972 2.286609 H 3.743152 -4.413579 0.788349 C 3.883593 -2.286875 0.640039 O 4.687033 -1.518682 0.093224 O 2.637264 -2.073137 0.785268 O 1.118558 -4.365929 0.295659 H 0.756095 -4.024549 -0.535132 H 1.605424 -3.592760 0.637285 |
| --- | --- |
| Cellobiose-OAc-2H2O C 2.416035 2.509333 -0.248453 C 1.138708 2.737485 0.551178 C 0.180882 0.748908 -0.337916 C 1.396768 0.430743 -1.201678 C 2.618533 1.024138 -0.505096 H 1.254207 2.253242 1.538393 H 2.311121 3.033318 -1.218963 H 0.317215 0.275546 0.655389 H 1.257008 0.907544 -2.187390 H 2.681355 0.538584 0.484947 O 3.506257 3.009028 0.481398 O 3.817050 0.856911 -1.196686 H 4.165727 -0.026749 -0.923018 O 1.499882 -0.949736 -1.382512 H 1.929256 -1.350130 -0.568085 O -0.959453 0.286280 -0.958691 O 0.043959 2.152347 -0.147706 C 0.798113 4.207092 0.712406 H 1.665367 4.717286 1.154162 H 4.274007 2.567806 0.086627 O 0.520705 4.802903 -0.527735 H -0.060257 4.188307 -0.995107 H -0.058471 4.298010 1.407327 C -2.036624 -0.106094 -0.134803 C -2.468064 -1.506976 -0.556889 C -4.674451 -1.047420 0.040174 C -4.386352 0.376770 0.497493 C -3.165640 0.918511 -0.224927 H -2.750932 -1.491548 -1.628401 H -1.708930 -0.151270 0.920658 H -4.922684 -1.023462 -1.045387 H -4.149710 0.328754 1.578233 H -3.429218 1.036653 -1.296865 O -2.794362 2.137252 0.347703 H -1.874943 2.321528 0.094950 O -5.499080 1.190300 0.242776 H -6.248587 0.758518 0.670555 O -5.748872 -1.509466 0.786931 H -5.927006 -2.416402 0.512713 O -3.577993 -1.891391 0.235815 C -1.355553 -2.544799 -0.396923 H -1.842856 -3.510461 -0.195310 O -0.575556 -2.683289 -1.548136 H 0.062076 -1.936924 -1.601145 H -0.743177 -2.307960 0.493921 C 4.315580 -3.607660 0.915704 H 5.349299 -3.776465 0.594905 H 4.243104 -3.665951 2.011387 H 3.638733 -4.371278 0.505367 C 3.817321 -2.247613 0.456725 O 4.580912 -1.474945 -0.126904 O 2.582488 -2.007666 0.713788 O 1.103703 -4.342172 0.127087 H 0.688392 -3.986285 -0.672957 H 1.549117 -3.559767 0.497123 O 1.768493 -0.139267 2.585738 H 2.580455 0.373414 2.666516 H 2.033739 -0.875064 1.994544 | Cellobiose-OAc-3H2O C 2.328699 2.355585 -0.496801 C 1.117319 2.641356 0.382351 C 0.024031 0.699360 -0.468153 C 1.177969 0.328923 -1.394949 C 2.448816 0.860498 -0.742673 H 1.258107 2.142908 1.359165 H 2.184111 2.883404 -1.458402 H 0.191635 0.221354 0.516765 H 1.013502 0.813583 -2.372743 H 2.515091 0.377305 0.246419 O 3.503250 2.814987 0.138017 O 3.622373 0.627169 -1.465586 H 3.978403 -0.220179 -1.118868 O 1.214049 -1.054022 -1.585793 H 1.624629 -1.476719 -0.779494 O -1.168115 0.293883 -1.027140 O -0.034162 2.108408 -0.269542 C 0.851172 4.124033 0.560077 H 1.756553 4.595807 0.966675 H 4.217752 2.438876 -0.401105 O 0.551417 4.736038 -0.667250 H -0.091818 4.161189 -1.102544 H 0.029698 4.250217 1.290193 C -2.213997 -0.042340 -0.139030 C -2.725449 -1.431745 -0.508332 C -4.870353 -0.875735 0.212854 C -4.502161 0.546817 0.615143 C -3.305363 1.024044 -0.189209 H -3.077881 -1.421087 -1.559131 H -1.830333 -0.082072 0.897598 H -5.185768 -0.867194 -0.855446 H -4.205734 0.516731 1.681567 H -3.626763 1.129345 -1.246676 O -2.855630 2.239508 0.331493 H -1.938789 2.372155 0.041063 O -5.596267 1.396347 0.400350 H -6.332259 1.014069 0.893614 O -5.911629 -1.278623 1.036359 H -6.142435 -2.183205 0.795488 O -3.795418 -1.756797 0.361251 C -1.645925 -2.510606 -0.407137 H -2.152524 -3.454576 -0.157576 O -0.955444 -2.692670 -1.609499 H -0.296245 -1.973632 -1.717428 H -0.962359 -2.286799 0.433944 C 3.994475 -3.785671 0.699524 H 5.016576 -3.937248 0.335799 H 3.970058 -3.920349 1.790960 H 3.294313 -4.510727 0.261784 C 3.508662 -2.384070 0.377419 O 4.330869 -1.517842 0.019784 O 2.260485 -2.184998 0.510200 O 0.720581 -4.482749 -0.077521 H 0.277915 -4.091707 -0.845736 H 1.199534 -3.721971 0.294239 O 1.564333 -0.176455 2.407319 H 2.486317 0.135945 2.467916 H 1.672721 -0.976473 1.864385 O 4.247828 0.605026 1.963153 H 4.041070 1.416989 1.474951 H 4.399374 -0.066303 1.271360 |
| Cellobiose-OAc-4H2O C 2.498373 2.309068 -0.351520 C 1.238586 2.529256 0.470858 C 0.160998 0.739785 -0.629538 C 1.319327 0.411433 -1.562943 C 2.607883 0.887968 -0.888543 H 1.273930 1.913794 1.388100 H 2.462209 3.003534 -1.210868 H 0.312692 0.198639 0.321750 H 1.175619 0.935796 -2.521715 H 2.757295 0.225252 -0.013127 O 3.634287 2.575309 0.447214 O 3.736541 0.882926 -1.713880 H 4.040415 -0.056550 -1.792028 O 1.341300 -0.973431 -1.809612 H 1.454403 -1.442974 -0.925393 O -1.040934 0.393900 -1.203301 O 0.134834 2.129530 -0.330789 C 1.008306 3.986716 0.825178 H 1.886305 4.358778 1.371267 H 4.379643 2.265166 -0.091095 O 0.845153 4.773768 -0.325240 H 0.197402 4.316781 -0.877304 H 0.126704 4.047747 1.490371 C -2.101622 0.114601 -0.302419 C -2.718264 -1.218150 -0.718574 C -4.807126 -0.561752 0.074275 C -4.334813 0.817782 0.511018 C -3.126776 1.248303 -0.304588 H -3.089448 -1.132732 -1.759878 H -1.699468 0.013185 0.723799 H -5.155179 -0.494917 -0.982005 H -4.016500 0.734703 1.568075 H -3.460078 1.397521 -1.353451 O -2.612740 2.427468 0.237805 H -1.682154 2.499142 -0.027836 O -5.375861 1.743072 0.348999 H -6.122971 1.393387 0.849613 O -5.846489 -0.925322 0.918268 H -6.139883 -1.806636 0.659982 O -3.789528 -1.515655 0.156589 C -1.715155 -2.367012 -0.687344 H -2.276247 -3.293860 -0.501960 O -1.031868 -2.516421 -1.903074 H -0.345840 -1.826788 -1.979389 H -1.017638 -2.244548 0.161264 C 2.232993 -3.260472 2.441901 H 3.181154 -3.571424 2.893111 H 1.669099 -2.638854 3.154488 H 1.611320 -4.130087 2.188911 C 2.475630 -2.422382 1.200673 O 3.611145 -1.956192 0.988019 O 1.458384 -2.207364 0.468877 O 0.214044 -4.630412 -0.454880 H -0.155701 -4.233411 -1.256191 H 0.645251 -3.856219 -0.058860 O 0.410716 -0.410027 2.525730 H 1.323523 -0.065729 2.563609 H 0.479049 -1.127535 1.878643 O 3.136305 0.438083 2.408191 H 3.424394 1.203606 1.884147 H 3.540866 -0.331987 1.968225 O 4.119705 -1.716699 -1.689818 H 3.211809 -1.802148 -2.019030 H 4.018032 -1.841768 -0.718612 | Cellobiose-OAc-5H2O C 2.136658 2.625970 -0.421010 C 0.807589 2.837843 0.290359 C -0.030266 0.826397 -0.619937 C 1.202037 0.520074 -1.459860 C 2.400753 1.164335 -0.766454 H 0.842142 2.363327 1.287362 H 2.108490 3.204310 -1.363123 H 0.124107 0.416429 0.393701 H 1.070849 0.940714 -2.469828 H 2.523626 0.624294 0.195317 O 3.184235 3.085299 0.408167 O 3.581642 1.137586 -1.501600 H 4.036823 0.266236 -1.302830 O 1.358876 -0.872703 -1.575478 H 1.605897 -1.235190 -0.677063 O -1.161268 0.287765 -1.192029 O -0.209923 2.230553 -0.496661 C 0.430559 4.302523 0.417340 H 1.243843 4.831210 0.933642 H 3.987795 2.761504 -0.030392 O 0.253259 4.894937 -0.842339 H -0.306111 4.290647 -1.347633 H -0.484706 4.374871 1.034579 C -2.211104 -0.049852 -0.298458 C -2.669082 -1.462553 -0.647180 C -4.837421 -0.995887 0.055126 C -4.528369 0.450028 0.420270 C -3.352019 0.962125 -0.394523 H -3.017684 -1.478841 -1.699739 H -1.831069 -0.045222 0.740993 H -5.154701 -1.027520 -1.012146 H -4.231214 0.460894 1.486574 H -3.670165 1.012618 -1.457608 O -2.981780 2.218526 0.086861 H -2.072133 2.395292 -0.201995 O -5.657548 1.245812 0.182554 H -6.374413 0.852722 0.694974 O -5.857742 -1.423023 0.891287 H -6.060082 -2.338075 0.665395 O -3.724198 -1.827432 0.220339 C -1.547592 -2.491702 -0.533693 H -2.020565 -3.464661 -0.333270 O -0.813504 -2.606535 -1.724495 H -0.209743 -1.839787 -1.799025 H -0.892613 -2.252999 0.325237 C 2.068159 -2.791025 2.974970 H 2.950984 -2.975838 3.596154 H 1.321755 -2.228931 3.557278 H 1.607623 -3.733610 2.651394 C 2.426922 -1.935875 1.772181 O 3.482120 -1.279775 1.790741 O 1.569083 -1.905696 0.831493 O 1.240159 -4.195976 -0.726110 H 0.485628 -3.876586 -1.252201 H 1.306468 -3.510049 -0.035717 O 0.017709 -0.151236 2.592461 H 0.821538 0.397074 2.671221 H 0.296013 -0.855551 1.988847 O 2.542741 1.214859 2.612959 H 2.870160 1.906375 2.014840 H 3.068843 0.423846 2.389959 O 4.577148 -1.110066 -0.731009 H 4.171439 -1.866610 -1.210566 H 4.251073 -1.174201 0.189735 O 3.181525 -2.907622 -2.227816 H 2.594204 -2.162303 -2.426750 H 2.594689 -3.512984 -1.726700 |
| Cellobiose-OAc-6H2O C 2.018872 2.519855 -0.367095 C 0.624761 2.816969 0.195364 C -0.237577 0.796063 -0.620045 C 0.983219 0.442361 -1.447950 C 2.217095 1.059608 -0.786291 H 0.567954 2.415871 1.223461 H 2.158612 3.136303 -1.274333 H -0.089912 0.445689 0.418034 H 0.854870 0.858668 -2.459837 H 2.385447 0.482621 0.146008 O 2.925208 2.903936 0.644281 O 3.332956 0.991298 -1.628653 H 3.647151 0.043328 -1.631858 O 1.117945 -0.954198 -1.560036 H 1.460157 -1.317542 -0.697188 O -1.375709 0.235276 -1.156668 O -0.379768 2.207619 -0.600870 C 0.322236 4.304475 0.201532 H 1.133006 4.821160 0.733204 H 3.763762 2.392436 0.564892 O 0.257154 4.814358 -1.104230 H -0.294707 4.200532 -1.606103 H -0.624065 4.470180 0.750594 C -2.431703 -0.032713 -0.244816 C -2.931140 -1.445262 -0.532364 C -5.085877 -0.881754 0.149274 C -4.729552 0.566136 0.459945 C -3.541611 1.008708 -0.377722 H -3.272434 -1.503072 -1.586053 H -2.043600 -0.006624 0.790612 H -5.408180 -0.943388 -0.915256 H -4.427543 0.605506 1.524276 H -3.863124 1.029318 -1.440726 O -3.129301 2.269870 0.055532 H -2.235861 2.429399 -0.288944 O -5.834221 1.387902 0.197745 H -6.563020 1.030000 0.719125 O -6.115814 -1.243273 1.003899 H -6.352402 -2.157933 0.812164 O -3.999724 -1.741895 0.343801 C -1.839758 -2.496193 -0.352585 H -2.339791 -3.449394 -0.126758 O -1.078309 -2.676070 -1.517282 H -0.491792 -1.902799 -1.641562 H -1.210253 -2.233723 0.518473 C 2.324932 -2.569521 3.011428 H 3.232769 -2.555002 3.623585 H 1.514044 -2.032527 3.527004 H 1.983335 -3.599523 2.842767 C 2.558054 -1.878084 1.680718 O 3.593053 -1.196296 1.528403 O 1.643448 -2.001836 0.811252 O 0.989750 -4.302079 -0.632571 H 0.190389 -3.939876 -1.057093 H 1.185889 -3.630480 0.045476 O -0.242606 -0.526232 2.442286 H 0.460129 0.130299 2.608274 H 0.209087 -1.159271 1.861815 O 2.129225 1.048302 2.632849 H 2.403083 1.827688 2.113276 H 2.815425 0.393065 2.428429 O 4.268618 -1.380179 -1.188243 H 3.794873 -2.127694 -1.624004 H 4.058108 -1.444022 -0.238496 O 2.667653 -3.129955 -2.464628 H 2.075749 -2.373401 -2.594628 H 2.158225 -3.698571 -1.845690 O 4.997803 1.142314 0.603815 H 4.685505 0.319070 1.016315 H 4.828509 0.988928 -0.341087 |  |

Table S 6 The optimized geometries of DFT calculated Cellobiose-Bmim-nH2O (n=0-6) clusters.

| Cellobiose-Bmim C 3.570448 -2.344147 -0.560453 C 2.226755 -2.070564 -1.243907 C 2.292347 0.247662 -0.513248 C 3.635847 0.036382 0.157207 C 4.396622 -1.068621 -0.549157 H 2.412286 -1.828819 -2.306677 H 3.384113 -2.648605 0.484396 H 2.446470 0.642237 -1.538502 H 3.447266 -0.271687 1.203466 H 4.565190 -0.761585 -1.602012 O 4.306626 -3.314723 -1.257618 O 5.608197 -1.224737 0.126862 H 6.098544 -1.937382 -0.304040 O 4.321016 1.254178 0.093232 H 5.234683 1.097858 0.373120 O 1.554295 1.118259 0.250116 O 1.578498 -0.979663 -0.588903 C 1.249104 -3.226311 -1.137595 H 1.686801 -4.119505 -1.605332 H 4.125679 -4.188070 -0.893991 O 0.955847 -3.522413 0.202580 H 0.872488 -2.683187 0.675159 H 0.337115 -2.966263 -1.709324 C 0.555188 1.901986 -0.376740 C 0.619357 3.307948 0.225530 C -1.679952 3.611311 -0.060312 C -1.878576 2.237261 -0.687350 C -0.824675 1.284227 -0.163077 H 0.469974 3.226089 1.320652 H 0.754056 1.970390 -1.463032 H -1.790537 3.530233 1.044051 H -1.738020 2.362231 -1.777120 H -0.963285 1.176438 0.931687 O -0.979051 0.040430 -0.803244 H -0.135430 -0.446221 -0.754458 O -3.164504 1.737325 -0.395935 H -3.769725 2.484478 -0.515612 O -2.646708 4.427932 -0.607763 H -2.598723 5.302394 -0.201364 O -0.401703 4.092025 -0.357720 C 1.967226 4.000744 0.015944 H 1.776516 5.079286 0.118122 O 2.908659 3.628069 0.968676 H 3.313946 2.785071 0.717431 H 2.311803 3.830038 -1.022432 C -4.526182 -2.975992 0.610461 C -5.554590 -2.384206 -0.063062 C -3.714912 -1.244659 -0.484676 H -4.509482 -3.846206 1.259768 H -6.608723 -2.638612 -0.118152 H -3.016243 -0.485323 -0.843069 N -3.392079 -2.250554 0.326016 N -5.021527 -1.304726 -0.733893 C -2.053450 -2.418776 0.906320 H -1.970565 -3.453682 1.262643 H -1.330007 -2.292017 0.092545 C -1.806217 -1.393749 2.009173 H -2.174996 -0.415840 1.656228 H -2.401349 -1.654976 2.899380 C -5.743550 -0.362009 -1.582676 H -5.085115 0.494516 -1.764243 H -6.014387 -0.839612 -2.532007 H -6.647775 -0.027483 -1.061517 C -0.330339 -1.269524 2.374567 H 0.064663 -2.259510 2.662480 H 0.226910 -0.937192 1.480597 C -0.088323 -0.271813 3.501301 H 0.983391 -0.163357 3.712425 H -0.476329 0.723135 3.234339 H -0.588109 -0.588661 4.427783 | Cellobiose-Bmim-H2O C 3.798143 -2.248659 -0.540410 C 2.486968 -1.991277 -1.290348 C 2.446346 0.301206 -0.483947 C 3.754798 0.102510 0.255924 C 4.586151 -0.953945 -0.444106 H 2.722886 -1.713263 -2.334099 H 3.562562 -2.588528 0.483284 H 2.649373 0.736913 -1.483754 H 3.517252 -0.249471 1.278030 H 4.803052 -0.605627 -1.475028 O 4.597937 -3.179658 -1.220845 O 5.762520 -1.099758 0.293679 H 6.293976 -1.787340 -0.129125 O 4.407693 1.339706 0.275115 H 5.311560 1.194767 0.591129 O 1.640477 1.126965 0.263346 O 1.770053 -0.937988 -0.644286 C 1.544161 -3.180190 -1.269972 H 2.026284 -4.036263 -1.762570 H 4.415868 -4.067723 -0.895114 O 1.219880 -3.548610 0.044620 H 1.077687 -2.737137 0.550402 H 0.643091 -2.922872 -1.859714 C 0.665453 1.908799 -0.398540 C 0.678868 3.309053 0.219043 C -1.594365 3.602658 -0.226543 C -1.739358 2.222476 -0.854462 C -0.716965 1.267770 -0.272914 H 0.451008 3.221189 1.300024 H 0.916424 1.996712 -1.472649 H -1.784520 3.530552 0.868217 H -1.539290 2.338282 -1.934570 H -0.919340 1.135837 0.810346 O -0.811870 0.036449 -0.943888 H 0.041154 -0.430716 -0.870278 O -3.048206 1.727497 -0.649830 H -3.646627 2.432135 -0.943941 O -2.524286 4.405558 -0.851995 H -2.498391 5.291121 -0.467993 O -0.302630 4.090041 -0.433732 C 2.032809 4.012806 0.111504 H 1.826061 5.089464 0.203391 O 2.903722 3.641222 1.128887 H 3.347609 2.813399 0.892420 H 2.454450 3.849911 -0.899404 C -4.253062 -3.053566 0.578569 C -5.313585 -2.493847 -0.070091 C -3.494216 -1.428876 -0.695951 H -4.203587 -3.877363 1.283972 H -6.373288 -2.725982 -0.033263 H -2.812376 -0.693432 -1.128463 N -3.130446 -2.378780 0.161838 N -4.811505 -1.491535 -0.865277 C -1.777563 -2.506197 0.709387 H -1.615484 -3.557368 0.982543 H -1.082164 -2.267513 -0.103611 C -1.579981 -1.551244 1.882914 H -2.023060 -0.581391 1.606591 H -2.157685 -1.908942 2.751332 C -5.601902 -0.491959 -1.568876 H -4.952164 0.037986 -2.273241 H -6.415505 -0.981992 -2.115078 H -5.999240 0.211920 -0.826253 C -0.113790 -1.368234 2.257398 H 0.326086 -2.344996 2.525905 H 0.431980 -0.989967 1.375576 C 0.078942 -0.385924 3.406736 H 1.142864 -0.246232 3.638571 H -0.335484 0.601412 3.150542 H -0.425044 -0.735978 4.319035 O -4.429409 0.241618 1.298365 H -4.532887 0.599033 2.186525 H -3.865601 0.877181 0.827011 |
| --- | --- |
| Cellobiose-Bmim-2H2O C 3.519675 -2.679561 -0.566480 C 2.151295 -2.309880 -1.149803 C 2.476938 0.014549 -0.503190 C 3.832042 -0.310118 0.095928 C 4.447141 -1.480287 -0.644291 H 2.266372 -2.136629 -2.235585 H 3.393765 -2.952379 0.495390 H 2.611784 0.374031 -1.543732 H 3.678216 -0.592861 1.154885 H 4.559606 -1.201041 -1.712309 O 4.111071 -3.720225 -1.299635 O 5.690068 -1.728870 -0.059176 H 6.082054 -2.489570 -0.508271 O 4.622445 0.839512 -0.020017 H 5.538958 0.587467 0.168094 O 1.864485 0.968387 0.274818 O 1.644660 -1.137933 -0.507277 C 1.102167 -3.376977 -0.893832 H 1.419071 -4.321665 -1.357351 H 3.903988 -4.568701 -0.893460 O 0.932732 -3.591378 0.481923 H 0.926587 -2.724606 0.911664 H 0.157192 -3.068966 -1.383147 C 1.013519 1.914820 -0.337220 C 1.251479 3.269279 0.334839 C -0.949633 3.923649 -0.069771 C -1.310858 2.612663 -0.759109 C -0.452494 1.485997 -0.219402 H 1.024950 3.173428 1.415328 H 1.264884 2.010027 -1.410619 H -1.142912 3.826843 1.022403 H -1.096714 2.746998 -1.835496 H -0.677085 1.350244 0.857187 O -0.724970 0.298889 -0.929121 H 0.007006 -0.327829 -0.775316 O -2.689530 2.345766 -0.570955 H -3.150945 3.180063 -0.761480 O -1.753011 4.884842 -0.644938 H -1.586939 5.740143 -0.228366 O 0.396814 4.218259 -0.272009 C 2.694297 3.765635 0.224225 H 2.655639 4.852902 0.389178 O 3.522263 3.194966 1.183785 H 3.875705 2.359573 0.844027 H 3.058476 3.607054 -0.808799 C -4.255019 -2.792570 1.160709 C -5.340569 -2.447356 0.410561 C -3.565400 -1.531562 -0.503525 H -4.171908 -3.409353 2.050412 H -6.390755 -2.698048 0.523290 H -2.948112 -0.902037 -1.147408 N -3.159337 -2.218030 0.560353 N -4.880226 -1.672321 -0.626903 C -1.790039 -2.198015 1.070307 H -1.536355 -3.203887 1.431801 H -1.142366 -1.989262 0.209160 C -1.599707 -1.123473 2.133479 H -2.023957 -0.184337 1.742844 H -2.190750 -1.377575 3.029263 C -5.694313 -0.952155 -1.599854 H -5.024975 -0.553113 -2.371318 H -6.425586 -1.636491 -2.044419 H -6.201604 -0.127045 -1.084242 C -0.131384 -0.942253 2.503864 H 0.267116 -1.892746 2.900894 H 0.444961 -0.706169 1.592668 C 0.088423 0.167832 3.525087 H 1.155541 0.302919 3.744638 H -0.296011 1.129046 3.148751 H -0.430646 -0.050123 4.469458 O -4.309426 0.611170 1.014606 H -4.540096 1.007816 1.861421 H -3.708987 1.249723 0.596674 O -2.958670 0.478150 -2.715049 H -2.003983 0.328975 -2.727927 H -3.041066 1.166036 -2.035103 | Cellobiose-Bmim-3H2O C 3.370225 -2.785059 -0.477715 C 1.955108 -2.389707 -0.917744 C 2.423545 -0.071018 -0.398104 C 3.818691 -0.418541 0.085170 C 4.323547 -1.623432 -0.679878 H 1.935569 -2.249123 -2.013188 H 3.347625 -3.031578 0.597830 H 2.472531 0.227583 -1.465295 H 3.757520 -0.671116 1.160535 H 4.337424 -1.373099 -1.760751 O 3.854056 -3.862094 -1.239893 O 5.611676 -1.899149 -0.215024 H 5.924893 -2.691984 -0.670298 O 4.632122 0.700924 -0.133351 H 5.553180 0.417356 -0.033588 O 1.925848 0.954905 0.375522 O 1.556122 -1.183109 -0.261622 C 0.926937 -3.428545 -0.506333 H 1.205824 -4.400719 -0.937249 H 3.651511 -4.692508 -0.796371 O 0.884516 -3.562167 0.892341 H 0.913129 -2.669628 1.264230 H -0.047519 -3.133296 -0.929880 C 1.107566 1.924129 -0.238447 C 1.466381 3.302695 0.328945 C -0.703707 4.091278 -0.082586 C -1.141645 2.759593 -0.674193 C -0.376950 1.626073 -0.021552 H 1.277418 3.297747 1.420616 H 1.304013 1.940321 -1.327176 H -0.897693 4.094732 1.013134 H -0.881335 2.790287 -1.748256 H -0.570621 1.637928 1.070759 O -0.806291 0.415977 -0.578398 H -0.102382 -0.258651 -0.534475 O -2.536612 2.575124 -0.527881 H -2.952501 3.422266 -0.758259 O -1.442842 5.058655 -0.731855 H -1.226125 5.928584 -0.372989 O 0.659024 4.274465 -0.312037 C 2.932903 3.687758 0.128918 H 2.975876 4.783312 0.223939 O 3.762553 3.119338 1.087300 H 4.042187 2.244730 0.777956 H 3.237647 3.438553 -0.905429 C -4.289360 -2.370641 1.449866 C -5.344147 -2.071611 0.640302 C -3.495159 -1.564195 -0.435212 H -4.257016 -2.787201 2.451906 H -6.413403 -2.168252 0.800095 H -2.794250 -1.225822 -1.198575 N -3.149213 -2.054428 0.750467 N -4.821984 -1.579723 -0.531802 C -1.783418 -2.051806 1.274934 H -1.559414 -3.044700 1.688807 H -1.127670 -1.896936 0.408721 C -1.591479 -0.932917 2.291566 H -1.967000 -0.003581 1.834910 H -2.218635 -1.125976 3.178736 C -5.586962 -0.994707 -1.624126 H -4.876592 -0.581544 -2.347886 H -6.221561 -1.755871 -2.092992 H -6.200357 -0.180474 -1.219688 C -0.133325 -0.779125 2.710909 H 0.226103 -1.731892 3.138435 H 0.478816 -0.574075 1.817074 C 0.074756 0.339151 3.725608 H 1.136408 0.452709 3.980900 H -0.274922 1.303906 3.326085 H -0.480240 0.144081 4.654667 O -4.208370 0.797941 0.904572 H -4.401223 1.123238 1.790279 H -3.565262 1.430844 0.546274 O -2.819024 0.573501 -2.631730 H -3.002822 1.160088 -3.374593 H -2.751837 1.157826 -1.854060 O -0.883519 -1.488128 -2.392476 H -1.304784 -0.619093 -2.523949 H -1.119250 -1.995610 -3.177295 |
| Cellobiose-Bmim-4H2O C 3.699335 -2.628317 -0.319525 C 2.248178 -2.348455 -0.727123 C 2.611306 0.037386 -0.447667 C 4.052256 -0.198317 -0.036782 C 4.576647 -1.451661 -0.702606 H 2.182562 -2.315088 -1.829674 H 3.740463 -2.754386 0.776263 H 2.570339 0.254952 -1.534966 H 4.073622 -0.336954 1.060648 H 4.513635 -1.320017 -1.802633 O 4.195511 -3.761634 -0.986859 O 5.901826 -1.615293 -0.293496 H 6.234649 -2.430285 -0.691838 O 4.778181 0.934379 -0.425217 H 5.719630 0.726306 -0.333343 O 2.125270 1.091209 0.287485 O 1.809623 -1.105432 -0.172374 C 1.293318 -3.397852 -0.183652 H 1.633212 -4.390822 -0.511483 H 4.095863 -4.539941 -0.428731 O 1.263051 -3.379355 1.219035 H 1.252284 -2.452420 1.494294 H 0.296148 -3.220021 -0.620853 C 1.173823 1.960253 -0.290843 C 1.430724 3.372627 0.239576 C -0.849752 3.946315 0.109463 C -1.253002 2.558542 -0.372232 C -0.239022 1.513207 0.052561 H 1.358750 3.353261 1.345511 H 1.293565 1.976277 -1.391402 H -0.887191 3.973800 1.221124 H -1.254942 2.623531 -1.477106 H -0.293464 1.402544 1.151180 O -0.598015 0.296038 -0.574456 H 0.132563 -0.355250 -0.541278 O -2.510259 2.176591 0.112180 H -3.223654 2.487731 -0.474285 O -1.727477 4.832103 -0.463940 H -1.530777 5.723247 -0.150000 O 0.457590 4.230221 -0.315422 C 2.815475 3.915342 -0.117316 H 2.760625 5.005815 0.016944 O 3.817987 3.416304 0.706071 H 4.099866 2.548823 0.380332 H 3.007480 3.730762 -1.192023 C -4.121216 -2.543729 1.380630 C -5.117463 -2.369277 0.465183 C -3.223321 -1.744056 -0.457850 H -4.151591 -2.907383 2.403219 H -6.185068 -2.554857 0.530136 H -2.478382 -1.422883 -1.182946 N -2.950996 -2.156052 0.776617 N -4.530529 -1.875356 -0.676363 C -1.620663 -2.095147 1.388972 H -1.425096 -3.053562 1.889855 H -0.908330 -2.004161 0.559612 C -1.481058 -0.906993 2.329062 H -1.798501 -0.008936 1.778214 H -2.170169 -1.018217 3.182527 C -5.211400 -1.545675 -1.926383 H -4.448371 -1.269304 -2.662821 H -5.772440 -2.420460 -2.275355 H -5.873857 -0.685887 -1.774768 C -0.047954 -0.735804 2.824677 H 0.295794 -1.675830 3.289785 H 0.609273 -0.543763 1.956928 C 0.093443 0.406307 3.824770 H 1.138937 0.541156 4.130902 H -0.253877 1.358428 3.393808 H -0.503277 0.215927 4.728364 O -4.290078 0.512093 1.300723 H -4.853901 0.853372 2.004453 H -3.554552 1.146645 1.220984 O -2.295740 0.286331 -2.645705 H -2.147579 0.990626 -3.289272 H -1.662692 0.444153 -1.903241 O -0.523210 -1.851813 -2.318855 H -1.039555 -1.192590 -2.810442 H -0.464691 -2.615122 -2.905618 O -4.664243 1.427491 -1.349710 H -4.715095 1.008988 -0.472467 H -3.939607 0.959596 -1.793478 | Cellobiose-Bmim-5H2O C 2.831526 -3.137076 0.554165 C 1.484842 -2.597995 0.060933 C 2.379444 -0.345916 -0.012670 C 3.736608 -0.833708 0.453552 C 3.948563 -2.265365 0.008934 H 1.448881 -2.684231 -1.036844 H 2.859466 -3.094240 1.657323 H 2.350749 -0.319664 -1.119284 H 3.750634 -0.793277 1.559244 H 3.896755 -2.299575 -1.098593 O 3.053445 -4.444316 0.087005 O 5.207438 -2.658845 0.470181 H 5.335657 -3.583065 0.219530 O 4.693436 0.026045 -0.101637 H 5.564941 -0.366779 0.052442 O 2.157306 0.894620 0.535698 O 1.351911 -1.223400 0.449391 C 0.301577 -3.301722 0.692164 H 0.377153 -4.381951 0.502718 H 2.766209 -5.081412 0.749399 O 0.258072 -3.088089 2.080671 H 0.585787 -2.192454 2.241256 H -0.616246 -2.945328 0.190744 C 1.407453 1.836709 -0.199152 C 1.965160 3.227097 0.110034 C -0.145075 4.189749 -0.145657 C -0.829959 2.871421 -0.489144 C -0.075351 1.730921 0.158808 H 1.918854 3.397524 1.203966 H 1.522459 1.659108 -1.284072 H -0.167495 4.331107 0.958730 H -0.785765 2.757087 -1.587844 H -0.171479 1.816037 1.255207 O -0.632149 0.500741 -0.280668 H -0.078992 -0.248582 0.034745 O -2.168039 2.909293 -0.033739 H -2.505160 3.784799 -0.283774 O -0.866885 5.169603 -0.794821 H -0.502448 6.036831 -0.577024 O 1.178641 4.181151 -0.577960 C 3.422514 3.399878 -0.320068 H 3.607429 4.483926 -0.352931 O 4.316767 2.824987 0.574858 H 4.389331 1.875302 0.396286 H 3.537991 3.018948 -1.352938 C -4.877235 -1.582065 1.193679 C -5.372216 -1.857097 -0.047569 C -3.180537 -1.744468 -0.194823 H -5.380864 -1.440159 2.145275 H -6.392026 -2.000854 -0.391349 H -2.172029 -1.758644 -0.618635 N -3.508722 -1.529152 1.075345 N -4.292475 -1.961934 -0.892378 C -2.554163 -1.197447 2.135967 H -2.817382 -1.792944 3.021452 H -1.572413 -1.557280 1.800316 C -2.525704 0.293045 2.438957 H -2.449747 0.845618 1.490732 H -3.476854 0.595722 2.909294 C -4.327363 -2.223119 -2.326921 H -3.295627 -2.369047 -2.665197 H -4.916406 -3.127538 -2.518482 H -4.771560 -1.366203 -2.847517 C -1.355938 0.661433 3.346062 H -1.381190 0.052319 4.264265 H -0.413376 0.396646 2.832548 C -1.362551 2.143658 3.703627 H -0.459400 2.431056 4.258078 H -1.427423 2.762574 2.794703 H -2.233535 2.391366 4.327329 O -4.228748 1.066158 -0.438345 H -5.027482 1.405337 -0.020380 H -3.534403 1.725489 -0.241262 O 0.211245 0.715304 -3.052288 H -0.627034 0.937432 -3.483160 H -0.068747 0.501727 -2.146301 O 1.623942 -1.581225 -3.092815 H 1.305021 -0.693005 -3.352538 H 2.149605 -1.914585 -3.828824 O -2.472184 0.381597 -2.366816 H -3.377360 0.653756 -2.148354 H -2.018630 0.467551 -1.508745 O -0.925839 -1.950553 -2.117674 H -0.055025 -2.050451 -2.548000 H -1.358907 -1.220576 -2.587879 |
| Cellobiose-Bmim-6H2O C 2.218675 -3.517335 0.517293 C 0.982846 -2.739243 0.051806 C 2.272182 -0.691860 -0.018700 C 3.518421 -1.420592 0.444019 C 3.470087 -2.857332 -0.028524 H 0.916276 -2.809143 -1.046264 H 2.263492 -3.494337 1.619858 H 2.249889 -0.663897 -1.124795 H 3.536346 -1.403371 1.550092 H 3.405836 -2.860679 -1.136015 O 2.191085 -4.837840 0.034582 O 4.640462 -3.479653 0.412864 H 4.594063 -4.409315 0.153737 O 4.617427 -0.738010 -0.094729 H 5.399939 -1.294056 0.033832 O 2.280723 0.572948 0.522407 O 1.098813 -1.364363 0.444452 C -0.287528 -3.252845 0.698572 H -0.393971 -4.323118 0.467355 H 1.800944 -5.416398 0.698255 O -0.241833 -3.106601 2.094607 H 0.175153 -2.254649 2.281299 H -1.160301 -2.747955 0.247661 C 1.775905 1.642003 -0.248504 C 2.601910 2.892565 0.056311 C 0.752175 4.271487 -0.293545 C -0.190718 3.117701 -0.618057 C 0.298460 1.860837 0.067030 H 2.552798 3.099404 1.144108 H 1.880337 1.422056 -1.327449 H 0.733133 4.453262 0.804758 H -0.163883 2.972325 -1.713321 H 0.195315 1.995581 1.156282 O -0.488990 0.757997 -0.359407 H -0.094076 -0.084896 -0.045236 O -1.491489 3.444296 -0.174303 H -1.659311 4.348998 -0.482432 O 0.271825 5.357313 -0.994724 H 0.811895 6.133501 -0.799019 O 2.054905 3.966989 -0.682942 C 4.077944 2.751555 -0.316445 H 4.480055 3.774456 -0.369247 O 4.801428 2.036461 0.630256 H 4.698518 1.088348 0.458722 H 4.152540 2.320628 -1.333345 C -4.717184 -0.474295 1.716763 C -5.503546 -0.627184 0.613035 C -3.417479 -0.938081 0.005225 H -4.972970 -0.253625 2.748524 H -6.580921 -0.566114 0.494542 H -2.531451 -1.138734 -0.594868 N -3.420123 -0.684537 1.309299 N -4.668992 -0.921045 -0.439097 C -2.217009 -0.576717 2.132540 H -2.304415 -1.286369 2.967654 H -1.388288 -0.922930 1.502627 C -1.952531 0.844220 2.601907 H -1.962925 1.508130 1.721550 H -2.764958 1.181749 3.267359 C -5.065103 -1.196158 -1.816015 H -4.330905 -0.728469 -2.482278 H -5.068264 -2.279305 -1.978793 H -6.054171 -0.758926 -1.988303 C -0.616338 0.936594 3.334456 H -0.622758 0.253710 4.199886 H 0.188045 0.573882 2.668461 C -0.309302 2.354352 3.802963 H 0.682691 2.418472 4.269117 H -0.339524 3.065285 2.961707 H -1.051373 2.693807 4.539841 O -3.824042 1.952850 -0.249628 H -4.491488 2.394426 0.286031 H -3.019689 2.500613 -0.161136 O 0.267864 0.848100 -3.130399 H -0.530381 1.173226 -3.570619 H -0.031800 0.716679 -2.214638 O 1.361668 -1.597506 -3.120414 H 1.182791 -0.675807 -3.401232 H 1.782407 -2.041051 -3.865908 O -2.438359 0.878329 -2.327348 H -3.263729 1.332919 -2.097188 H -1.947238 0.917470 -1.486524 O -1.168489 -1.635633 -2.111426 H -0.299155 -1.762603 -2.546973 H -1.590923 -0.890815 -2.571159 O -3.095814 -3.421705 -1.285239 H -2.343504 -3.011731 -1.750046 H -2.944985 -4.371342 -1.329540 |  |