Supporting Information

Preparation of magnetic graphene photocatalytic nano-adsorbent for the sustainable removal of polycyclic aromatic hydrocarbons from aqueous solution

Qi Ying, Taiguang Li, Yongmei Hao *

School of Chemical Sciences, University of the Chinese Academy of Sciences, 19(A) Yu Quan Road, Beijing, 100049, China

Corresponding author at: School of Chemical Sciences, University of the Chinese Academy of Sciences, 19(A) Yu Quan Road, Beijing, 100049, China, PR China. Tel.: +86 10 88256414; fax: +86 10 88256093;

E-mail addresses: ymhao@ucas.ac.cn (Yongmei Hao);

Notes: The authors declare that there is no conflict of interests regarding the publication of this paper.

Fig. S1. XRD patterns (a), FTIR (b) and Raman spectrum (c) of as-prepared four samples.

Fig. S2. SEM images of MGS-1 (a), MGS-2 (b), MGS-3 (c), MGS-4 (d), (e) and MGS-5 (f).

Fig. S3. XPS spectra of MGST: survey scan (a), C 1s (b), Fe 2p (c), Si 2p (d), Ti 2p (e), and magnetic hysteresis loops of Fe3O4/MGST (f).

Fig. S4. The removal efficiencies of different adsorbents (a) and adsorption capacities of four adsorbents (b) for NAP.

Table S1 The element mass content ratio (%) of MGST

|  | C | O | Fe | Si | Ti |
| --- | --- | --- | --- | --- | --- |
| MGST | 73.98 | 17.87 | 0.69 | 5.22 | 2.23 |

Table S2 The concentration of related elements in solution (pH=2) for varied time.

| Day | Fe (ng ml-1) | Si (ng ml-1) | Ti (ng ml-1) |
| --- | --- | --- | --- |
| 0.5 | 0.134 | 0.023 | 0.151 |
| 1 | 0.278 | 0.035 | 0.337 |
| 3 | 0.569 | 0.076 | 0.683 |
| 5 | 1.028 | 0.152 | 1.096 |
| 7 | 1.673 | 0.241 | 1.752 |
| 10 | 2.512 | 0.493 | 2.55 |
| 15 | 3.741 | 1.134 | 3.326 |