Supporting Information

# Formation of Chlorate and Perchlorate during Electrochemical Oxidation by Magnéli Phase Ti4O7 Anode: Inhibitory Effects of Coexisting Constituents

Lu Wanga, b, Yaye Wangc, Yufei Suic, Junhe Lub, Baowei Hua, Qingguo Huangc, *

a School of Life Science, Shaoxing University, Shaoxing, 312000, China

b Department of Environmental Science and Engineering, Nanjing Agricultural University, Nanjing, 210095, China

c Department of Crop and Soil Sciences, University of Georgia, Griffin, GA 30223, USA

*Corresponding author:

E-mail: qhuang@uga.edu Telephone: +1-770-2293302

2 texts, 3 figures

Text S1

## Electrode fabrication and characterization

The Magnéli phase Ti4O7 electrode was fabricated through a high temperature sintering process as described in our previous study (H. Lin et al. Chemical Engineering Journal, 2018, 354,1058-1067). In brief, TiO2 powder was heated at 950 ◦C and reduced to Ti4O7 powder under controlled H2 flow. The Ti4O7 powder was mixed (0.5%, m/m) with polyacrylamide/polyvinyl alcohol (95/5, m/m) to form a slurry that was then spray-dried to form ceramic granulates. The ceramic granulates were then pressed to make a ceramic preform that was dried and then sintered at 1350 °C in a vacuum for 11 h to form a bulk electrode.

The chemical composition of the Magnéli phase Ti4O7 electrode was characterized using an X’Pert PRO MRD X-ray diffractometer (XRD) (PANalytical, Netherlands) with CuKα1 radiation at 40 kV/40 mA. The surface morphology of Ti4O7 electrode was examined using scanning electron microscopy (SEM) on a Hitachi’s-4800 FE-SEM system (Hitachi, Japan). The porosimetry analysis of the anode was measured using a Micromeritics Autopore IV 9500 mercury porosimeter (Norcross, GA) according to method ISO 15901-1.

The XRD pattern confirmed Magnéli phase Ti4O7 as the dominant composition of the electrode material (Fig. S3 A and B). The SEM image (Fig. S3 C) shows fairly uniform interconnecting pores with diameters smaller than 10 µm on the surface of Magnéli phase Ti4O7 anode material. Mercury intrusion porosimetry analysis (Fig. S3 D) indicates a porosity of 21.6%, and a median pore diameter of 3.6 μm (based on volume) or 2.8 μm (based on area), and an average pore diameter of 2.6 μm.

Text S2

UPLC-MS/MS Analysis

Formation of ClO3− and ClO4− were quantified using the ultra-high performance liquid chromatography and mass spectrometry (UPLC-MS/MS, Waters ACQUITY, Milford, MA). An ACQUITY UPLC BEH 1.7-micron C18 column (Waters, Milford, MA) was used for UPLC separation. The mobile phase consists of 50% water (A) and 50% MeOH (B) running at 0.3 mL min1. Electrospray ionization was operated in negative mode with the capillary voltage at 3 kV and the source temperature at 400 °C. ClO3− and ClO4− were quantified using multiple reactions monitoring (MRM) based on the transition m/z = 83 > 67 for ClO3−, and m/z = 99 > 83 for ClO4−. Quantification was achieved using a five-point calibration curve. The detection limits for ClO3− and ClO4− were 50.0 μg L1 and 25.0 μg L1, respectively, with an injection volume of 10.0 μL.

Fig. S1 The anodic potential on Ti4O7 in Na2SO4 solution with MeOH (a) and KI (b) spiked during the oxidation of Cl−. [Cl−]0= 1 mM, [Na2HPO4]= 100 mM, current density = 10 mA‧cm-2.

Fig. S2 Formation of ClO3− and ClO4− during the electrochemical oxidation of Cl− in the presence of H2O2 on Ti4O7 anodes. Conditions: [Cl−]0= 1 mM, [Na2HPO4] = 100 mM, current density = 10 mA‧cm-2.

Fig. S3 XRD data of Magnéli phase Ti4O7 electrode material (A) and reference Ti4O7 powder (B); SEM image of Ti4O7 electrode material (C); Result of mercury intrusion analysis of pore size distribution (D).