Experimental section

1.1. Materials

Hydrochloric acid (HCl), Nitric acid (HNO3), Glacial acetic acid (CH3COOH), Sodium hydroxide (NaOH), Ethanol (C2H5OH), 2,2,6,6-Tetramethyl-1-piperidinyloxy (TEMPO) and Sodium hypochlorite (NaClO) were purchased from Sigma Aldrich. Sodium chlorite (NaClO2), Gelatin (GT) and Urea were purchased from Shanghai Aladdin Biochemical Technology Co., Ltd. Bacterial cellulose Hydrogels (BC) was purchased from Guilin Qihong Technology Co., Ltd. Attapulgite (APT) was purchased from Dingbang Mineral Products Technology Co., Ltd. Sodium phosphate buffer solution is a mixture of sodium dihydrogen phosphate and disodium hydrogen phosphate. Dysprosium oxide was purchased from Shanghai Sinian Metal Materials Co., Ltd. The dysprosium nitrate (Dy(NO3)3) used in this study was prepared by dissolving dysprosium oxide with excessive concentrated nitric acid and reheating. The water used in this experiment was distilled water, and all reagents were not further purified unless otherwise specified.

1.2. Instruments

Scanning electron microscope (SEM, JEOL, Japan) was used to observe the surface morphology of the aerogels. Automatic specific surface and porosity analyzer (BET, ASAP 2460, USA) was used to analyze the specific surface area (SBET) of aerogels. The samples were tested by a Fourier transform infrared spectrophotometer (FT-IR, IS50, United States). Under N2 atmosphere, the aerogels were subjected to thermogravimetric analysis using a thermogravimetric analyzer (Q600-TGA/DSC, United States). The remaining concentrations of Dy(III), Nd(III) and Pr(III) were measured by Inductively coupled plasma atomic emission spectrometer (ICP-OES, Vista-AX, United States) at wavelengths of 353.17 nm, 401.22 nm and 417.94 nm, respectively.

1.3. Preparation of Samples

The synthesis of the BC aerogel: The BC aerogel was prepared after ultrasonic treatment of the BC hydrogel for 30 minutes and freeze-drying for 24 hours.

The synthesis of TEMPO-oxidized BC aerogel (OBC): 1.13 g of NaClO2 and 0.016 g of TEMPO were put into a flask containing 90 mL of sodium phosphate buffer solution (0.1M, pH=6.8) and mixed well. 16 g of BC wet gel was immersed in the above mixed solution, the flask was shaken at 40 ℃ for 30 minutes, and 1 mL of NaClO was added, and the bottle was immediately stoppered, and the flask was shaken at 40 ℃ for 5 hours. Then we added 5 mL of C2H5OH to stop the reaction and shaken at room temperature for 30 minutes. Then we washed the oxidized BC with deionized water. Finally, we immersed the oxidized BC in 0.05 M NaOH solution and shook for 1 hour, and we washed the oxidized BC with deionized water until the washing solution was neutral. The prepared OBC can be immersed in deionized water for storage before use. Finally, the OBC wet gel was freeze-dried to prepare aerogel.

The synthesis of APT-GT-OBC aerogel: 5 g of OBC hydrogel was immersed in 100 mL of a mixed solution of NaOH/urea/H2O with a ratio of 7:12:81 and stirred rapidly at -12°C. Then we heated 0.2 g of gelatin and poured it into the mixture, added 0.5 g of acidified and purified APT, and sonicated for 30 minutes. The mixture was freeze-thawed three times, with a freeze-thaw cycle of 12 hours at -20°C and 4 hours of room temperature thawing. After freezing and thawing, the complex was repeatedly washed by distillation until the NaOH and urea were removed and the washing solution was neutral. Finally, freeze-drying was performed to prepare the APT-GT-OBC aerogel.

The synthesis of imprinted APT-GT-OBC aerogel (I-APT-GT-OBC aerogel): In the above mixture of OBC hydrogel, gelatin and APT, we added 5 mg of Dy(NO3)3 and adjusted the pH value of the solution to 5.0, then we sonicated for 30 minutes and freezeed-thawed three times and freezed-dried to prepare the aerogel. The aerogel was transferred to the eluent with a volume ratio of glacial acetic acid to water of 1:9 and soaked for 48 hours to remove the template. Finally, the imprinted I-APT-GT-OBC aerogel was prepared by repeated washing with distilled water to remove the residual glacial acetic acid.

1.4. Adsorption experiment

Effect of pH on adsorption: Dy(NO3)3 was used to prepare a stock solution with Dy(III) concentration of 50 mg L-1. At room temperature, 10 mg of adsorbents were immersed in 10 mL of Dy(Ⅲ) stock solution with different pH (2.0 to 7.0) for 24 hours. The pH value was adjusted by 0.1 M NaOH and 0.1 M HCl. After the adsorption was completed, the mixture was centrifuged (10000 r min-1, 15 min) and the absorbents were removed using a 0.22 μm filter. The residual concentration of Dy(III) in the mixed solution was measured by the ICP-OES. The adsorption capacities Qt (mg g-1) were calculated by the following formula [1]:

|  | Qt=VC0-Ctm | (1) |
| --- | --- | --- |

Where C0 and Ct (mg L-1) are the initial concentration and the residual concentration of Dy(III) in mixed solution, respectively. V (L) is the volume of Dy(III) stock solution, and m (g) is the mass of aerogel.

Adsorption dynamics: At room temperature, 10 mg of adsorbents separately immersed in 10 mL of Dy(Ⅲ) stock solution (50 mg L-1, pH=4.0), separately. The residual concentrations of Dy(III) in mixed solution were determined at different contact times (0 minutes to 24 hours). We used the pseudo-ﬁrst-order kinetic model (PFOKM, equations (2)) and pseudo-second-order kinetic model (PSOKM, equations (3)) to fit the adsorption kinetic data, and then analyzed the adsorption mechanism [2].

| Qt=Qe-Qee-k1t | (2) |
| --- | --- |
| Qt=k2Qe2t1+k2Qet | (3) |

Where, Qt (mg g-1) and Qe (mg g-1) are the adsorption amount of aerogels at time t and equilibrium, respectively. k1 (min-1) and k2 (g mg-1 min-1) represent the rate constants of PFOKM and PSOKM, respectively.

Adsorption isotherms: At room temperature, 10 mg of adsorbents were immersed in the Dy(Ⅲ) stock solutions (10 mL, pH=4.0) with different initial concentrations (0, 25, 50, 100, 150 and 200 mg L-1). The residual concentrations of Dy(III) in the solution were determined after 24 hours. Langmuir (Eq. (4)) and Freundlich (Eq. (5)) models were used to fit the experimental equilibrium data [3].

| Qe=KLQmCe1+KLCe | (4) |
| --- | --- |
| Qe=KFCe1/n | (5) |

Ce (mg L-1) is the concentration of Dy(III) in solution at equilibrium, Qm (mg g-1) is the maximum adsorption capacity of aerogels for Dy(III). KL (L mg-1) is the Langmuir parameter denoted the energy of adsorption and affinity of binding sites. KF (mg g-1) is the Freundlich sorbent adsorption strength, while 1/n is the heterogeneity factors.

Adsorption thermodynamics: 10 mg of adsorbents were immersed in Dy(Ⅲ) stock solution (10 mL, pH=4.0) with different initial concentrations (25, 50, 100 mg L-1). Adsorption tests were carried out at 298.15 K, 308.15 K and 318.15 K, respectively. The residual Dy(III) concentration in the solution was determined after 24 hours. The values of Gibbs energy (∆G°) are calculated by equation Eq. (6) [4]:

| ∆G°=-RTlnK° | (6) |
| --- | --- |

Where thermodynamic equilibrium constant K° is calculated by plotting the function of ln(Cs/Ce) versus Cs. Wherein, Cs (mmol g-1) is the adsorption amount per gram of aerogels, and Ce is the concentration of Dy(III) in the mixed solution at adsorption equilibrium. R (8.314 J mol-1 K-1) is the universal gas constant, and T is the given temperature. Eventually, entropy (∆S°) and the enthalpy (∆H°) values are obtained from van’t Hoff equation Eq. (7) [5]:

| lnK°=∆SR-∆HRT | (7) |
| --- | --- |

Selective tests: 10 mg of the aerogels were immersed in 10 mL of mixed solution with coexisting system (Dy(III), Nd(III) and Pr(III) were provided by Dy(NO3)3, Nd(NO3)3 and Pr(NO3)3 respectively). The initial concentration of each cation was 50 mg L-1, and the pH value was adjusted to 5.0 with 0.1M HCl. The concentration in the mixed solution was measured 24 hours after the tubes were placed at 25℃. The selectivity of aerogels was evaluated by Kd (mL g-1). Relationships are listed as follow (Eq. (8)) [6]:

| Kd=VC0-CfmCf | (8) |
| --- | --- |

Where, C0 and Cf are the initial and final concentration of each rare earth ion, respectively. The C0 of each cation is 50 mg L-1.

Reusability tests: After the adsorption process has been over, the adsorbents were eluted, and the adsorbents were soaked in a 10% glacial acetic acid solution for 24 hours to remove the adsorbed Dy(III). Then at room temperature, these adsorbents (10 mg) were re-injected into the Dy(III) stock solution (10 mL, pH=4.0) for 24 hours, and the remaining concentration of Dy(III) in the solution was measured. The whole adsorption-desorption experiment was repeated five times. The reusability of the aerogels was verified by the changes of five adsorption capacities of the aerogels.

References

[1] Z. Mahdi, Q.J. Yu, A. El Hanandeh, Competitive adsorption of heavy metal ions (Pb2+, Cu2+, and Ni2+) onto date seed biochar: batch and fixed bed experiments, Sep. Sci. Technol. 54 (2018) 888-901.

[2] L. Wang, X. Zhao, J. Zhang, Z. Xiong, Selective adsorption of Pb(II) over the zinc-based MOFs in aqueous solution-kinetics, isotherms, and the ion exchange mechanism, Environ. Sci. Pollut. R. 24 (2017) 14198-14206.

[3] Y. Zhu, Y. Niu, H. Li, B. Ren, R. Qu, H. Chen, Y. Zhang, Removal of Cd(II) and Fe(III) from DMSO by silica gel supported PAMAM dendrimers: Equilibrium, thermodynamics, kinetics and mechanism, Ecotox. Environ. Safe. 162 (2018) 253-260.

[4] L. Zhang, L. Li, D. Shi, X. Peng, F. Song, F. Nie, Kinetics and mechanism study of lithium extraction from alkaline solution by HFTA and TOPO and stripping process using Lewis cell technique, Sep. Purif. Technol. 211 (2019) 917-924.

[5] X.D. Zheng, Y. Zhang, T.T. Bian, Y.Z. Zhang, Z.Y. Li, J.M. Pan, Oxidized carbon materials cooperative construct ionic imprinted cellulose nanocrystals films for efficient adsorption of Dy(III), Chem. Eng. J. 381 (2020) 10.

[6] D. Sun, Y. Zhu, M. Meng, Y. Qiao, Y. Yan, C. Li, Fabrication of highly selective ion imprinted macroporous membranes with crown ether for targeted separation of lithium ion, Sep. Purif. Technol. 175 (2017) 19-26.