1. Multispectral images of the whole “Prince Sattva Sacrifices Himself to the Starving Tigress” mural (A1–A4).

2. Multispectral references of the pigment samples

3. Sources of the pigment samples used for the multispectral references No.; Item Name; Main Phase; Chromogenic Phase; Chemical Formula of the Chromogenic Phase; Particle Size (µm); Source of Pigment. 1; Red earth; Quartz, Calcite, Albite, Chlorite, Hematite; Hematite; Fe2O3; <80; China-Tibet. 2; Cinnabar; Cinnabar, Calcite (trace amounts); Cinnabar; HgS; <20; China-Tibet. 3; Lac; ——; ——; C20H14O11; ——; Natural Pigments (USA). 4; Madder; ——; ——; ——; ——; Commercial (China). 5; Red lead; Red lead; Red lead; Pb3O4; 45; China-Tibet. 6; Realgar; Arsenic Sulfide; Arsenic Sulfide; As4S4; ——; China-Tibet. 7; litharge; litharge; litharge; PbO; ——; China-Tibet. 8; Orpiment; Orpiment; Orpiment; As2S3; ——; China-Tibet. 9; Yellow Ochre; Quartz, Muscovite, Albite, Lepidocrocite, Chlorite; Lepidocrocite; FeO(OH); 0–80; China-Tibet. 10; Gambogic; ——; ——; ——; ——; Commercial (China). 11; Turmeric; ——; ——; ——; ——; Commercial (China). 12; Amur cork; ——; ——; ——; ——; Commercial (China). 13; Malachite; Malachite; Malachite; CuCO3·Cu(OH)2; 79.7–99.3; China-Tibet. 14; Malachite; Malachite; Malachite; CuCO3·Cu(OH)2; 48.5–66.6; China-Tibet. 15; Malachite; Malachite; Malachite; CuCO3·Cu(OH)2; 11.5–32.8; China-Tibet. 16; Malachite; Malachite; Malachite; CuCO3·Cu(OH)2; 4.2–17.5; China-Tibet. 17; Atacamite; Atacamite, Malachite (small amounts); Atacamite, Malachite (small amounts); Cu2Cl(OH)3 Cu2(CO3)(OH)2; 0–80; KREMER Company (Germany). 18; Green earth; Quartz, Glauconite, Calcite; Glauconite; K(Fe,Al)2(Si,Al)4O10(OH)2; 0–120; China-Tibet. 19; Verdigris; ——; ——; Cu(CH3COO)2·[Cu(OH)2]3·2H2O; ——; KREMER Company (Germany). 20; Phthalo Blue; ——; ——; Fe4[Fe(CN)6]3; ——; KREMER Company (Germany). 21; Lapis lazuli; Lapis, Sodalite; Lapis, Sodalite; Na2O3Al6SiO2·2Na2S Na4Al3(SiO4)3Cl; 20; KREMER Company (Germany). 22; Azurite; Azurite, Quartz, Rosasite; Azurite, Rosasite; Cu3(CO3)2(OH)2 CuZn(CO3)(OH)2; 80–100; KREMER Company (Germany). 23; Azurite; Azurite, Quartz, Rosasite; Azurite, Rosasite; Cu3(CO3)2(OH)2 CuZn(CO3)(OH)2; 63–80; KREMER Company (Germany). 24; Azurite; Azurite, Quartz, Rosasite; Azurite, Rosasite; Cu3(CO3)2(OH)2 CuZn(CO3)(OH)2; <38; KREMER Company (Germany). 25; Azurite; Azurite, Quartz, Rosasite; Azurite, Rosasite; Cu3(CO3)2(OH)2 CuZn(CO3)(OH)2; <38; KREMER Company (Germany). 26; Ultramarine Blue; Ultramarine Blue; Ultramarine Blue; Na6Ca2Al6Si6O24(SO4)2; ——; KREMER Company (Germany). 27; Han Blue; Barium Copper Silicate; Barium Copper Silicate; BaCuSi4O10 BaCuSi2O6; 40; KREMER Company (Germany). 28; Han Purple; Barium Copper Silicate; Barium Copper Silicate; BaCuSi2O6; <40; KREMER Company (Germany). 29; Indigo; Indigo, quartz, albite; Indigo; C16H10N2O2; ——; KREMER Company (Germany). 30; Calcite; Calcite; Calcite; CaCO3; 20; KREMER Company (Germany). 31; Kaolin; Kaolinite, Quartz, Albite, Chlorite, Muscovite, Amphibole; Kaolinite; Al4Si4O10·(OH)8; ——; Commercial (China). 32; Talcum; Talc, Magnesite, Quartz, Chlorite; Talc, Magnesite; Mg6Si8O20(OH)4, MgCO3; ——; Commercial (China). 33; Plaster; Gypsum; Gypsum; CaSO4·2H2O; 0–80; KREMER Company (Germany). 34; White lead; White lead; White lead; PbCO3; ——; Commercial (China). 35; Zinc white; Zinc white; Zinc white; ZnO; 0.10–0.27; Commercial (China). 36; Carbon ink; ——; ——; C; ——; Commercial (China).