Polymeric microneedle-based platform enables simultaneous delivery of cancer immunomodulatory drugs and detection of biomarkers in the skin.

Pere Dosta1,2*, Núria Puigmal1,2*, Alexander M. Cryer1,2, Alma Lorena Rodríguez1,2, Ella Scott3, Ralph Weissleder3,4,5, Miles A. Miller3,4, Natalie Artzi1,2,6

1Institute for Medical Engineering and Science

Massachusetts Institute of Technology

Cambridge, MA 02139

2Department of Medicine

Division of Engineering in Medicine

Brigham and Women’s Hospital

Harvard Medical School

Boston, MA 02115

*E-mail: nartzi@mit.edu; nartzi@bwh.harvard.edu

3Center for Systems Biology

Massachusetts General Hospital Research Institute

Boston, MA 02114

*E-mail: miles.miller@mgh.harvard.edu

4Department of Radiology

Massachusetts General Hospital

Harvard Medical School

Boston, MA 02114

5Department of Systems Biology

Harvard Medical School

6Wyss Institute for Biologically Inspired Engineering

Harvard University

Boston, MA, 02115

Keywords: microneedles, immunotherapy, cancer, poly(beta-amino ester)s, theranostics

Figure S1: a, Chemical structure of HA-SS-NH2 polymer. b, 1H-NMR of HA-SS-NH2 Polymer (400MHz, DMSO-d6, TMS) (ppm)

Figure S2: HA-based MN platform for simultaneous transdermal drug delivery and Interstitial fluid Sampling for cancer treatment.  HA-based MN fabrication was performed by casting an aqueous amine-modified HA (HA-SS-NH2) solution into the PDMS mold by centrifugation and crosslinked using the NHS-terminated 8-arm PEG crosslinker. CpG Nanoparticles were loaded and a PLGA back layer was added (bottom scheme).

Figure S3: Synthesis of arginine modified poly (beta-amino) formulation. a, Synthesis of pBAE polymer. A mixture of 5-amino-1-pentanol, hexylamine, and  1,4-butanediol diacrylate (0.5:0.5:1.2) were used for the synthesis of pBAE C6 polymer. b, Arginine-modified pBAE are formulated mixing acrylate-terminate pBAE polymer with polyarginine peptide containing a cysteine amino acid (Cys-Arg-Arg-Arg).

Figure S4 a, Chemical structure of C6-CR3 Polymer. b, 1H-NMR of C6-CR3 Polymer (400MHz, Methanol-d4, TMS) (ppm): δ = 4.41-4.33 (br, NH2-C(=O)-CH-NH-C(=O)-CH-NH-C(=O)-CH-NH-C(=O)-CH-CH2-, 4.16 (t, CH2-CH2-O), 3.58 (t, CH2-CH2-OH), 3.25 (br, NH2-C(=NH)-NH-CH2-, OH-(CH2)4-CH2-N-), 3.04 (t, CH2-CH2-N-), 2.82 (dd, -CH2-S-CH2), 2.48 (br, -N-CH2-CH2-C(=O)-O), 1.90 (m, NH2-C(=NH)-NH-(CH2)2-CH2-CH-), 1.73 (br, -O-CH2-CH2-CH2-CH2-O), 1.69 (m, NH2-C(=NH)-NH-CH2-CH2-CH2-), 1.56 (br, -CH2-CH2-CH2-CH2-OH), 1.39 (br, -N-(CH2)2-CH2-(CH2)2-OH), 0.88 (t, CH2-CH2-CH3).

Figure S5: a, Agarose retardation assay of arginine-modified pBAE. Nanoparticles were formed using CpG and arginine-modified pBAE at different w/w ratios and loaded onto an agarose gel to assess CpG mobility by electrophoresis. b, Stability study of CpG-NPs in PBS (determined by DLS).

Figure S6: Cell viability profile of different concentrations of CpG-NPs and CpG-Crt-NP were analyzed 24 h post treatment. Samples were normalized to untreated cells. Data are represented as mean ± SD (n = 3).

Figure S7: Dose-response of the NF-kB response produced by CpG-NP and CpG-Crt-NP released from the MNs in mouse TLR9 Reporter HEK293 cell line (n = 4 biologically independent samples).

Figure S8: Mice body weight following CpG therapy. Mice with 20-40 mm3 orthotopic tumors were treated with empty microneedles or microneedles loaded with CpG-NPs five times, 3 days apart. Body weigh was measured every other day.

Figure S9: Macrophages gating strategy. Cells were extracted using microneedles.