Supplementary Information

Room temperature synthesis of water-soluble spherical particles of a uniform diameter

composed of carbon nanobelts and C60 molecules

Sieun Choi1,†, Shunji Kurosu2,†, Yuta Mashiko1,†, Takanobu Minakawa1

and Toru Maekawa1,2,*

1 Graduate School of Interdisciplinary New Science, Toyo University, 2100, Kujirai, Kawagoe, Japan

2 Bio-Nano Electronics Research Centre, Toyo University, 2100, Kujirai, Kawagoe, Japan

† Equal contribution as the first author

* Corresponding author: maekawa@toyo.jp

--------------------------------------------------------------------

H

C

Fig. 1	(6,6)carbon nanobelt.

Fig. 2	Solutions of (6,6)carbon nanobelts, C60 molecules and a mixture of (6,6)carbon nanobelts and C60 molecules dissolved in 1,2-dichlorobenzene. (a) (6,6)carbon nanobelts dissolved in 1,2-dichlorobenzene. The concentration of (6,6)carbon nanobelts is 0.70 µmol ml-1. (b) C60 molecules dissolved in 1,2-dichlorobenzene. The concentration of C60 is 0.70 µmol ml-1. (c) A mixture of (6,6)carbon nanobelts and C60 molecules dissolved in 1,2-dichlorobenzene. The concentrations of (6,6)carbon nanobelts and C60 are 0.35 µmol ml-1.

Fig. 3	Size distributions of particles formed by (6,6)CNBs and C60 molecules. The concentrations of (6,6)CNBs and C60 molecules are, respectively, 0.35 and 0.70 µmol ml-1. (a) 2 h after the mixture of the two solutions. The diameter of a particle is (4.63 ± 1.78) × 102 nm. (b) 3 h. (5.99 ± 0.38) × 102 nm. (c) 4 h. (6.19 ± 0.52) × 102 nm. (d) 24 h. (6.73 ± 0.47) × 102 nm. (e) 168 h. (7.12 ± 0.63) × 102 nm.

Fig. 4	Size distributions sand SEM images of particles formed by (6,6)CNBs and C60 molecules 168 h after the mixture of the two solutions. (a) The ratio of the molar concentration of CNBs to that of C60 molecules in 1,2-dichlorobenzene is 1 : 1 (the concentrations of (6,6)CNBs and C60 molecules are 0.35 µmol ml-1). The diameter of a particle is (6.10 ± 1.30) × 102 nm. (b) The ratio is 1 : 2 (the concentrations of (6,6)CNBs and C60 molecules are 0.35 and 0.70 µmol ml-1). (7.12 ± 0.63) × 102 nm. (c) The ratio is 1 : 3 (the concentrations of (6,6)CNBs and C60 molecules are 0.35 and 1.05 µmol ml-1). (7.71 ± 2.36) × 102 nm. The scale bars represent 5 µm.

Fig. 5	Absorption spectra by the supernatant of the solution. (6,6)CNBs and C60 molecules are dissolved in 1,2-dichlorobenzene. (a) Absorption spectra measured 168 h after the mixture of two solutions. The ratio of the molar concentration of CNBs to that of C60 is changed. (b) Time variation of the absorption spectra by the supernatant of the solution. The ratio of the molar concentration of CNBs to that of C60 is 1 : 2 (the concentrations of (6,6)CNBs and C60 molecules are 0.35 and 0.70 µmol ml-1).

Fig. 6	Absorption spectra by supernatant of the solution of (a) C60 molecules and (b) (6,6)CNBs dissolved in 1,2-dichlorobenzene.

Fig. 7	Snapshots of a suspension of particles formed by (6,6)CNBs and C60 molecules dispersed in distilled water. (a) The initial state; 0 h. (b) 8 h after dispersion. (c) 16 h. (d) 24 h. The arrows indicate the top of the solution.

Fig. 8	Time variation of the turbidity of the solution of particles dispersed in distilled water. The intensity of the transmitted light of 500 and 600 nm wavelength through the whole solution confined in a glass container was measured. The turbidity was defined as 1-ItransIin×100 %, where Iin and Itrans are, respectively, the intensities of the incident and transmitted light.

Fig. 9	Mass spectra of the components forming particles. The particles formed 168 h after the mixture of the two solutions are targeted. (6,6)CNBs are positively charged, whereas C60 molecules are negatively charged. (a) (6,6)CNBs. (b) C60.

Fig. 10	Compounds composed of (6,6)CNB and C60 molecules calculated by the PM6 method. (a) Compound formed by one (6,6)CNB and one C60 molecules; (6,6)CNB-C60. (b) Compound formed by one (6,6)CNB and two C60 molecules; (6,6)CNB-(C60)2. (c) Configuration of [(6,6)CNB-(C60)2]2. (d) Configuration of [(6,6)CNB-(C60)2]3.

Fig. 11	TEM image of a particle composed of (6,6)CNBs and C60 molecules. The particle was synthesized setting the molar concentration of (6,6)CNBs and C60 molecules, respectively, at 0.35 and 0.7 µmol ml-1. The scale bar represents 5 nm.

Video-1.mp4	Time variation of the precipitation process of the particles dispersed in distilled water from 0 up to 24 h. The arrow indicates the top of the suspension. Although the particles gradually precipitate due to their weight, they can be monodispersed again once the suspension is shaken (see Video-2.mp4).

Video-2.mp4	Monodispersibility of the particles in distilled water. The particles were forced to precipitate on the bottom of the microtube by centrifugation. The particles were monodispersed again in distilled water without any agglomeration by shaking the suspension by hand thanks to the high absolute value of the zeta potential of the particles.