The aging behavior of biochar and its immobilizing ability to heavy metals in rhizosphere

Jie Wanga, Lulu Zhaia, Xiyang Zhanga, Yuting Pana, Long Zhanga, Zhenguo Shenab, Yahua Chenabc*

a College of Life Sciences, Nanjing Agricultural University, Nanjing 210095, China

b Jiangsu Collaborative Innovation Center for Solid Organic Waste Resource, Nanjing Agricultural University, Nanjing 210095, China

c National Joint Local Engineering Research Center for Rural Land Resources Use and Consolidation, Nanjing Agricultural University, Nanjing 210095, China

Corresponding author: Yahua Chen; E-mail: yahuachen@njau.edu.cn;

Tel: +86-25-84396391; Fax: +86-25-84396542

- Formula

  - Eq. R50, biochar = T50, biochar /T50, graphite×100%, where T 50, biochar and T 50, graphite are the temperature values corresponding to 50% weight loss by oxidation of biochar and graphite, respectively (Harvey et al., 2012). T50, graphite is 844℃ (Yang et al., 2016)

1.2 Langmuir model was used to describe the isotherms: Ce / Qe= Ce / Qmax+1 / (KL Qmax) Eq. where Ce and Qe are the same above, Qmax (mg/g) is the max adsorption per gram of biochar, KL (min-1) are the rate constants of Langmuir sorption isotherm model (Quan et al., 2020).

References：

- Harvey, O. R., Kuo, L. J., Zimmerman, A. R., Louchouarn, P., Amonette, J. E., Herbert, B. E., 2012. An index-based approach to assessing recalcitrance and soil carbon sequestration potential of engineered black carbons (biochars). Environ. Sci. Technol. 46 (3), 1415−1421.

- Yang, F., Zhao, L., Gao, B., Xue, X., Cao, X., 2016. The interfacial behavior between biochar and soil minerals and its effect on biochar stability. Environ. Sci. Techn. 50(5): 2264-2271.

- Quan, G., Fan, Q., Cui, L., Zimmerman, A.R., Wang, H., Zhu, Z., Gao, B., Wu, L., Yan, J., 2020. Simulated photocatalytic aging of biochar in soil ecosystem: Insight into organic carbon release, surface physicochemical properties and cadmium sorption, Environ. Res. 183, 109241.

- Figure

Fig. S1 N2 adsorption-desorption isotherms of RH BC (A) and Sl BC (B) before and after aging. N-RA: aging in the non-rhizosphere; RA: aging in the rhizosphere; RH BC: rice husk biochar; Sl RH: sludge biochar.

Fig. S2 Effect of wheat roots and biochar on water dissolved nitrogen. The lower-case letters represent significant differences among treatments (p < 0.05). Error bars represent standard error (SE). RH BC: rice husk biochar; Sl BC: sludge biochar; Bulk soil: non-planting of wheat; Rhizosphere soil: planting of wheat (Simulated rhizosphere soil).

Fig. S3 The dry mass (A), Cd (B), Pb (C) and Zn (D) concentration of wheat in the different treatment treatments. The lower-case letters represent significant differences among treatments (p < 0.05). Error bars represent standard error (SE). RH BC: rice husk biochar; Sl BC: sludge biochar.

- Table

Table S1 The R50% of pristine and aged biochar

| Treatments | R50% | Treatments | R50% |
| --- | --- | --- | --- |
| Pristine Sl BC | 53.8 | Pristine RH BC | 67.1 |
| N-RA Sl BC | 54.2 | N-RA RH BC | 60.9 |
| RA-Sl BC | 52.8 | RA RH BC | 64.6 |

Note: N-RA: aging in the non-rhizosphere; RA: aging in the rhizosphere; RH BC: rice husk biochar; Sl BC: sludge biochar.

| Biochar sample | Cd2+ |  |  | Pb2+ |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Qmax (mg/g) | K1 (L/mg) | R2 | Qmax (mg/g) | K1 (L/mg) | R2 |
| PristineRH BC | 9.87 | 0.032 | 0.986 | 45.7 | 0.006 | 0.989 |
| N-RA RH BC | 9.11 | 0.037 | 0.971 | 75.7 | 0.003 | 0.998 |
| RA-RH BC | 14.43 | 0.020 | 0.986 | 140.0 | 0.002 | 0.997 |
| Pristine Sl BC | 6.5 | 0.043 | 0.990 | 57.8 | 0.004 | 0.995 |
| N-RA Sl BC | 8.5 | 0.031 | 0.992 | 57.3 | 0.004 | 0.999 |
| RA Sl BC | 26.1 | 0.010 | 0.995 | 140.4 | 0.002 | 0.996 |

Table S2 Parameters for Langmuir modelling

N-RA: aging in the non-rhizosphere; RA: aging in the rhizosphere; RH BC: rice husk biochar; Sl BC: sludge biochar.