Supplementary Information

for

“Giant enhancement of superconducting critical temperature in substitutional alloy (La,Ce)H9”

Jingkai Bi1, Yuki Nakamoto2, Katsuya Shimizu2, Bo Zou1, Mi Zhou1, Guangtao Liu1, *, Hongbo Wang1, *, and Yanming Ma1, 3, *

1State Key Laboratory of Superhard Materials and International Center of Computational Method & Software, College of Physics, Jilin University, Changchun 130012, China

2Center for Quantum Science and Technology under Extreme Conditions, Osaka University, Toyonaka, Osaka 560-8531, Japan

3International Center of Future Science, Jilin University, Changchun 130012, China

FIG. S1 Scanning electron microscopy image and energy-dispersive X-ray spectrum of the La-Ce alloy. Representative (a) scanning electron microscope (SEM) image of La-Ce alloy at 0 GPa and corresponding (b) energy-dispersive X-ray (EDX) spectrum from the area highlighted by the red rectangle in the SEM image.

Table. S1 Detailed parameters of the DACs used in the experiments.

| Number | Culet size (μm) | Gasket | Composition | Temperature (K) | Pressures (GPa) | Measurement |
| --- | --- | --- | --- | --- | --- | --- |
| #Cell-1 | 80 | Re+Al2O3/epoxy | La-Ce alloy+ NH3BH3 | 2100 | 110 | SC*, Run-1, XRD |
| #Cell-2 | 80 | Re+Al2O3/epoxy | La-Ce alloy+ NH3BH3 | 2200 | 97 | SC, Run-2 |
| #Cell-3 | 80 | Re+Al2O3/epoxy | La-Ce alloy+ NH3BH3 | 2100 | 85-115 | SC, Run-3 |
| #Cell-4 | 80 | Re+Al2O3/epoxy | La-Ce alloy+ NH3BH3 | 2300 | 110 | SC, Run-4, XRD, MF** |
| #Cell-5 | 80 | Re+Al2O3/epoxy | La-Ce alloy+ NH3BH3 | 2200 | 115 | SC, Run-5 |
| #Cell-6 | 60 | Re+Al2O3/epoxy | La-Ce alloy+ NH3BH3 | 2100 | 125-172 | SC, Run-6 |
| #Cell-S1 | 80 | Re+Al2O3/epoxy | La-Ce alloy+ NH3BH3 | 2100 | 115 | XRD |

* Superconductivity electrical transport measurement (SC).

** Transport measurements under varying external magnetic fields (MF).

Table. S2 Crystal structure information of (La,Ce)H9.

| Number | P (GPa) | Structure | Lattice parameter (Å) | Unit cell volume (Å3) |
| --- | --- | --- | --- | --- |
| #Cell-4 | 110 (experiment) | P63/mmc (La,Ce)H9 | a = 3.76 c = 5.68 | 34.80 |

FIG. S2 Phase analysis of the composition in Cell-S1 according to synchrotron X-ray diffraction (0.4131 Å) data. The weak peak marked with an asterisk may be from undetermined hydride impurity.

FIG. S3 Experimental equation of state (EOS) for different samples and calculated curves of LaH9, CeH9, and La0.5Ce0.5H9. Also shown for comparison are data on CeH9 were taken from work by Wuhao Chen, et al., Nilesh P. Salk et al., and Xin Li et al. reported in ref. [1-3].

FIG. S4 Superconducting transitions on warming cycle in Run-1.

FIG. S5 Superconducting transitions on warming cycle in Run-2.

FIG. S6 Superconducting transitions on warming cycles in Run-3.

FIG. S7 Superconducting transitions on warming cycle in Run-4.

FIG. S8 Superconducting transitions on warming cycle in Run-5.

FIG. S9 Superconducting transitions on warming cycles in Run-6.

Reference:

- Chen, W. et al. High-Temperature Superconducting Phases in Cerium Superhydride with a Tc up to 115 K below a Pressure of 1 Megabar. Phys. Rev. Lett. 127, 117001 (2021).

- Salke, N. P. et al. Synthesis of clathrate cerium superhydride CeH9 at 80-100 GPa with atomic hydrogen sublattice. Nat. Commun. 10, 4453 (2019).

- Li, X. et al. Polyhydride CeH9 with an atomic-like hydrogen clathrate structure. Nat. Commun. 10, 3461 (2019).